Compositional engineering of phase-stable and highly efficient deep-red emitting phosphor for advanced plant lighting systems

Jianwei Qiao1*, Dehong Li1, Qiufeng Shi1*, Haijie Guo1, Ping Huang1, Lei Wang1*

1College of Physics, Taiyuan University of Technology, Taiyuan 030024, P.R. China

Correspondence:

Jianwei Qiao (qiaojianwei@tyut.edu.cn)

Qiufeng Shi (shiqiufeng@tyut.edu.cn)

Lei Wang (wanglei_keke@163.com)

Fig. S1 Rietveld refinement results of O-NaMgPO4 XRD patern synthesized through arc-imaging furnace (a) and rapid quenching method (b) reported by Toda et al.1, 2 Obviously, there are impure phases in the samples using both synthesis methods.

Fig. S2 (a) XRD patterns of NaMgPO4:Eu synthesized by traditional high-temperature solid state and rapid quenching method, and the simulated standard card of O-NaMgPO4, G-NaMgPO4, and Na5.52Mg1.4(PO4)3. (b-f) Rietveld refinement results of Na1+xMgP1-xSixO4:Eu2+ (x = 0-0.08) X-ray powder diffraction pattern.

Fig. S3 (a) SEM images of the NaMgPO4:Eu microcrystal particles and the enlarged particles (b). (c) EDS elemental mapping of the cross section of NaMgPO4:Eu. (d) SEM images of the Na1.06MgP0.96Si0.04O4:Eu microcrystal particles and the enlarged particles (e). (f) EDS elemental mapping of the cross section of Na1.06MgP0.96Si0.04O4:Eu.

Fig. S4 EDX spectra of NaMgPO4:Eu (a) and Na1.06MgP0.96Si0.04O4:Eu (b). The detected mole ratio of Na, Mg, P elements is close to the stoichiometric ratio of NaMgPO4.

Fig. S5 (a) Raman spectra of NaMgPO4:Eu and Na1.06MgP0.94Si0.06O4:Eu samples. (b) Si-2p XPS binding energies of NaMgPO4:Eu, Na1.06MgP0.94Si0.06O4:Eu and Na1.08MgP0.92Si0.08O4:Eu.

Fig. S6 Emission spectra (a) and integration intensity of Na1+xMgP1-xSixO4:Eu2+ (x = 0-0.08) phosphors (b).

Fig. S7 The emission spectrum of the NaMgPO4:Eu2+ measured at low temperature 78 K and Gaussian fitting curves.

Fig. S8 Decay curves of Na1+xMgP1-xSixO4:Eu2+ (x = 0-0.08) measured at 300 K under 450 nm pulse laser diode excitation.

Fig. S9 The distortion indexes (a) and bond lengths (b) of NaO6, MgO6 and PO4 polyhedra in Na1+xMgP1-xSixO4:Eu2+ (x=0-0.08) depending on x values.

Fig. S10 (a) Diffuse reflection spectra of Na1+xMgP1-xSixO4:Eu2+ (x=0-0.08) phosphors (a) and NaMgPO4, Na1.06MgP0.94Si0.06O4 host (b). (c) The calculated energy gap by Tauc equation for NaMgPO4 and Na1.06MgP0.94Si0.06O4.

Fig. S11 Excitation line of BaSO4 and the emission spectra of the NaMgPO4:Eu (a) and Na1+xMgP1-xSixO4:Eu2+ (x = 0.02-0.08) phosphors (b) collected using an integrating sphere.

In this work, the quantum yield (QY) test was performed at room temperature by using a barium sulfate coated integrating sphere (150 mm in diameter) that attached to FLS1000. The internal quantum efficiencies (η) were calculated by using the following equations:

η=εα=LSER-ES

where ε is the number of photons emitted by the sample, and α is the number of photons absorbed by the sample. LS is the luminescence emission spectrum of the sample; ES is the spectrum of the light used for exciting the sample; ER is the spectrum of the excitation light without the sample in the sphere; and all the spectra were collected using the sphere.

Fig. S12 Band structure of NaMgPO4 (a) and Na1.06MgP0.94Si0.06O4 (b) host.

Fig. S13 O1s XPS spectra of NaMgPO4:Eu2+(a) and Na1.06MgP0.94Si0.06O4:Eu2+ (b).

Fig. S14 (a) The PL spectra of Na1.06MgP0.94Si0.06O4:Eu2+ when immersed in water for 0-365 days. (b) The PL spectra of the pristine Na1.06MgP0.94Si0.06O4:Eu2+ and the samples treated in degradation conditions at 80% relative humidity (RH) and 80 oC for different time, respectively.

Table S1 Main parameters of processing and refinement of the Na1+xMgP1-xSixO4:Eu (x = 0-0.08) samples.

| x | 0 | 0.02 | 0.04 | 0.06 | 0.08 |
| --- | --- | --- | --- | --- | --- |
| Sp. Gr. | Pnma | Pnma | Pnma | Pnma | Pnma |
| a, Å | 10.27008(18) | 10.26847(23) | 10.27376(15) | 10.27793(17) | 10.27195(16) |
| b, Å | 6.18430(10) | 6.18614(12) | 6.183361(87) | 6.18196(11) | 6.186442(93) |
| c, Å | 4.936995(86) | 4.93706(11) | 4.938817(74) | 4.939748(91) | 4.939643(80) |
| V, Å3 | 313.5648(93) | 313.613(12) | 313.7450(80) | 313.8603(96) | 313.8986(85) |
| Z | 4 | 4 | 4 | 4 | 4 |
| Rwp, % | 5.245 | 4.595 | 4.868 | 6.548 | 4.507 |
| Rp, % | 3.824 | 3.526 | 3.71 | 4.718 | 3.483 |
| Rexp, % | 2.838 | 2.843 | 2.840 | 2.873 | 2.891 |
| χ2 | 1.848 | 1.616 | 1.714 | 2.279 | 1.559 |
| RB, % | 2.682 | 2.125 | 2.252 | 3.867 | 2.259 |

Table S2 Fractional atomic coordinates and isotropic displacement parameters (Å2) of Na1+xMgP1-xSixO4:Eu (x = 0-0.08) samples.

| Atom | x | y | z | Biso | Occ. |
| --- | --- | --- | --- | --- | --- |
| x = 0 |  |  |  |  |  |
| Na | 0 | 0 | 0 | 0.698 | 1 |
| Mg | 0.28140(11) | 0.25 | 0.99838(27) | 0.2 | 1 |
| P | 0.10956(11) | 0.25 | 0.44465(19) | 0.469(27) | 1 |
| O1 | 0.11091(23) | 0.25 | 0.75769(41) | 0.2 | 1 |
| O2 | 0.46627(23) | 0.25 | 0.15088(40) | 0.2 | 1 |
| O3 | 0.17633(18) | 0.05264(25) | 0.31232(27) | 0.3503 | 1 |
| x = 0.02 |  |  |  |  |  |
| Na | 0 | 0 | 0 | 0.6978 | 1 |
| Nainsert | 0.06118(31) | 0.5630(37) | 0.0229(52) | 0.6978 | 0.01 |
| Mg | 0.28103(13) | 0.25 | 0.99998(33) | 0.2 | 1 |
| P | 0.11014(13) | 0.25 | 0.44488(24) | 0.577(35) | 0.98 |
| Si | 0.11014(13) | 0.25 | 0.44488(24) | 0.577(35) | 0.02 |
| O1 | 0.11700(29) | 0.25 | 0.75794(48) | 0.2 | 1 |
| O2 | 0.46615(28) | 0.25 | 0.15279(48) | 0.2 | 1 |
| O3 | 0.17632(23) | 0.05216(31) | 0.31105(34) | 0.3503 | 1 |
| x = 0.04 |  |  |  |  |  |
| Na | 0 | 0 | 0 | 0.6978 | 1 |
| Nainsert | 0.06205(23) | 0.5652(46) | 0.0234(36) | 0.6978 | 0.02 |
| Mg | 0.28163(11) | 0.25 | 0.99880(28) | 0.2 | 1 |
| P | 0.11002(11) | 0.25 | 0.44401(20) | 0.568(27) | 0.96 |
| Si | 0.11002(11) | 0.25 | 0.44401(20) | 0.568(27) | 0.04 |
| O1 | 0.11756(24) | 0.25 | 0.75427(41) | 0.2 | 1 |
| O2 | 0.46644(23) | 0.25 | 0.15241(40) | 0.2 | 1 |
| O3 | 0.17788(19) | 0.05180(26) | 0.30858(29) | 0.3503 | 1 |
| x = 0.06 |  |  |  |  |  |
| Na | 0 | 0 | 0 | 0.6978 | 1 |
| Nainsert | 0.0623(27) | 0.5668(35) | 0.0202(60) | 0.6978 | 0.03 |
| Mg | 0.28158(14) | 0.25 | 0.99768(35) | 0.2 | 1 |
| P | 0.10790(13) | 0.25 | 0.44265(26) | 0.557(33) | 0.94 |
| Si | 0.10790(13) | 0.25 | 0.44265(26) | 0.557(33) | 0.06 |
| O1 | 0.11462(31) | 0.25 | 0.74988(52) | 0.2 | 1 |
| O2 | 0.4600(30) | 0.25 | 0.14957(51) | 0.2 | 1 |
| O3 | 0.17690(24) | 0.05285(32) | 0.30557(32) | 0.3503 | 1 |
| x = 0.08 |  |  |  |  |  |
| Na | 0 | 0 | 0 | 0.6978 | 1 |
| Nainsert | 0.0621(17) | 0.5672(28) | 0.0205(45) | 0.6978 | 0.04 |
| Mg | 0.28191(10) | 0.25 | 0.99811(26) | 0.2 | 1 |
| P | 0.108041(99) | 0.25 | 0.44384(18) | 0.392(25) | 0.92 |
| Si | 0.108041(99) | 0.25 | 0.44384(18) | 0.392(25) | 0.08 |
| O1 | 0.12098(22) | 0.25 | 0.75518(38) | 0.2 | 1 |
| O2 | 0.46465(22) | 0.25 | 0.15137(37) | 0.2 | 1 |
| O3 | 0.17894(18) | 0.05108(24) | 0.30621(27) | 0.3503 | 1 |

Table S3 Main bond lengths (d, Å), volumes (V, Å3) and Distortion index (Dis) of NaO6, MgO6 and PO6 polyhedra in Na1+xMgP1-xSixO4:Eu (x = 0-0.08) crystal structure.

|  | Na-d (Å) | Na-V (Å3) | Na-Dis | Mg-d (Å) | Mg-V (Å3) | Mg-Dis | P-d (Å) | P-V (Å3) | P-Dis |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| x=0 | 2.3348 | 14.9496 | 0.0206 | 2.1525 | 12.3133 | 0.0297 | 1.5452 | 1.8802 | 0.0034 |
| x=0.02 | 2.3416 | 15.0593 | 0.0154 | 2.1428 | 12.1661 | 0.0298 | 1.5496 | 1.8981 | 0.0018 |
| x=0.04 | 2.3478 | 15.2077 | 0.0151 | 2.1402 | 12.1246 | 0.0283 | 1.5514 | 1.9046 | 0.0059 |
| x=0.06 | 2.3484 | 15.3905 | 0.0129 | 2.1376 | 12.0902 | 0.029 | 1.5586 | 1.9301 | 0.0126 |
| x=0.08 | 2.3559 | 15.4032 | 0.0128 | 2.1288 | 11.9356 | 0.0300 | 1.5641 | 1.9513 | 0.0123 |

Table S4 The crystal radii and ionic radii of Eu2+, Na+, Mg2+, P5+, Si4+ in the different fold of coordination.

| Ion | Coordination number | Crystal radii (Å) | Ionic radii (Å) |
| --- | --- | --- | --- |
| Na+ | 6 | 1.16 | 1.02 |
| Mg2+ | 6 | 0.86 | 0.72 |
| P5+ | 4 | 0.31 | 0.17 |
| Si4+ | 4 | 0.4 | 0.26 |
| Eu2+ | 6 | 1.31 | 1.17 |

Table S5 Luminescent decay times (τ1, τ2) and the fitting constants (A1, A2) of the fast and slow components, average decay times (τav) and standard error of τav. These decay times were measured by FLS1000 equipped with 450 nm pulse laser diode as excitation. All the datas were fitted by the Origin software.

| λex= 440 nm, Temperature = 300 K |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| x | A1 | τ1 | A2 | τ2 | τav (μs) | R2 |
| 0 | 15570.63 | 1.943 | 13019.06 | 2.582 | 2.27 | 0.9997 |
| 0.02 | 15160.08 | 2.128 | 10138.45 | 2.605 | 2.34 | 0.9998 |
| 0.04 | 19813.94 | 2.112 | 17565.382 | 2.713 | 2.43 | 0.9996 |
| 0.06 | 13078.69 | 1.851 | 13886.94 | 2.906 | 2.51 | 0.9997 |
| 0.08 | 25110.06 | 2.414 | 1219.99 | 4.923 | 2.58 | 0.9996 |
| λex= 440 nm, Temperature = 78 K |  |  |  |  |  |  |  |
| 0 | 40067.25 | 2.339 | 1227.36 | 4.426 | 2.45 | 0.9997 |
| 0.04 | 25412.04 | 2.373 | 1388.18 | 4.232 | 2.53 | 0.9998 |
| 0.08 | 40499.6 | 2.357 | 4225.87 | 4.083 | 2.62 | 0.9998 |

Average decay times are calculated by the following question:

τav=A1τ12+A1τ22A1τ1+A2τ2

Where A1 and A2 are the corresponding fitting constants; τ1, τ2 are lifetimes for the fast and slow components.

Table S6 Hirshfeld surface analysis calculates the NaO6 and MgO6 as the center, volume, surface area and the contribution of P-O and Si-O to the HS surface in Na1+xMgP1-xSixO4:Eu (x = 0-0.08).

|  | Na-V (Å3) | Na-A (Å2) | Na-[ P-O] (%) | Na-[O-Si] (%) | Mg-V (Å3) | Mg-A (Å2) | Mg-[P-O] (%) | Mg-[Si-O] (%) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| x=0 | 56.53 | 106.26 | 33.7 | 0 | 61.85 | 94.33 | 38.5 | 0 |
| x=0.02 | 56.82 | 106.65 | 22.1 | 12.3 | 61.70 | 93.92 | 12.0 | 26.5 |
| x=0.04 | 57.04 | 107.06 | 20.9 | 12.4 | 61.71 | 93.80 | 11.9 | 26.4 |
| x=0.06 | 57.29 | 107.47 | 20.7 | 12.5 | 61.80 | 93.77 | 11.6 | 26.2 |
| x=0.08 | 57.49 | 107.84 | 20.5 | 12.4 | 61.68 | 93.34 | 11.6 | 26.3 |

References

1. Kim, S. W. et al. Efficient red emission of blue-light excitable new structure type NaMgPO4:Eu2+ phosphor. ECS Solid State Lett. 2, R49 (2013).

2. Hasegawa, T. et al. Phase stabilization of red-emitting olivine-type NaMgPO4:Eu2+phosphorsviamolten-phase quenching. Inorg. Chem. Front. 7, 4040-4051 (2020).