# Tables

Table 1 Chemical composition of 17-4PH martensitic stainless steel (wt%)

| Elemental | C | Si | Mn | Ni | Cr | Cu | P | Fe |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Value | 0.04 | 0.6 | 0.3 | 4.32 | 16.39 | 3.4 | 0.023 | allowance |

Table 2 Main mechanical and physical propetries of 17-4PH martensitic stainless steel

| Heat treatment | Yield Strength σ0.2/MPa | Tensile Strength σb/MPa | Elongation δ5/% | Hardness HRC | Grain size |
| --- | --- | --- | --- | --- | --- |
| 1030° solution, 480° failure | 1235 | 1425 | 12 | 43 | Level 6 |

Table 3 Effect of tool orientation on ball end milling cutter wear

| Experiment No. | Inclination angle (°) | Rotational angle (°) | Lead angle (°) | Tilt angle (°) |
| --- | --- | --- | --- | --- |
| 1 | 5 | 60 | 2.51 | 4.33 |
| 2 | 15 | 60 | 7.63 | 13.07 |
| 3 | 25 | 60 | 13.12 | 21.99 |
| 4 | 45 | 60 | 26.57 | 40.89 |
| 5 | 65 | 60 | 47.00 | 61.70 |
| 6 | 15 | 0 | 15 | 0 |
| 7 | 15 | 120 | -7.63 | 13.07 |
| 8 | 15 | 180 | -15 | 0 |
| 9 | 15 | 240 | -7.63 | -13.07 |
| 10 | 15 | 300 | 7.63 | -13.07 |

Table 4 Effect of surface curvature on ball end milling cutter wear

| radius of curvature (mm) | Inclination angle (°) | Rotational angle (°) |
| --- | --- | --- |
| Convex 30 | 5、10、15、20、25 | 60 |
| Convex 50 | 5、10、15、20、25 |  |
| Convex 70 | 5、10、15、20、25 |  |
| Concave -30 | 5、10、15、20、25 |  |
| Concave -50 | 5、10、15、20、25 |  |
| Concave -70 | 5、10、15、20、25 |  |