List of Tables

Table.1. Chemical composition of the alloy (in wt.%).

| Elements | Cr | Mo | Ti | Ni |
| --- | --- | --- | --- | --- |
| Concentration | 45.0 % | 1.4 % | 0.13 % | Balance |

Table 2.  Values of domain size (Ds) and microstrain (εL) and dislocation density (ρ) for irradiated NiCrMo alloy irradiated at different doses.

| Sample | domain size (Ds) (±20 Å) | Change in domain size (Å) | dislocation density (ρ) (×1014 m-2) | Change in dislocation density (ρ) (×1014 m-2) |
| --- | --- | --- | --- | --- |
| Unirradiated | 356 | -- | 2.30 | -- |
| 1.5 dpa | 244 | 110 | 3.90 | 1.59 |
| 9.6 dpa | 160 | 196 | 5.19 | 2.88 |
| 33.9 dpa | 136 | 219 | 5.91 | 3.60 |

Table 3. Values of the critical indentation depth (hc), Nix Gao parameters, change in hardness (∆H) and hardening rate for unirradiated and irradiated NiCrMo samples.

| Samples | hc (nm) | H0 (GPa) | h* (nm) | ∆H (GPa) | Hardening rate (MPa/dpa) | Dislocation Density (1014 /m2) |
| --- | --- | --- | --- | --- | --- | --- |
| Unirradiated | -- | 2.48 | 266 |  |  | 5.8 |
| 1.5 dpa | 243 | 3.0 | 174 | 0.52 | 347 | 8.4 |
| 9.6 dpa | 238 | 3.35 | 143 | 0.87 | 193 | 10.5 |
| 33.9 dpa | 227 | 3.51 | 131 | 1.03 | 26 | 11.6 |