Table 1. The geometrical and mechanical properties of RSTF.

| Shape |  | Length (mm) |  | Diameter (mm) |  | Aspect Radio (Length /Diameter) |  | Tensile strength (MPa) |  | Specific gravity (Ton/m3) |  | Elastic modulus (GPa) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | 20 - 40 |  | 0.3 - 0.36 |  | 67 – 112 |  | 3120 |  | 6.9 |  | 210 |

Table 2. The geometrical and mechanical properties of STF.

| Shape |  | Length (mm) |  | Diameter (mm) |  | Aspect Radio (Length /Diameter) |  | Tensile strength (MPa) |  | Specific gravity (Ton/m3) |  | Elastic modulus (GPa) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | 35 |  | 0.4 |  | 87.5 |  | 2830 |  | 7.8 |  | 210 |