Supporting Information

Construction Of High Energy Density and Long Cycle Life Zinc-ion Hybrid Capacitors Based on Wedelia Chinensis-Derived Biomass Porous Carbon

Shenteng Wan, Letong Wang, Zengwei Pang, Tong Yao, Xiaohui Niu, Kunjie Wang*, Hongxia Li*

School of Petrochemical Engineering, Lanzhou University of Technology Lanzhou, 730050, P. R. China

* Corresponding author E-mail address: Wangkj80@lut.edu.cn, lhxwkj790425@lut.edu.cn

Figure 1. SEM images of (a) WPAC-2, (b) WPAC-4.

Figure 2. (a) XPS survey scan of WPAC-X. (b, d) C 1s spectra, (c, e) O 1s spectra of WPAC-2 and WPAC-4 samples, respectively.

Figure 3. (a, c) CV curves, (b, d) charge-discharge curves of WPAC-2 and WPAC-4 electrode materials, separately in three electrode system.

Figure 4. (a, c) CV curves, (b, d) charge-discharge curves of WPAC-2 and WPAC-4 electrode materials, separately in symmetrical capacitors.

Table S1 Specific surface area and pore structure data of samples

| Sample | SBET (m2 g-1) | Vt (cm3 g-1) | Average Pore width (nm) |
| --- | --- | --- | --- |
| WPAC-2 | 1619.964 | 0.76 | 2.21 |
| WPAC-3 | 2215.377 | 0.96 | 2.18 |
| WPAC-4 | 2030.457 | 0.931 | 2.31 |

Table S2 The XPS results of WPAC-X samples

| Samples | C1s(at%) |  |  |  | O1s(at%) |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | C=C | C-C | C=O | COOR | O=C | C-OH | COOH |  |
| WPAC-2 | 17.5 | 37.4 | 31.6 | 13.6 | 17.4 | 10.6 | 6.0 |  |
| WPAC-3 | 16.2 | 37.0 | 29.1 | 17.8 | 28.0 | 24.5 | 13.2 |  |
| WPAC-4 | 8.3 | 45.8 | 21.1 | 24.7 | 12.2 | 18.6 | 34.0 |  |