Supplementary Information

Title

Development and in vitro/in vivo evaluation of taste-masked orodispersible films of dapoxetine hydrochloride using ion exchange resins

Ying Zhoua, 1, Peng Yana, 1, Xiangcheng Zhaoa, Hailong Zhanga, b, Yan Yangb, Jinsong Dinga, *

aXiangya School of Pharmaceutical Sciences, Central South University, Changsha, Hunan 410006, China

bChangsha Jingyi Pharmaceutical Technology Co., LTD, Changsha, Hunan 410006, China

*Corresponding authors

E-mail addresses: dingjs0221@csu.edu.cn (Jinsong Ding).

ORCID: 0009-0001-0964-2558

1These authors contributed equally to this work.

Table S1 Formulations for screening of film-forming material types and amounts

| Ingredients | Formulations (%, w/w) |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | F1 | F2 | F3 | F4 | F5 | F6 | F7 | F8 | F9 | F10 | F11 | F12 |
| DRC | 50 | 50 | 50 | 50 | 50 | 50 | 50 | 50 | 55 | 45 | 40 | 35 |
| PEO | 45 | - | - | - | 40 | 36 | 30 | 22.5 | 35.6 | 44.4 | 48.9 | 53.3 |
| HPMC | - | 45 | - | - | 5 | 9 | 15 | 22.5 | 4.4 | 5.6 | 6.1 | 6.7 |
| PVA | - | - | 45 | - | - | - | - | - | - | - | - | - |
| PVP | - | - | - | 45 | - | - | - | - | - | - | - | - |
| Propylene Glycol | 4 | 4 | 4 | 4 | 4 | 4 | 4 | 4 | 4 | 4 | 4 | 4 |
| Sucralose | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 |

Table S2 Formulations for screening the type and amount of plasticizers and the amount of sweeteners

| Ingredients | Formulations (%, w/w) |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | F13 | F14 | F15 | F16 | F17 | F18 | F19 |
| DRC | 45 | 45 | 44 | 46 | 47 | 48 | 49 |
| PEO | 44.4 | 44.4 | 44.4 | 44.4 | 44.4 | 44.4 | 44.4 |
| HPMC | 5.6 | 5.6 | 5.6 | 5.6 | 5.6 | 5.6 | 5.6 |
| Propylene Glycol | - | - | 5 | 3 | 2 | 1 | 0 |
| Glycerol | 4 | - | - | - | - | - | - |
| Polyethylene glycol | - | 4 | - | - | - | - | - |
| Sucralose | 1 | 1 | 1 | 1 | 1 | 1 | 1 |

Table S3 Effect of plasticizer amounts on the appearance of ODF (n = 3)

| The content of plasticizer | Area of ODF with 30 mg dapoxetine |
| --- | --- |
| 0% | 7.51 ± 0.07 |
| 1% | 7.76 ± 0.08 |
| 2% | 8.06 ± 0.09 |
| 3% | 8.29 ± 0.13 |
| 4% | 8.51 ± 0.12 |
| 5% | 8.72 ± 0.09 |

All values represented mean ± SD.

Table S4 The content and uniformity of ODF

| Number | relative content （%） | Average relative content（%） | S | A+2.2S | L |
| --- | --- | --- | --- | --- | --- |
| 1 | 98.77 | 99.87 | 1.92 | 4.35 | 15.00 |
| 2 | 99.30 |  |  |  |  |
| 3 | 99.30 |  |  |  |  |
| 4 | 99.60 |  |  |  |  |
| 5 | 100.03 |  |  |  |  |
| 6 | 100.57 |  |  |  |  |
| 7 | 104.93 |  |  |  |  |
| 8 | 98.07 |  |  |  |  |
| 9 | 98.53 |  |  |  |  |
| 10 | 99.63 |  |  |  |  |

All values represented mean.

Fig S1. Appearances of ODF with different single film-form materials. Appearances of (A) F1 ODF, (B) F2 ODF, (C) F3 ODF, and (D) F4 ODF.

Fig S2. Appearances of ODF with different radio of PEO and HPMC. Appearances of (A) F5 ODF, (B) F6 ODF, (C) F7 ODF, and (D) F8 ODF.

Fig S3. Appearances of ODF at different the content of composite film forming material with a radio of PEO and HPMC of 8:1. Appearances of (A) F9 ODF, (B) F5 ODF, (C) F10 ODF, and (D) F11 ODF, and (E) F12 ODF.