Supplementary Information

Insight into the role of meso-Y zeolites in CsPMo/meso-Y composites on the selective oxidation of sulfides enhancement

Chang Sun1,3, Yutong Han1,3, Yingzhen Wei2, Zhong Zhang1, Xiaohui Li1, Guocheng Liu1, Xiuli Wang1,*

1College of Chemistry and Materials Engineering, Bohai University, Professional Technology Innovation Center of Liaoning Province for Conversion Materials of Solar Cell, Jinzhou 121013, P. R. China.

2State Key Laboratory of Inorganic Synthesis and Preparative Chemistry, College of Chemistry, Jilin University, Changchun 130012, P. R. China.

3These authors contributed equally.

*Corresponding author. E-mail address: wangxiuli@bhu.edu.cn.

Figure S1. SEM images of (a) meso-Y, (b) 3.3% CsPMo/meso-Y, (c) 4.6% CsPMo/meso-Y, (d) 6.0% CsPMo/meso-Y, (e) 7.5% CsPMo/meso-Y and (f) 9.3% CsPMo/meso-Y.

Figure S2. TEM images of (a) meso-Y and (b) 7.5% CsPMo/meso-Y.

Figure S3. N2 adsorption-desorption isotherms of (a) meso-Y, (b) 3.3% CsPMo/meso-Y, (c) 4.6% CsPMo/meso-Y, (d) 6.0% CsPMo/meso-Y, (e) 7.5% CsPMo/meso-Y and (f) 9.3% CsPMo/meso-Y.

Table S1. Physicochemical properties of meso-Y and X% CsPMo/meso-Y.

| Catalyst | Surface Area (m2/g) | Pore volume (cm3/g) | Average pore diameter (nm) | Mo (%)a |
| --- | --- | --- | --- | --- |
| meso-Y | 662 | 0.20 | 4.94 |  |
| 3.3% CsPMo/meso-Y | 546 | 0.15 | 3.06 | 1.72 |
| 4.6% CsPMo/meso-Y | 570 | 0.16 | 3.80 | 2.43 |
| 6.0% CsPMo/meso-Y | 569 | 0.13 | 3.40 | 3.10 |
| 7.5% CsPMo/meso-Y | 558 | 0.13 | 2.92 | 3.94 |
| 9.3% CsPMo/meso-Y | 557 | 0.16 | 4.74 | 4.86 |

aMeasured by ICP-OES analysis.

Figure S4. EDS images of 7.5% CsPMo/meso-Y. (a) Cs, (b) P, (c) Mo, (d) Si and (e) Al.

Figure S5. The images of (a) CsPMo, (b) 3.3% CsPMo/meso-Y, (c) 4.6% CsPMo/meso-Y, (d) 6.0% CsPMo/meso-Y, (e) 7.5% CsPMo/meso-Y and (f) 9.3% CsPMo/meso-Y.

Table S2. The molar ratio of MoVI/MoV in the X% CsPMo/meso-Y composites obtained by XPS.

| Catalyst | MoVI/MoV |
| --- | --- |
| 3.3% CsPMo/meso-Y | 5.14 |
| 4.6% CsPMo/meso-Y | 3.58 |
| 6.0% CsPMo/meso-Y | 3.46 |
| 7.5% CsPMo/meso-Y | 2.92 |
| 9.3% CsPMo/meso-Y | 3.31 |

Table S3. The polarity parameters of different solvents.

| Entry | Solvent | εa | π*b | ET(30)(kcal mol−1)c |
| --- | --- | --- | --- | --- |
| 1 | methanol | 32.7 | 0.586 | 55.4 |
| 2 | ethanol | 24.6 | 0.540 | 51.9 |
| 3 | n-propanol | 20.1 | 0.534 | 50.7 |
| 4 | n-butanol | 17.8 | 0.503 | 49.7 |
| 5 | n-pentanol | 13.9 | 0.400 | 49.1 |
| 6 | cyclohexane | 2.02 | 0 | 30.9 |

aε: dielectric constant.

bπ*: polarity/polarizability index.

cET(30): Dimroth-Reichardt’s polarity parameter.

Table S4. Results of selective oxidation of various sulfides in the presence of 7.5% CsPMo/meso-Y with TBHP as the oxidant.

| Entry | Substrate | Product | Con. (%) | Sel.d (%) |
| --- | --- | --- | --- | --- |
| 1a |  |  | 99.56 | 96.90 |
| 2a |  |  | 98.61 | 99.43 |
| 3b |  |  | 98.50 | 97.21 |
| 4a |  |  | 99.60 | 93.83 |
| 5b |  |  | 98.41 | 90.08 |
| 6b |  |  | 99.01 | 98.10 |
| 7c |  |  | 98.71 | 95.85 |

aReaction conditions: 10 mg 7.5% CsPMo/meso-Y, 0.5 mmol substrate, 1 mL ethanol, 0.58 mmol TBHP, 70 oC, 30 min.

bReaction conditions: 10 mg 7.5% CsPMo/meso-Y, 0.5 mmol substrate, 1 mL ethanol, 0.5 mmol TBHP, 60 oC, 30 min.

cReaction conditions: 10 mg 7.5% CsPMo/meso-Y, 0.5 mmol substrate, 1 mL ethanol, 0.65 mmol TBHP, 70 oC, 30 min.

dThe selectivity of sulfoxide, the byproduct is sulphone.

Figure S6. (a) PXRD patterns and (b) FTIR spectra of 7.5% CsPMo/meso-Y before and after the catalytic reaction.

Figure S7. EDS images of 7.5% CsPMo/meso-Y after the catalytic reaction. (a) Cs, (b) P, (c) Mo, (d) Si and (e) Al.

Figure S8. Raman spectra of 7.5% CsPMo/meso-Y before and after use.