Supplemental Materials

Specific heat analyses on optical-phonon-derived uniaxial negative thermal expansion system TrZr2 (Tr = Fe and Co1-xNix)

Yuto Watanabe1, Ceren Tayran2,3*, Md. Riad Kasem1, Aichi Yamashita1, Mehmet Çakmak4,5, Takayoshi Katase6, Yoshikazu Mizuguchi1*

1Department of Physics, Tokyo Metropolitan University, Hachioji, Tokyo 192-0397, Japan

2Department of Physics, Faculty of Science, Gazi University, 06500, Ankara, Turkey

3DIFFER–Dutch Institute for Fundamental Energy Research, De Zaale 20, 5612 AJ Eindhoven, The Netherlands

4Department of Photonics, Faculty of Applied Sciences, Gazi University, 06500, Ankara, Turkey

5Photonics Application and Research Center, Gazi University, 06500, Ankara, Turkey

6MDX Research Center for Element Strategy, International Research Frontiers Initiative, Tokyo Institute of Technology, Yokohama 226-8501, Japan

Corresponding authors: C. Tayran (c.tayran@gazi.edu.tr), Y. Mizuguchi (mizugu@tmu.ac.jp)

Figure S1 (a) XRD patterns of polycrystalline FeZr2 and Co1-xNixZr2 (x = 0, 0.2, 0.4, 0.6, 0.8, 1) with Cu-Kα radiation. (b) Nominal Ni amount (x) dependences of lattice constants a and c of Co1-xNixZr2. (c-d) Rietveld refinement results of FeZr2 and Co0.6Ni0.4Zr2, respectively. Impurity phase amounts of FeZr2 are in mass fraction.

Table S1. Actual compositions of FeZr2 and Co1-xNixZr2 (x = 0, 0.2, 0.4, 0.6, 0.8, 1) obtained from EDX.

| Tr | Co | Ni | Fe | Zr |
| --- | --- | --- | --- | --- |
| Fe | - | - | 0.80(3) | 2.20(3) |
| Co | 0.94(5) | - | - | 2.06(5) |
| Co0.8Ni0.2 | 0.75(2) | 0.174(6) | - | 2.07(2) |
| Co0.6Ni0.4 | 0.537(3) | 0.358(4) | - | 2.105(4) |
| Co0.4Ni0.6 | 0.357(6) | 0.52(1) | - | 2.12(1) |
| Co0.2Ni0.8 | 0.165(3) | 0.653(7) | - | 2.182(5) |
| Ni | - | 0.87(1) | - | 2.13(1) |

Figure S2 (a-b) SEM images with back scattering electron and elemental mapping images for FeZr2 and Co0.6Ni0.4Zr2, respectively. For FeZr2, we found a Fe-rich secondary phase (Fe2Zr) denoted as a solid arrow.