Supplementary Materials

Design van der Waals Layered Quantum Materials of MPd5I2 (M=Ga, In and 3d Transition Metals)

Niraj K. Nepal1, Tyler J. Slade1, Joanna M. Blawat2, Andrew Eaton3, Johanna C. Palmstrom2, Benjamin G. Ueland1,3, Adam Kaminski1,3, Robert J. McQueeney1,3, Ross D. McDonald2, Paul C. Canfield1,3# and Lin-Lin Wang1*

1Ames National Laboratory, U.S. Department of Energy, Ames, IA 50011, USA

2MAGLAB, Los Alamos National Laboratory, U.S. Department of Energy, Los Alamos, NM 87545, USA

3Department of Physics and Astronomy, Iowa State University, Ames, IA 50011, USA

#canfield@ameslab.gov

*llw@ameslab.gov

Figure S1. Phase stability and structural energies of MPd5I2 calculated in PBEsol. (a)-(j) are for MPd5I2 (M=Al, Ga, In, Ti, V, Cr, Mn, Fe, Co and Ni). The compounds on the ground state hull are labeled as green dots. The MPd5I2 are indicated with arrows and their respective hull energies are listed in parenthesis.

Figure S2. Electronic band structures of other MPd5I2 calculated in opt86b with spin-orbit coupling (SOC). The highest valence band (N) and band below (N-2) shown in red and blue, respectively. Green shade stands for I pz orbital projection. (a-g) are for MPd5I2 with M=Al, Ga, V, Mn, Fe, Co and Ni, where Al and Ga in (a-b)are non-magnetic, V and Mn in (c-d) are ferromagnetic, and Fe, Co and Ni in (e-g) are anti-ferromagnetic.

Figure S3. Electronic band structures of bulk and 1L TiPd5I2 calculated with spin-orbit coupling (SOC) using different exchange-correlation functionals. (a) Bulk in r2SCAN+rVV10, (b) bulk in mBJ, (c) 1L in r2SCAN+rVV10 and (d) 1L in HSE06 exchange-correlation functionals. The highest valence band (N) and band below (N-2) are shown in red and blue, respectively. Green shade stands for I pz orbital projection.

Figure S4. Electronic band structures of bulk and 1L InPd5I2 calculated with spin-orbit coupling (SOC) using different exchange-correlation functionals. (a) Bulk in r2SCAN+rVV10, (b) bulk in mBJ, (c) 1L in r2SCAN+rVV10 and (d) 1L in HSE06 exchange-correlation functionals. The highest valence band (N) and band below (N-2) are shown in red and blue, respectively. Green shade stands for I pz orbital projection.