Supplementary Materials for

Controllable Synthesis of Nonlayered Ultrathin Mn3O4 with High Dielectric Constant

Jiashuai Yuan1,2, Chuanyong Jian1, Zhihui Shang3, Yu Yao1, Bicheng Wang1, Yixiang Li1, Rutao Wang3, Zhipeng Fu1, Meng Li1,2, Wenting Hong1, Xu He1, Qian Cai1, Wei Liu1,4*

1CAS Key Laboratory of Design and Assembly of Functional Nanostructures, and Fujian Provincial Key Laboratory of Materials and Techniques toward Hydrogen Energy, Fujian Institute of Research on the Structure of Matter, Chinese Academy of Sciences, Fuzhou, Fujian, 350002, China.

2College of Chemistry and materials, Fujian Normal University, Fuzhou, Fujian, 350007, China.

3Shandong Provincial Key Laboratory of Processing and Testing Technology of Glass & Functional Ceramics, School of Material Science and Engineering, Qilu University of Technology (Shandong Academy of Sciences), Jinan 250353, China.

4Fujian Science & Technology Innovation Laboratory for Optoelectronic Information of China, Fuzhou, Fujian 350108.

*Corresponding author: liuw@fjirsm.ac.cn

Supplementary Fig. 1 | Schematic diagram of the CVD growth of Mn3O4 arrays. The precursors KCl and MnCl2·4H2O are placed in a quartz boat at the center of the heating zone, and a freshly cleaved natural mica substrate is placed above the quartz boat.

Supplementary Fig. 2 | EDS characterization of Mn3O4 nanoplates transferred onto a Cu grid. a-c EDS elemental maps of ultrathin vdW Mn3O4 nanoplates, revealing the uniform distribution of Mn and O elements. d Corresponding EDX spectrum of the Mn3O4 nanoplate, where the Cu signal originates from the Cu grid.

Supplementary Fig. 3 | EELS spectra of Mn3O4 nanoplates: a Mn L-edge and (b) O K-edge.

Supplementary Fig. 4 | XPS measurement spectrum of Mn3O4.

Supplementary Fig. 5 | Magnetism of Mn3O4 nanoplates. a Temperature-dependent magnetization of Mn3O4 nanoplates measured under an in-plane magnetic field of 0.1 T. b Hysteresis loops of Mn3O4 nanoplates measured under an in-plane magnetic field at temperatures ranging from 10 to 50 K.

Supplementary Fig. 6 | Schematic of the growth of ultrathin Mn3O4 nanosheets assisted by hydrates. a A sketch map illustrates the vertical and lateral growth of a new cluster (yellow) with n stacking subunits (lilac). The free energy change during vertical growth is primarily influenced by the interaction of subunits at the upper interface, whereas the lateral growth is significantly affected by the edge energy penalty. The symbols ΔEver and ΔElat indicate the free energy changes for vertical and lateral growth, respectively. The interaction energy between subunits n and n+1 is represented as εn, n+1. The average edge energies of the initial structure and the new cluster are denoted by λn and λB, respectively. AsB and AlB stand for the basal and lateral contact areas. b The balance between the ε term and the λ term is depicted. A smaller ε term favors lateral growth, while a smaller λ term encourages vertical growth. The circumstance correction terms for the interaction energy and edge energy are denoted by εc and λc, respectively.

Supplementary Fig. 7 | Tunability of the coverage and thickness of Mn3O4 nanoplate arrays on mica. a-f OM images of Mn3O4 nanoplates on mica for growth durations of approximately 3, 7, 10, 13, 17, and 20 minutes, respectively. g The change in coverage of Mn3O4 nanoplates with growth time. h The change in thickness of Mn3O4 nanoplates with growth time.

Supplementary Fig. 8 | Growth mechanism of Mn3O4 nanosheet on mica and sapphire, respectively. a, c Optical images of Mn3O4 nanosheets grown on mica and sapphire, respectively. The red line indicates the growth orientation of Mn3O4 nanosheets. b, d Lattice mismatch model of Mn3O4 grown on mica and sapphire, respectively. The low lattice mismatch between the nanostructured Mn3O4 and mica of 1.9% leads to the growth of arrays along a single orientation.

Supplementary Fig. 9 | AFM images of ultrathin Mn3O4 nanosheets of varying thicknesses on the same mica substrate. The image is composed of five single AFM images, displaying the height profile across the AFM images. Images and height profiles confirm the atomic flatness of the Mn3O4 nanosheets.

Supplementary Fig. 10 | Air stability of 5.5 nm thick Mn3O4 nanosheets on mica. AFM monitoring revealed negligible changes in the surface morphology of 5.5 nm thick Mn3O4 nanosheets after over a year of air exposure, indicating their excellent environmental stability.

Supplementary Fig. 11 | AFM characterization of Mn3O4 nanoplate arrays on mica. a-c AFM images of Mn3O4 nanoplates on mica for growth durations of approximately 10, 15, and 20 minutes, respectively. d Height profile of the Mn3O4 nanoplate in (a), corresponding to the dashed line in (a). The images and height profile confirm the uniform thickness of the Mn3O4 nanoplates in (a) and the controlled synthesis of high-quality uniform films.

Supplementary Fig. 12 | Determination of the dielectric constant of Mn3O4 at different thicknesses using dual-gated graphene FETs. a, b, e, h, k Schematics and optical images of dual-gated graphene (Gr) FETs with Mn3O4 top gate dielectrics of various thicknesses on SiO2/p-type Si (p-Si) substrates. c, f, i, l Total resistance of typical dual-gated graphene FETs as a function of Vbg for different Vtg values. Vds = 10 mV. d, g, j, m Relationship between the back gate Dirac point voltage of graphene FETs and Vbg, with the slope of the linear fit represented by the red solid line. The thicknesses of Mn3O4 are 39 nm (c, d), 35 nm (f, g), 21 nm (i, j), and 66 nm (l, m), respectively.

Supplementary Fig. 13 | Validation of the dielectric constant of Mn3O4 using dual-gated graphene FETs. a, b Schematic and OM image of a dual-gated MoS2 FET with a 48 nm Mn3O4 top gate dielectric on a SiO2/p-type Si (p-Si) substrate. c Dual-gated transfer curves of the MoS2/Mn3O4 FET at different back gate voltages (Vbg) from 0 to 12 V. d Threshold voltage Vth as a function of Vbg extracted from (c). Linear fitting yields a slope of -0.0044 and a high dielectric constant of ~149.

Supplementary Fig. 14 | Band structure and density of states (DOS) of Mn3O4. The band structure (left) shows a band gap of 4.21 eV. The DOS (right) indicates contributions from total states, oxygen (O), and manganese (Mn).

Supplementary Fig. 15 | Bandgap measurement of ultrathin Mn3O4. Low-loss electron energy loss spectroscopy (EELS) plot, with bandgap estimation provided by linear fitting.

Supplementary Fig. 16 | Leakage current density measurement of Mn3O4 at different thicknesses using dual-gated graphene FETs. a Schematic of a dual-gated graphene (Gr) FET with Mn3O4 top gate dielectric on a SiO2/p-type Si (p-Si) substrate. b Leakage current density of dual-gated (Gr) FETs with Mn3O4 of different thicknesses within the range of top gate voltages.

Supplementary Fig. 17 | Breakdown field strength of Mn3O4 at different thicknesses. a, c, e, g AFM images of Mn3O4 monolayers at various thicknesses. b, d, f, h Corresponding breakdown field strengths for Mn3O4 at different thicknesses. The breakdown field strength for samples of varying thicknesses is consistently maintained at around 10 MV/cm.

Supplementary Fig. 18 | Breakdown tests for Mn3O4 of different thicknesses. a Schematic of a metal/Mn3O4/graphene (MIM) structure. b-e OM images before and after breakdown corresponding to those in Supplementary Fig. 17.

Supplementary Fig. 19 | Extraction of hysteresis and DIBL values from transmission curves obtained from top-gated MoS2/Mn3O4 FETs (Fig. 4c, main text). a Transfer characteristics operated at different Vds to extract DIBL values. Vds = 0.1 V (purple) and 1.0 V (blue). The inset shows an OM image of a MoS2 FET with graphene acting as the top gate electrode. b Low DIBL value of approximately 20 mV/V extracted from (a). c Dual-sweep transfer characteristics obtained at Vds = 1.0 V for the same device in (a). d The hysteresis between forward and backward scans is about 5 mV.

Supplementary Fig. 20 | Comparison of modulation performance between top-gated Mn3O4 and back-gated SiO2 in MoS2 FETs. a, b Schematic and OM image of a dual-gated MoS2 FET with a 16 nm Mn3O4 top gate dielectric on a SiO2/p-type Si (p-Si) substrate. c, e Transfer characteristics (Ids-Vtg) curves controlled by top-gated Mn3O4 and back-gated SiO2 of few-layer MoS2 FETs. d, f Output characteristics (Ids-Vds) of the same device. Compared to back-gated SiO2 FET modulation performance, top-gated Mn3O4 exhibits a steeper subthreshold slope, lower operating voltage, and more saturated current density curves.

Supplementary Fig. 21 | Hysteresis measurements in MoS2 FETs. a, c Enlarged dual-sweep hysteresis transfer curves at different Vds, extracted from Supplementary Fig. 20c and e. b, d Hysteresis of Mn3O4/MoS2 FET and SiO2/MoS2 FET at different Vds.

Supplementary Fig. 20, Supplementary Fig. 21: The hysteresis characteristics of Mn3O4/MoS2 FETs were explored to study the charge trap states induced by Mn3O4 nanosheets and the SiO2 substrate. The hysteresis phenomenon is primarily used to assess the stability of FETs during operation, which is closely related to charge trapping and release associated with defects at the semiconductor channel, dielectric, and their interfaces.1 Considering the inert nature of the MoS2 surface, directly depositing traditional ultrathin oxide dielectrics on it poses certain challenges, as traps at the interface may lead to charge carrier trapping, release, and the accompanying Coulomb scattering phenomena.2 Furthermore, the surface roughness and defects of the dielectric layer significantly impact the electrical performance of the device and have a notable effect on the Ids-Vtg hysteresis.3 As shown in Supplementary Fig. 20, employing single-crystal dielectric Mn3O4 in 2D semiconductor FETs can effectively reduce the hysteresis. When traditional SiO2 is used as the back gate dielectric layer, double-scan hysteresis under different Vds conditions shows a significant increase. This is mainly attributed to the high-quality monocrystalline Mn3O4 and MoS2 forming a clean, defect-free vdW interface, effectively reducing the charge carrier scattering at the dielectric/channel interface. As shown in Supplementary Fig. 21, further observation of the enlarged transfer curves of the top-gate and back-gate FETs confirmed that using Mn3O4 can achieve hysteresis as low as 40 mV, which is a significant improvement compared to the performance when SiO2 is used. Recent studies have found that high-κ dielectrics impose a significant n-type doping effect on MoS2 via atomic layer deposition techniques, requiring larger negative top gate voltages to turn off the transistor.4 This doping effect stems from an imbalance of positive charges in the dielectric layer. In contrast, due to the atomically smooth surfaces between Mn3O4 and MoS2 contribute to the formation of a perfect vdW interface, with the doping effect of Mn3O4 on MoS2 being minimal, indicating very little net charge.

Supplementary Table 1. Integration of high-κ dielectrics on 2D semiconductors via van der Waals (vdW) assembly.

|  | t (nm) | Ebd (MV/cm) | κ | Hysteresis (mV) | EOT (nm) | ref. |
| --- | --- | --- | --- | --- | --- | --- |
| Sb2O3 | 40 | 2.7 | 11.5 | 500 | N/A | 5 |
| HfO2 | 16 | 8 | 11 | 800 | N/A | 6 |
| HfO2 | 3.37 | 16.5 | 16.8 | 10 | 1 | 7 |
| Ta2O5 | 13 | N/A | 15.5 | 30 | N/A | 8 |
| Al2O3 | 2.5 | 7.8 | 4.5 | 50 | N/A | 9 |
| ZrO2(ZrS2) | 1.4 | 7.22 | 19 | N/A | 0.29 | 10 |
| Y2O3 | 10-20 | 2 | 16.8 | 200 | N/A | 11 |
| HfO2/ Sb2O3 | 4/1 | 19.3 | 17.5 | N/A | 0.67 | 12 |
| HfS2(HfOx) | 3 | 9.33 | ~10 | 10 | N/A | 13 |
| Bi2SeO5 | 20 | 16 | 21 | N/A | 0.9 | 14 |
| SrTiO3 | 4~32 | 6.3 | 22~105 | N/A | 1 | 15 |
| Bi2SeO5 | 36 | >10 | 16.5 | 40 | N/A | 16 |
| β-Bi2SeO5 | 2.3 | N/A | 22 | 20-60 | 0.5 | 17 |
| CaF2 | 2 | 10 | 8.43 | 32 | <1 | 18 |
| h-BN | 32 | 7.8 | 3.5~3.8 | N/A | N/A | 19 |
| SrTiO3 | 16 | 5.75 | 17~20 | 47.5 | N/A | 20 |
| LaOCl | 23.8~39.3 | 11.3 | 10.8 | 0~30 | N/A | 21 |
| Mn3O4 | 39 | 13.2 | 237 | 5 | 0.57 |  |

Supplementary Table 2. Comparison of MoS2 mobility before and after Mn3O4 encapsulation.

| Device number | Measurement configuration | μ (W/O Mn3O4) (cm2/Vs) |  | μ (With Mn3O4) (cm2/Vs) | MoS2 thickness(nm) |
| --- | --- | --- | --- | --- | --- |
| 1 | Two-probe | 11.3 |  | 22.6 | 3.7 |
| 2 | Two-probe | 13.2 |  | 19.8 | 2.3 |
| 3 | Two-probe | 12.6 |  | 20.8 | 1.6 |
| 4 | Two-probe | 11.9 |  | 21.3 | 3.5 |

In dual-probe measurements, the mobility can be extracted from the Ids-Vbg plot, as shown in Fig. 5b. The mobility can be calculated using the formula:

Ids=WLμCSiO2(Vbg-Vth-Vds2)Vds

Where W, L, μ, CSiO2, and Vth represent the channel width, channel length, electron mobility, SiO2 area capacitance (1.21×10-8 F/cm2), and threshold voltage, respectively.

Supplementary Note 1 The bandgap is determined using Electron Energy Loss Spectroscopy (EELS)

The low-loss part of the EELS spectrum corresponds to the zero-loss peak of the probing beam. For wide bandgap semiconductors and dielectrics, following the zero-loss peak is a flat region (~zero intensity), after which the intensity sharply rises again at the energy of the material's bandgap. Therefore, low-loss EELS analysis can be utilized to measure the material's bandgap. Following the methodology in reference 22, 23, we apply a linear fitting approach to determine the bandgap. Analysis of the EELS spectrum shown in Supplementary Fig. 15 yields an estimated bandgap, Eg = 3.9 eV.

Supplementary References

[1] Amit, I. et al. Role of charge traps in the performance of atomically thin transistors. Adv. Mater. 29, 1605598 (2017).

[2] Guo, Y. et al. Charge trapping at the MoS2-SiO2 interface and its effects on the characteristics of MoS2 metal-oxide-semiconductor field effect transistors. Appl. Phys. Lett. 106 (2015).

[3] Geiger, M. et al. Effect of the degree of the gate‐dielectric surface roughness on the performance of bottom‐gate organic thin‐film transistors. Adv. Mater. Interfaces. 7, 1902145 (2020).

[4] Zou, X. et al. Dielectric engineering of a boron nitride/hafnium oxide heterostructure for high‐performance 2D field effect transistors. Adv. Mater. 28, 2062-2069 (2016).

[5] Liu, K. et al. A wafer-scale van der Waals dielectric made from an inorganic molecular crystal film. Nat. Electron. 4, 906-913 (2021).

[6] Zou, X. et al. Dielectric engineering of a boron nitride/hafnium oxide heterostructure for high‐performance 2D field effect transistors. Adv. Mater. 28, 2062-2069 (2016).

[7] Li, W. et al. Uniform and ultrathin high-κ gate dielectrics for two-dimensional electronic devices. Nat. Electron. 2, 563-571 (2019).

[8] Chamlagain, B. et al. Thermally Oxidized Two-dimensional TaS2 as a High-k Gate Dielectric for MoS2 Field-Effect Transistors. arXiv preprint arXiv:1808.08303 (2018).

[9] Cheng, L. et al. Sub-10 nm tunable hybrid dielectric engineering on MoS2 for two-dimensional material-based devices. ACS nano 11, 10243-10252 (2017).

[10] Jin, Y. et al. Controllable Oxidation of ZrS2 to Prepare High‐κ, Single‐Crystal m‐ZrO2 for 2D Electronics. Adv. Mater. 35, 2212079 (2023).

[11] Wang, L. et al. A general one-step plug-and-probe approach to top-gated transistors for rapidly probing delicate electronic materials. Nat. Nanotechnol. 17, 1206-1213 (2022).

[12] Xu, Y. et al. Scalable integration of hybrid high-κ dielectric materials on two-dimensional semiconductors. Nat. Mater. 22, 1078-1084 (2023).

[13] Luo, P. et al. Molybdenum disulfide transistors with enlarged van der Waals gaps at their dielectric interface via oxygen accumulation. Nat. Electron. 5, 849-858 (2022).

[14] Li, T. et al. A native oxide high-κ gate dielectric for two-dimensional electronics. Nat. Electron. 3, 473-478 (2020).

[15] Huang, J.-K. et al. High-κ perovskite membranes as insulators for two-dimensional transistors. Nature 605, 262-267 (2022).

[16] Zhang, C. et al. Single-crystalline van der Waals layered dielectric with high dielectric constant. Nat. Mater. 22, 832-837 (2023).

[17] Zhang, Y. et al. A single-crystalline native dielectric for two-dimensional semiconductors with an equivalent oxide thickness below 0.5 nm. Nat. Electron. 5, 643-649 (2022).

[18] Illarionov, Y. Y. et al. Ultrathin calcium fluoride insulators for two-dimensional field-effect transistors. Nat. Electron. 2, 230-235 (2019).

[19] Chen, T.-A. et al. Wafer-scale single-crystal hexagonal boron nitride monolayers on Cu (111). Nature 579, 219-223 (2020).

[20] Yang, A. J. et al. Van der Waals integration of high-κ perovskite oxides and two-dimensional semiconductors. Nat. Electron. 5, 233-240 (2022).

[21] Li, L. et al. Ultrathin Van der Waals Lanthanum Oxychloride Dielectric for 2D Field‐Effect Transistors. Adv. Mater. 2309296 (2023).

[22] Park, J. et al. Bandgap measurement of thin dielectric films using monochromated STEM-EELS. Ultramicroscopy 109, 1183-1188 (2009).

[23] Garvie, L. et al. Interband transitions of crystalline and amorphous SiO2: An electron energy-loss spectroscopy (EELS) study of the low-loss region. Solid State Commun. 106, 303-307 (1998).