Supporting Information

Structural, thermal and electrical properties of Na1+xAlxTi2-xP3O12 (x = 0.3) solid electrolytes

Ademola J. Adetona,1* Ge Wang,2 Ayorinde O. Nejo,3 Cheryl Shaw,4 Beatia In Siame1

1Department of Materials Science and Engineering, University of Sheffield, Sheffield, UK. S1 3JD.

2Department of Materials, University of Manchester, Manchester, UK. M13 9PL.

3Department of Chemistry, University of Lagos, Lagos State, Nigeria.

4Sorby Centre for Electron Microscopy, The University of Sheffield, Sheffield, UK. S3 7HQ.

Corresponding author: Ademola J. Adetona

Email: Adetonaademola077@gmail.com; Ajadetona1@sheffield.ac.uk

Table S1

The grain size distribution of the Na1.3Al0.3Ti1.7P3O12 green powder.

| Record Number | Sample Name | Dx (10) (μm) | Dx (50) (μm) | Dx (90) (μm) |
| --- | --- | --- | --- | --- |
| 1 | Na1.3Al0.3Ti1.7P3O12 | 1.46 | 6.89 | 15.30 |
| 2 | Na1.3Al0.3Ti1.7P3O12 | 1.43 | 6.87 | 15.20 |
| 3 | Na1.3Al0.3Ti1.7P3O12 | 1.41 | 6.85 | 15.20 |
| 4 | Na1.3Al0.3Ti1.7P3O12 | 1.40 | 6.84 | 15.20 |
| 5 | Na1.3Al0.3Ti1.7P3O12 | 1.38 | 6.82 | 15.00 |
| 6 | Na1.3Al0.3Ti1.7P3O12 | 1.37 | 6.80 | 14.90 |
| 7 | Na1.3Al0.3Ti1.7P3O12 | 1.36 | 6.80 | 14.90 |
| 8 | Na1.3Al0.3Ti1.7P3O12 | 1.36 | 6.80 | 14.90 |
| 9 | Na1.3Al0.3Ti1.7P3O12 | 1.36 | 6.83 | 15.20 |
| 10 | Na1.3Al0.3Ti1.7P3O12 | 1.35 | 6.80 | 14.90 |
| Mean |  | 1.39 | 6.83 | 15.10 |
| Std. Dev |  | 0.03 | 0.03 | 0.15 |

Figure S1. Thermogravimetry Analysis (TGA) plot of Na1.3Al0.3Ti1.7(PO4)3 as a function of Temperature.

Figure S2. Differential Scanning Calorimetry plot of Na1.3Al0.3Ti1.7(PO4)3 as a function of Temperature.