Supporting Information

for

Highly Tunable Flexible AgCu/Cotton Pressure Sensor using Surface Morphological Engineering for Enhanced Performance

Jiaojiao Zheng*, Tianyu Cao, Jianxiao Wang, Wenhao Xu, Yihan Qu, Jiafen Wang, Yunlong Wu, Yanyan Song, Lizhong He, Xudong Chen, Jie Yang*, Yinhu Qu

School of Materials Science and Engineering, Xi’an Key Laboratory of Textile Composites, Xi’an Polytechnic University, Xi’an 710048, PR China

*Email address: zhengjiaojiao@xpu.edu.cn

Supplementary Figures and Tables

Supplementary Fig.1 SEM image of the obtained Cu NWs.

Supplementary Fig.2 A jet of water (dyed with red ink) bounced off from the AgCu/cotton fabric.

Supplementary Fig.3 The electrical stability of the AgCu/cotton under HCl (a), NaOH (b), and NaCl droplets (c) on its surface. WCAs of the AgCu/cotton after immersed in different solutions for 5 min (d).

Supplementary Fig.4 Schematic illustrating the possible formation mechanism of AgCu nanosheets.

Supplementary Fig.5 Fabrication process of the AgCu/cotton sensor.

Supplementary Tab. 1 Comparison of select piezoresistive pressure sensors based on microengineered features.

| Structure | Structure fabrication method | Sensitivity (kPa-1) | Sensing Range | Waterproof-ness | Breath-ability | Ref. |
| --- | --- | --- | --- | --- | --- | --- |
| Interlocked micropillars | Silicon mold | 10.41 | <2.5 kPa | NR | NR | 12 |
| Hybrid porous | Epipremnum aureum leaf and sugar as template | 83.9 | <140 Pa | NR | NR | 16 |
| Microspinous | Abrasive paper template | 151.4 | 0~4.7 kPa | NR | NR | 20 |
| Random spinosum | Abrasive paper template | 25.1 | 0~2.6 kPa | NR | NR | 22 |
| Porous and surface pillars | NaCl powders and nonwoven fabric as template | 10.0805 | 1 Pa~1 kPa | NR | NR | 1 |
| Interlocked connection | Silicon wafer mold | 20.08 | 0.05−0.8 kPa | NR | NR | 2 |
| Interlocked nanocone array | AAO template | 268.36 | 0~200 Pa | NR | NR | 3 |
| Surface wrinkles and dome-like microstructure | Pre-strained VHB tape as substrate | 178 | 100-200 Pa | NR | NR | 4 |
| Microcone array | Plant leaf template | 528.87 | <2 kPa | NR | NR | 5 |
| Multiscale surface | Surface wrinkling and rose petal-template | 70 | <0.5 kPa | NR | NR | 6 |
| Wrinkled structure | Pre-stretched polyacrylate tape as substrate | 148.26 | 7-16 kPa | NR | NR | 7 |
| Irregular microdome | Internal popping of microspheres | 50.45 | 0-50 Pa | NR | NR | 8 |
| Hierarchical gradient protrusion | Dip-coating and galvanic replacement | 117 | 2-7.5 kPa | Yes | Yes | Our work |

Note: NR represent not reported.

Supplementary Tab. 2 Elemental contents of AgCu/cotton fabrics calculated by EDS results.

| Element (At%) | Samples |  |  |  |
| --- | --- | --- | --- | --- |
|  | AgCu/cotton-1 | AgCu/cotton-2 | AgCu/cotton-3 | AgCu/cotton-4 |
| C | 72.71 | 57.47 | 72.74 | 58.12 |
| N | 9.33 | 9.13 | 6.68 | 7.72 |
| Ag | 16.99 | 32.95 | 20.26 | 33.92 |
| Cu | 0.97 | 0.45 | 0.31 | 0.24 |

Supplementary References

[1] Li, W.; Jin, X.; Han, X.; Li, Y.; Wang, W.; Lin, T.; Zhu. Z. Synergy of Porous Structure and Microstructure in Piezoresistive Material for High-Performance and Flexible Pressure Sensors. ACS Appl. Mater. Interfaces 2021, 13, 19211-19220.

[2] Mao, Y.; Ji, B.; Chen, G.; Hao, C.; Zhou, B.; Tian, Y. Robust and Wearable Pressure Sensor Assembled from Ag NW-Coated PDMS Micropillar Sheets with High Sensitivity and Wide Detection Range. ACS Appl. Nano Mater. 2019, 2, 3196-3205.

[3] Lu, Y; He, Y.; Qiao, J.; Niu, X.; Li, X.; Liu, H.; Liu. L. Highly Sensitive Interlocked Piezoresistive Sensors Based on Ultrathin Ordered Nanocone Array Films and Their Sensitivity Simulation. ACS Appl. Mater. Interfaces 2020, 12, 55169-55180.

[4] Jia, J.; Huang, G.; Deng, J.; Pan. K. Skin-Inspired Flexible and High-Sensitivity Pressure Sensors Based on rGO Films with Continuous Gradient Wrinkles. Nanoscale 2019,11, 4258-4266.

[5] Yang, J.; Liu, L.; Zhang, D.; Zhang, H.; Ma, J.; Zheng, J.; Wang, C. Dual-Stage Surficial Microstructure to Enhance the Sensitivity of MXene Pressure Sensors for Human Physiological Signal Acquisition. ACS Appl. Mater. Interfaces 2024, 16, 1096-1106.

[6] Yu, S.; Li, L.; Wang, J.; Liu, E.; Zhao, J.; Xu, F.; Cao, Ya.; Lu. C. Light-Boosting Highly Sensitive Pressure Sensors Based on Bioinspired Multiscale Surface Structures. Adv. Funct. Mater. 2020, 30, 1907091.

[7] Yan, J.; Ma, Y.; Li, X.; Zhang, C.; Cao, M.; Chen, W.; Luo, S.; Zhu, M.; Gao. Y. Flexible and High-Sensitivity Piezoresistive Sensor Based on MXene Composite with Wrinkle Structure. Ceram. Int. 2020, 46, 23592-23598.

[8] Jung, Y.; Choi, J.; Lee, W.; Ko, J. S.; Park, I.; Cho. H. Irregular Microdome Structure-Based Sensitive Pressure Sensor using Internal Popping of Microspheres. Adv. Funct. Mater. 2022, 32, 2201147.