Supporting information

Intrinsically Anisotropic 1D NbTe4 for Self-Powered Polarization-Sensitive Photodetection

Huahu Luo1,#, Fafa Wu1,#, Chaowei He1, Wanfu Shen2, Chunguang Hu2, Weina Zhao3,*, Peng Yu1,*, Guowei Yang1

1State Key Laboratory of Optoelectronic Materials and Technologies, Guangzhou Key Laboratory of Flexible Electronic Materials and Wearable Devices, Nanotechnology Research Center, School of Materials Science and Engineering, Sun Yat-sen University, Guangzhou 510275, P.R. China

2 State Key Laboratory of Precision Measuring Technology and Instruments, Tianjin University, Tianjin 300072, P. R. China.

3School of Environmental Science and Engineering, Guangdong University of Technology, Guangzhou 510006, P. R. China

#These authors contributed equally to this paper

*e-mail: zhaowngd@gdut.edu.cn, yupeng9@mail.sysu.edu.cn

Fig. S1 The optical image of NbTe4 single crystals.

Fig. S2 The Raman mapping of NbTe4. a) The optical image of NbTe4. b-h) The Raman mapping at the 126.3, 138.8, 146.1, 157.5, 165.8 197.9 and 215.5 cm-1, respectively.

Fig. S3 Vibrational symmetry of phonon modes for NbTe4 along with their respective mode frequencies experimental results. The green and yellow spheres represent Nb and Te atoms, respectively.

Fig. S4 The contour plot of temperature-dependent Raman spectroscopy of NbTe4.

Fig. S5 Polar plots of Polar plots of Raman peak intensity with polarization angle at a) 126.3 cm-1, b) 146.1 cm-1, c) 157.7 cm-1, and d) 165.8 cm-1, respectively.

Fig. S6 a) ADRDM optical image of NbTe4 on an isotropic SiO2/Si substrate. b) Angle-dependence ADRDM results of NbTe4 in the area marked by the position 1 and (c) position 2 in a). d) ADRDM images of NbTe4 as a function of the rotation angle.

Fig. S7 Typical I-V curves under different power density at a) 532, b) 671 and c) 1064 nm, respectively.

Fig. S8 Time-resolved dynamic photoresponse curves under different power density under a)532 and b)1064 nm laser, respectively.

Fig. S9 Rise times and decay times under a) 532 and b) 1064 nm light, respectively.

Fig. S10 Angle-resolved photocurrents under different power density at 1064 nm.