Supplementary materials for

Interparticle Distance-Driven Diffusion Field Transforming Selectivity in Oxygen Reduction Reaction

Guangxing Yang,a,# Jie Chen, a,# Dongqin Liu, a Jiayu Yuan,b Zenan Wu,a  Zhiting Liu,a Qiao Zhang,a Hao Yu,b and Feng Penga,*

aSchool of Chemistry and Chemical Engineering, Guangzhou University, Guangzhou 510006 China

bSouth China University of Technology, Guangzhou 510641 China

# Authors contribute equally.

E-mail: fpeng@gzhu.edu.cn (F. Peng)

This PDF file includes:

Supplementary text

Supplementary Figures S1-8

Supplementary Table S1

Supplementary References

Supplementary text

Calculations

The ratio of distance between particles to particle size (δ=d/D) was used as a descriptor for the particle spacing effect.

ni represents the number of particles with a diameter of di, and the average particle size is calculated by the following formula:

D=i=1nnidi3i=1nnidi2

d represents the particle distance is calculated by the following formula:

d=ρD3Sc100-y63y

where,  represents the density of Pt, g nm⁻³.D represents the average particle diameter, nm. Sc is the specific surface area of the carbon support, nm² g⁻¹. y represents the mass fraction of metal in the Pt/C catalyst.

Catalysts were denoted as Ptδ, representing the Pt/C catalyst with a ratio of δ between particles to particle size.

Measurement of H2O2

In acidic conditions, cerium sulfate can undergo a redox reaction with hydrogen peroxide, described by the following mechanism:

2Ce4++H2O2→2Ce3++2H++O2↑

The orange-yellow Ce4+ is reduced to colorless and transparent Ce3+, leading to a change in the absorbance of the solution. Since Ce4+ has a maximum absorption at 320 nm, the concentration of hydrogen peroxide can be calculated according to the reaction quantitative relationship between cerium sulfate and hydrogen peroxide in solution.

Measurement of standard curves of data as shown in Table S1.

Figure S1. (a) Adsorption and desorption isotherms of N2 at 77 K; (b) BET surface area of each material.

Figure S2. XRD patterns of Ptδ materials

Figure S3.  XPS spectra of Ptδ materials

Figure S4. (top) Cyclic voltametric curves of Ptδ materials in the Ar-saturated HClO4 electrolyte at the scan rate of 50 mV s−1. (bottom) Linear scan curves of Ptδ materials in the O2-saturated HClO4 electrolyte at the scan rate of 10 mV s−1 from the positive to negative potential.

Figure S5.   Schematic of the GDE cell for H2O2 generation. (b) Calibration curve of absorbance with respect to H2O2 concentration.

Figure S6. Potential effect on the Nyquist plots of (a) Pt54, (b) Pt25, (c) Pt12, (d) Pt6.6 and (e) Pt5.9 at 1600 rpm with total catalyst loading of 20 μg in O2 bubbling electrolyte. (f) equivalent electric circuit.

Figure S7. Catalyst loading effect on the Nyquist plots of (a) Pt54, (b) Pt25, (c) Pt12, and (d) Pt5.9 at 1600 rpm in O2 bubbling electrolyte.

Figure S8. Ration rate effect on the Nyquist plots of (a) Pt54, (b) Pt25, (c) Pt12, and (d) Pt5.9 with total catalyst loading of 20 μg in O2 bubbling electrolyte.

Table S1 The concentration of the components of the standard solution

|  | CH2O2/mM | 1 mM Ce(SO4)2/mL | 0.5 M H2SO4/mL | 10 mM H2O2/μL |
| --- | --- | --- | --- | --- |
| 1 | 0 | 5.00 | 5.00 | 0 |
| 2 | 0.1 | 5.00 | 4.95 | 50 |
| 3 | 0.2 | 5.00 | 4.90 | 100 |
| 4 | 0.3 | 5.00 | 4.85 | 150 |
| 5 | 0.4 | 5.00 | 4.80 | 200 |