Inventory of Supporting Information

Fig. S1 Properties of halogen ions, Hofmeister series

Fig. S2 Coulombic efficiency of Zn||Cu asymmetric cell with different electrolytes by Aurbach’s method under the conditions (a) (1 mA cm-2, 5 mAh cm-2)+( 1 mA cm-2, 1 mAh cm-2)*10, (b) (5 mA cm-2, 10 mAh cm-2)+(5 mA cm-2, 5 mAh cm-2)*20

Fig. S3 Coulombic efficiency of Zn||Cu asymmetric cells in electrolytes with single anion addition (a) 2M+0.06M Cl-, (b) 2M+0.06M Br-, and (c) 2M+0.06M I- electrolytes

Fig. S4 Long-cycle performance of Zn||Zn symmetric cells with different electrolytes at 10 mA cm-2 and 5 mAh cm-2

Fig. S5 Average Coulombic efficiency of Zn||Cu asymmetric cells using different electrolytes at (a) 1 mA cm-2, 1 mAh cm-2, (b) 5 mA cm-2, 5 mAh cm-2, (c) 10 mA cm-2, 10 mAh cm-2, and (d) 10 mA cm-2 and 5 mAh cm-2

Fig. S6 Ex-situ XRD of stainless steel collector in cells using (a) baseline electrolyte and (b) HESE. (c) XRD pattern of zinc metal after 5 days of immersion in two electrolytes (inset is the optical photograph)

Fig.S7 The calculated configurational entropy (Sconf) (a) before and (b) after mixed

Fig. S8 Raman spectra fitting results of v-O-H portion (strong, medium, and weak H-bonds) in (a) 2M ZSO, (b) 1HESE, (c) HESE, (d) 3HESE, and (e) 5HESE

Fig. S9 The lifetime and the numbers of H-bonds of HESE and 2M ZSO

Fig.S10 Raman spectra fitting results of v-O-H portion (strong, medium, and weak H-bonds) in (a) 2M+0.06M Cl−, (b) 2M+0.06M Br−, and (c) 2M+0.06M I− electrolyte, (d) Statistical results

Fig. S11 3D snapshot and local amplification of MD simulations of 2M ZSO electrolyte system

Fig. S12 The coordination between Zn and each other atoms in HESE system

Fig. S13 (a) 3D snapshot and local amplification, (b) The coordination between Zn and I of 2M+0.06M I− electrolyte system

Fig. S14 Average Zn2+ cluster sizes in different electrolytes

Fig. S15 The pair distribution function (PDF) spectra of two electrolyte solutions

Fig. S16 EIS curves of Zn||Zn symmetric cells at different temperatures in (a) 2M ZSO and (b) HESE, and (c) the calculated activation energy (Ea)

Fig. S17 (a-b) EIS curves of two electrolytes at 25℃, Ionic conductivity at (c) 25℃ and (d) different temperatures

Fig. S18 Chronoamperograms (CA) and EIS curves in (a) 2M ZSO and (b) HESE, (c) the calculated transference number of Zn2+

Fig. S19 A summary of image snapshot with frontal view of the electrode-electrolyte interface in HESE system at (a) negative charge, (b) zero charge, and (c) positive charge in HESE, respectively.

Fig. S20 Density profiles for the Zn2+, Cl-, Br-, and I- as a function of distance from Zn anode with (a) zero charge, (b) negative charge, and (c) positive charge in HESE, respectively.

Fig. S21 CV curves of Zn||Zn symmertic cells in (a) 2M ZSO, (b) HESE, and the linear fits to calculate (c) Electrical double-layer capacitor (EDLC), (d) Differential capacitance curves of Zn||Ti half-cells in different electrolytes

Fig. S22 EIS and Distribution of relaxation times (DRT) fitting curves of Zn||Zn symmetric cell with (a-b) 2M ZSO, (b) HESE. (1): the relaxation of electrons, (2): the adsorption and desolvation process of Zn(H2O)62− at the interface, (3): the migration and crystallization of Zn ions on the electrode, (4): the charge transfer process across the interface, (5): ion diffusion.

Fig. S23 CV curves of Zn||Cu asymmetric cells in (a) 2M ZSO, (b) HESE, (c) 2M+0.06M Cl-, (d) 2M+0.06M Br-, and (e) 2M+0.06M I- electrolyte

Fig. S24 Chronoamperograms (CA) curves in different electrolytes under a overpotential of −150 mV

Fig. S25 Digital photographs of the initial nucleation and growth processes of zinc in two electrolytes

Fig. S26 Distribution and SEM micrographs of zinc deposition (5 mAh cm-2) on copper (Cu) substrate in two electrolytes

Fig. S27 SEM images of deposited zinc morphology obtained under different deposition condition

Fig. S28 Initial Raman full-spectra of (a) 2M ZSO and (b) HESE

Fig. S29 In-situ Raman spectra of the Zn/electrolyte interface in 2M ZSO electrolyte during (a) plating and (b) stripping

Fig. S30 In-situ Raman spectra of v-O-H at the Zn/electrolyte interface in (a) 2M ZSO and (b) HESE during stripping and plating

Fig. S31 Raman spectra fitting of the v-O-H portion, the proportion statistics of strong and weak H-bonds (S-H and W-H) in 2M ZSO electrolyte during (a) stripping and (b) plating

Fig. S32 Raman spectra fitting of the v-O-H portion, the proportion statistics of strong and weak H-bonds (S-H and W-H) in HESE during (a) stripping and (b) plating

Fig. S33 LSV curves of two electrolytes, inset is the overpotential

Fig. S34 (a) Digital photos of battery expansion using 2M ZSO electrolyte and thickness changes of a single battery over time, (b) The thickness of Zn||Zn symmetric cells assembled with two electrolytes varies with the working time, (c) The regional corresponding distribution of cell thickness and cycle time

Fig. S35 In situ pH test and device diagram during charge and discharge process

Fig. S36 Zn deposition voltage profiles of Zn||Cu cells at 10 mA cm-2. A-E and F-J are time nodes of different deposition capacities, which are used to observe the deposition morphology

Fig. S37 Cross-section SEM images of deposited zinc morphology

Fig. S38 Ex-situ XRD patterns of deposited zinc with increased area capacity in (a) 2M ZSO and (b) 2HESE, (c) Proportion change of I(002)/I(100)

Fig. S39 The rate performance of Zn||Zn symmetric cells with areal capacity of (a) 1 mAh cm-2 and (b) 10 mAh cm-2

Fig. S40 The long-cycle performance of Zn||Zn symmetric cells at (a) 1 mA cm -2 and 1 mAh cm-2, (b) 10 mA cm -2 and 10 mAh cm-2 (DOD=34.2%)

Fig. S41 Long cycle performance and time-voltage curves of Zn||Zn symmetric cell using HESE under 10 mA cm-2, 1 mAh cm-2

Fig. S42 Comparison of cyclic reversibility in the recent reports.

Fig. S43 The Coulombic efficiency of Zn||Cu asymmetric cells under 40 mA cm-2, 10 mAh cm-2

Fig. S44 Comparison of CEs and CPC of Zn||Cu cells in the recent reports.

Fig. S45 Comparison of CD and CPC of Zn||Ti cells in the recent reports.

Fig. S46 XRD pattern of NaV3O8 (NVO) powder

Fig. S47 Digital photos and SEM images of high-loading (~19 mg cm-2) cathode electrodes and mapping of key elements

Fig. S48 Long cycle performance of Zn||NVO full cells with different electrolytes

Fig. S49 Cross-section SEM images of high-loading (~37.0 mg cm-2) cathode electrodes and mapping of key elements

Fig. S50 (a) CV curves at various scan rates, (b) The relations between peak current and scan rates of Zn||NVO full cell using HESE electrolyte

Fig.S51 EIS curves of Zn||NVO full cell after different cycles using (a) 2M ZSO and (b) HESE

Fig. S52 Comparison of self-discharge performances in Zn||NVO full cell with (a) 2M ZSO and (b) HESE evaluated by resting for 48, 72, 96 h at 100% state of charge (SOC), respectively

Fig. S53 Digital photo of Ah-level multi-layer pouch cell material

Table S1 CEs test results of different electrolytes

Table. S2 The types of solvation structures and their corresponding proportion in 2M ZSO electrolyte system

Table. S3 The types of solvation structures and their corresponding proportion in HESE system

Table. S3-2 Classified statistics

Table S4 Electrostatic potential and forming energy of main Zn solvation structure

Table S5. Performance comparison of symmetric Zn||Zn cells from the previously reported works involving electrolyte additives and our work

Table S6. Performance comparison of Zn||Cu cells from the previously reported works involving electrolyte additives and our work

Table S7. Performance comparison of Zn||Ti cells from the previously reported works involving electrolyte additives and our work

Table S8. Performance comparison of full cells from the previously reported works involving electrolyte additives and our work

Table S9. Battery design parameters for zinc ion full cell based onZn||NVO in HESE

Table S10. COSTING. Summary of prices of various reagents of one coin cell. Price data of all this were collected from Internet (https://www.alibaba.com/)

Supplementary References