Supporting information

Free radical scavenging polylactic acid fibers: A study of melt spinning preparation, characterization, and properties

Chenghui Zheng,1 Huanling Wu,1 Qingqing Zhou,1 Lingfang Wang,2 Jingchun Lv1 and Haiyan Mao 1 *

1 Department of Light-Chemical Engineering, College of Textiles and Clothing, Yancheng Institute of Technology, Yancheng, 224051, China

2 Department of Polymer and Composite Materials, College of Materials Science and Engineering, Yancheng Institute of Technology, Yancheng, 224051, China

*Corresponding author:

Email: mao-hai-yan@hotmail.com

Number of Tables: 3

Number of Figures: 5

TABLE S1. Tensile characteristic values of PLA/PEO/CUR fibers

| Code | Material | Tenacity /cN dtex-1 | Elongation at break /% | Initial modulus /cN dtex-1 |
| --- | --- | --- | --- | --- |
| M0 | PLA100 | 2.24 ± 0.22 | 12.1 ± 0.7 | 1.09 ± 0.08 |
| M1 | PLA/PEO-8/CUR-5 | 2.65 ± 0.14 | 41.3 ± 6.5 | 0.88 ± 0.03 |
| M2 | PLA/PEO-8/CUR-10 | 2.82 ± 0.13 | 35.2 ± 5.4 | 0.98 ± 0.02 |
| M3 | PLA/PEO-12/CUR-5 | 2.94 ± 0.16 | 58.6 ± 9.7 | 0.83 ± 0.03 |
| M4 | PLA/PEO-12/CUR-10 | 3.14 ± 0.02 | 47.6 ± 11.8 | 0.89 ± 0.02 |
| M5 | PLA/PEO-8 | 2.48 ± 0.12 | 53.9 ± 7.1 | 0.79 ± 0.02 |
| M6 | PLA/PEO-12 | 2.75 ± 0.13 | 83.5 ± 12.3 | 0.72 ± 0.02 |

TABLE S2. Crystallinity and crystallite size of PLA/PEO/CUR fibers

| Code | Material | 2θ of main crystalline peak/ º | Crystallinity /% | Crystallite size /nm |
| --- | --- | --- | --- | --- |
| M0 | PLA100 | 16.0 | 13.5 | 1.4 |
| M1 | PLA/PEO-8/CUR-5 | 16.2 | 22.0 | 2.9 |
| M2 | PLA/PEO-8/CUR-10 | 16.5 | 23.5 | 4.2 |
| M3 | PLA/PEO-12/CUR-5 | 16.5 | 26.6 | 6.5 |
| M4 | PLA/PEO-12/CUR-10 | 16.4 | 28.2 | 8.1 |

TABLE S3. Characteristic points of TG-DTA curves of PLA/PEO/CUR fibers

| Code* | Tg /℃ | Tc /℃ | Tm /℃ | Tonset /℃ | Tmax /℃ | Tdecom. /℃ | Tfinal /℃ | Residuals /% |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| M0 | 60.4 | 103.6 | 180.8 | 349.5 | 367.2 | 372.2 | 380.0 | 0.72 |
| M1 | 58.7 | 102.0 | 169.0 | 337.0 | 362.2 | 367.8 | 378.1 | 1.49 |
| M2 | 57.0 | 100.1 | 169.5 | 337.8 | 360.3 | 365.3 | 377.6 | 1.52 |
| M3 | 55.7 | 101.7 | 168.5 | 336.2 | 364.1 | 368.9 | 378.0 | 1.43 |
| M4 | 55.1 | 101.0 | 169.0 | 336.7 | 361.2 | 367.8 | 377.2 | 1.78 |

* M0, PLA100; M1, PLA/PEO-8/CUR-5; M2, PLA/PEO-8/CUR-10; M3, PLA/PEO-12/CUR-5; M4, PLA/PEO-12/CUR-10.

Characteristic points were obtained based on references. [1], [2]

FIGURE S1. XRD patterns of PLA/PEO/CUR fibers. Intensity was normalized for visible convenience. The main broad peak in M0 indicated quite low crystallinity because of mostly amorphous phase of PLA.

FIGURE S2. Broad XPS spectra of PLA/PEO/CUR fibers. a, PLA100; b, PLA/PEO-12; c, PLA/PEO-12/CUR-10.

FIGURE S3. TG-DTA curves of the composited fibers. (a) TG curves. The embedded figure depicted detailed inflection from 310 ℃ to 355 ℃. (b) DTA curves. Tonset, Tg , and Tm were obtained by determining intersections of two tangent lines from each curve.

| Code* | 14 days | 45 days -1 | 45 days-2 |
| --- | --- | --- | --- |
| M0 |  |  |  |
| M1 |  |  |  |
| M2 |  |  |  |
| M3 |  |  |  |
| M4 |  |  |  |

* M0, PLA100; M1, PLA/PEO-8/CUR-5; M2, PLA/PEO-8/CUR-10; M3, PLA/PEO-12/CUR-5; M4, PLA/PEO-12/CUR-10.

FIGURE S4. Microscopic images of PLA/PEO/CUR fiber surfaces after 14, 45 days (different magnification for 45 days) in soil at 50 ℃, 55% R.H. Fiber surfaces before buried in soil (0 days) were pictured in Figure 3, a ~ b.

| Code* | 0 days | 14 days | 45 days |
| --- | --- | --- | --- |
| M0 |  |  |  |
| M1 |  |  |  |
| M2 |  |  |  |
| M3 |  |  |  |
| M4 |  |  |  |

* M0, PLA100; M1, PLA/PEO-8/CUR-5; M2, PLA/PEO-8/CUR-10; M3, PLA/PEO-12/CUR-5; M4, PLA/PEO-12/CUR-10.

FIGURE S5. Photos of PLA/PEO/CUR fibers before (0 days) and after 14, 45 days in soil at 50 ℃, 55 % R.H.

REFERENCES

[1]	Zhou H, Green TB, Joo YL (2006) The thermal effects on electrospinning of polylactic acid melts Polymer 47: 7497. https://doi.org/10.1016/j.polymer.2006.08.042

[2]	Hutchinson JM (2009) Determination of the glass transition temperature Journal of Thermal Analysis and Calorimetry 98: 579. https://doi.org/10.1007/s10973-009-0268-0