Supplementary materials

Field verification of low-level biochar applications as effective ameliorants to mitigate cadmium accumulation into Brassica campestris L from polluted farmland soil

Youchi Zhanga, Jiajun Fana, Shanna Lina, Brian J. Reida.b, Frédéric Coulonc, Chao Caia*

a Key Lab of Urban Environment and Health, Institute of Urban Environment, Chinese Academy of Sciences, Xiamen, 361021, China

b School of Environmental Sciences, University of East Anglia, Norwich, NR4 7TJ, UK

c School of Water, Energy and Environment, Cranfield University, Cranfield MK43 0AL, UK

* Corresponding author

Address: Key Lab of Urban Environment and Health, Institute of Urban Environment, Chinese Academy of Sciences, 1799 Jimei Road, Jimei District, Xiamen, 361021, Fujian, China

E-mail: ccai@iue.ac.cn

S1 Set-up of Cd adsorption experiment

The characterization of Cd adsorption capacity of three biochars was conducted in the laboratory. In brief, the biochar was mixed with Cd(NO3)2 solution at the ratio of 50 mg : 5 mL, and shaken at 25 °C at 150 rpm for 48 hours. Thereafter the suspensions were passed through 0.22 µm filters, and the concentrations of Cd2+ ion measured by the ICP-OES. The initial concentrations of Cd2+ were 0 mg/L, 25 mg/L, 50 mg/L, 100 mg/L, 150 mg/L, 200 mg/L, and 250 mg/L, respectively, and the initial solution pH were set to 5.0±0.2. In some treatments, the initial solution pH was set to 3.0±0.2 or 4.0±0.2. Metal adsorption onto biochars was fitted using Langmiur and Freundlich isotherm.

Table S1 Fitted isotherms for Cd2+ adsorption onto three biochars

|  | Langmuir isotherm |  |  | Freundlich isotherm |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Q0 (mg/g) | b | R2 | Kf (mg/g) | 1/n | R2 |
| PM biochar | 33.3 | 0.02 | 0.86 | 2.74 | 0.43 | 0.94 |
| RS biochar | 43.5 | 0.14 | 0.95 | 8.55 | 0.34 | 0.93 |
| RH biochar | 24.4 | 0.007 | 0.90 | 0.37 | 0.68 | 0.93 |

Table S2 Relationship among concentrations of soil available Cd and Cd accumulation in plants

| Amendment | Relationship |
| --- | --- |
| PM biochar | Cedible=21.9 Csoil+268 (R2=0.995, p<0.05) |
|  | Croot=17.0 Csoil+380 (R2=0.985, p=0.077) |
|  | Cedible=1.26 Croot-202 (R2=0.964, p=0.121) |
| RS biochar | Cedible=32.3 Csoil+40.9 (R2=0.978, p=0.096) |
|  | Croot=33.7 Csoil+18.0 (R2=0.995, p<0.05) |
|  | Cedible=0.97 Croot+20.5 (R2=0.992, p=0.059) |
| RH biochar | Cedible=19.8 Csoil+313 (R2=0.972, p=0.106) |
|  | Croot=44.2 Csoil-203 (R2=0.692, p=0.375) |
|  | Cedible=0.28 Croot+514 (R2=0.530, p=0.481) |

Fig. S1 The SEM image of three biochars. Top left, PM biochar; Top right, RS biochar; Bottom left, RH biochar.

Fig. S2 Infrared spectra of PM, RS and RH biochars.

Fig. S3 Dry weight of rape plants grown in soil and soil amended with biochars. “*” indicates a value to be significantly different to the control (CK) value (p < 0.05). Like uppercase letters indicate no significant difference (p > 0.05) between groups with biochar amendment at like application rates.

Fig. S4 Final pH of batch equilibrium experiments where initial pH was 3, 4 and 5. Uppercase letters indicated significantly (p < 0.05) different final pH for a given biochar where initial pH was different; lowercase letters indicate significantly (p < 0.05) different final pH between biochars where the initial pH was the same.

References

Liu Y, He Z, Uchimiya M (2015) Comparison of biochar formation from various agricultural by-products using FTIR spectroscopy. Modern Appl Sci 9(4): 246.

Singh B, Fang Y, Johnston CT (2016) A fourier-transform infrared study of biochar aging in soils. Soil Sci Soc Am J 80(3): 613.

Zolfi Bavariani M, Ronaghi A, Ghasemi R (2019) Influence of pyrolysis temperatures on FTIR analysis, nutrient bioavailability, and agricultural use of poultry manure biochars. Commun. Soil Sci Plan 50(4): 402-411.