Supporting Information

Comparative study of biochar modified with different functional groups for efficient removal of Pb(II) and Ni(II)

Chengchen Liua#, Jiaxin Linb,c#, Haojia Chenb,c, Wanjun Wangb,c*, Yan Yanga,b,c*

a School of Environmental and Safety Engineering, Changzhou University, Jiangsu, 213164, China

b School of Environmental Science and Engineering, Institute of Environmental Health and Pollution Control, Guangdong University of Technology, Guangzhou, 510006, Guangdong, China

c Synergy Innovation Institute of GDUT, Shantou, 515041, Guangdong, China

#These authors contributed equally to this work.

*Corresponding author:

E-mail address: Prof. Wanjun Wang, wanjun@gdut.edu.cn; Prof. Yan Yang, yangyan1209@gdut.edu.cn.

Characterizations

The microscopic surface textures of the samples were examined by field emission scanning electron microscopy (S-3400N, S-570, Hitachi, Japan). The crystal structure of each biochar was examined by X-ray diffraction (D8 Advance, Bruker Co., Japan) analysis at 45 kV and with 100 mA CuKα radiation. Fourier transform-infrared spectroscopy was conducted to characterize the functional groups on the as-obtained biochar samples. The specific surface area of each test material was measured using a specific surface area and pore size analyzer (3H-2000PS2, Beijing). In the static volume method, 99.999% N2 was used as the adsorbate and the saturated vapor pressure was 1.0360 bar. Before sampling, all samples were degassed at 150°C under vacuum for 240 min to remove the substances adsorbed on the sample surfaces. The multipoint Brunauer–Emmett–Teller adsorption isotherm was employed to determine the specific surface area.

Figures

Fig. S1 Scanning electron microscopy images of (A) PBC; (B) E-PBC; (C) O-PBC, and (D) H-PBC.

Fig. S2 Plots of lnKc versus 1/T for the adsorption of (A) Ni2+ and (B) Pb2+ by PBC, H-PCB, E-PBC, and O-PBC

Tables

Table S1 Thermodynamic parameters for the adsorption of Ni2+ by PBC, H-PCB, E-PBC, and O-PBC at different temperatures

| Adsorbate |  | adsorbent | ∆H (kJ mol−1) |  | ∆S (J mol−1 K−1) | ∆G (kJ mol−1) |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  | 288.15 K | 298.15K | 308.15 K | 318.1K |
| Ni (II) | PBC H-PBC |  |  | 6.79 15.15 | 23.6 57.00 | −0.02 −1.27 | −0.25 −1.84 | −0.48 −2.41 | −0.72 −2.98 |
|  | E-PBC |  |  | 15.98 | 56.00 | −0.16 | −0.72 | −1.27 | −1.83 |
|  | O-PBC |  |  | 12.23 | 46.00 | −1.02 | −1.48 | −1.94 | −2.40 |

Table S2 Thermodynamic parameters for the adsorption of Pb2+ by PBC, H-PCB, E-PBC, and O-PBC at different temperatures

| Adsorbate | adsorbent |  | ∆H (kJ mol−1) | ∆S (J mol−1 K−1) | ∆G (kJ mol−1) |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | 288.15 K | 298.15K | 308.15 K | 318.1K |
| Pb (II) | PBC H-PCB | 8.62 4.27 |  | 31.00 32.00 | −0.31 −4.95 | −0.62 −5.27 | −0.93 −5.59 | −1.24 −5.91 |
|  | E-PBC | 5.85 |  | 34.00 | −3.94 | −4.28 | −4.62 | −4.96 |
|  | O-PBC | 4.68 |  | 33.00 | −4.83 | −5.16 | −5.49 | −5.82 |

Table S3 Comparison of various representative Ni2+ adsorbents

| Years | Biomass feedstock | Finishing materials | Maximum adsorption capacity (mg.g−1) | Reference |
| --- | --- | --- | --- | --- |
| 2017 | Straw |  | 25.06 | (Shen et al., 2017) |
|  | Rice husk |  | 10.15 |  |
| 2013 | Figs | H3PO4 | 18.78 | (Gupta et al., 2017) |
| 2017 | Sludge | Mercaptan | 52.40 | (Li et al., 2018) |
| 2017 | Sawdust | KOH | 94.49 | (Nayak et al., 2017) |
|  |  | ZnCl2 | 19.36 |  |
| 2020 | Cactus | NaOH | 44.35 | (Choudhary et al., 2020) |
| 2020 | Rice bran | Al(NO3)3、Mg(NO3)2、FeSO4 | 201.62 | (Guo et al., 2020) |
|  | Corn |  | 19.80 | This study |
|  |  | H3PO4 | 64.94 |  |
|  |  | EDTA | 47.17 |  |
|  |  | NaOH | 60.24 |  |

Table S4 Comparison of various representative Pb2+ adsorbents.

| Years | Biomass feedstock | Finishing materials | Maximum adsorption capacity（mg.g−1） | Reference |
| --- | --- | --- | --- | --- |
| 2014 | Eggshell | ALG and PEI | 344.8 | (Godiya et al., 2019) |
| 2014 | Bean shell |  | 45.3 | (Elaigwu et al., 2014) |
| 2014 | Sawdust | H3PO4 | 80.65 | (Ghasemi et al., 2014) |
| 2017 | Banana peel | Ammonium sulfate persulfate | 315.16 | (Zhou et al., 2017) |
| 2018 | Straw |  | 134.68 | (Cao et al., 2019) |
| 2019 | Shell | EDTA | 129.31 | (Li et al., 2019) |
| 2019 | Peanut shells | H3PO4 | 353.4 | (Jiang et al., 2019) |
|  |  | PEI | 214.0 |  |
| 2019 | Lignin | PEI和CS2 | 79.9 | (Wang et al., 2019) |
|  | Corn |  | 38.31 | This study |
|  |  | H3PO4 | 243.90 |  |
|  |  | EDTA | 156.25 |  |
|  |  | NaOH | 192.31 |  |

References

Cao Y, Xiao W, Shen G, Ji G, Zhang Y, Gao C, Han L (2019) Carbonization and ball milling on the enhancement of Pb(II) adsorption by wheat straw: competitive effects of ion exchange and precipitation. Bioresour Technol 273:70–76.

Choudhary M, Kumar R, Neogi S (2020) Activated biochar derived from opuntia ficus-indica for the efficient adsorption of malachite green dye, Cu(+2) and Ni(+2) from water. J Hazard Mater 392:122441

Elaigwu SE, Rocher V, Kyriakou G, Greenway GM (2014) Removal of Pb2+ and Cd2+ from aqueous solution using chars from pyrolysis and microwave-assisted hydrothermal carbonization of prosopis africana shell. J Ind Eng Chem 20:3467–3473.

Ghasemi M, Naushad M, Ghasemi N, Khosravi-fard Y (2014) A novel agricultural waste based adsorbent for the removal of Pb(II) from aqueous solution: kinetics, equilibrium and thermodynamic studies. J Ind Eng Chem 20:454–461.

Godiya CB, Liang M, Sayed SM, Li D, Lu X (2019) Novel alginate/polyethyleneimine hydrogel adsorbent for cascaded removal and utilization of Cu(2+) and Pb(2+) ions. J Environ Manage 232:829–841.

Guo Z, Chen R, Yang R, Yang F, Chen J, Li Y, Zhou R, Xu J (2020) Synthesis of amino-functionalized biochar/spinel ferrite magnetic composites for low-cost and efficient elimination of Ni(II) from wastewater. Sci Total Environ 722:137822.

Gupta VK, Pathania D, Sharma S (2017) Adsorptive remediation of Cu(II) and Ni(II) by microwave assisted H3PO4 activated carbon. Arab J Chem 10:S2836–S2844.

Jiang Q, Xie W, Han S, Wang Y, Zhang Y (2019) Enhanced adsorption of Pb(II) onto modified hydrochar by polyethyleneimine or H3PO4: an analysis of surface property and interface mechanism. Colloid Surf A: Physicochem Eng Asp 583:123962.

Li J, Xing X, Li J, Shi M, Lin A, Xu C, Zheng J, Li R (2018) Preparation of thiol-functionalized activated carbon from sewage sludge with coal blending for heavy metal removal from contaminated water. Environ Pollut 234:677–683.

Li M, Wei D, Liu T, Liu Y, Yan L, Wei Q, Du B, Xu W (2019) EDTA functionalized magnetic biochar for Pb(II) removal: adsorption performance, mechanism and SVM model prediction. Sep Purif Technol 227:10.

Nayak A, Bhushan B, Gupta V, Sharma P (2017) Chemically activated carbon from lignocellulosic wastes for heavy metal wastewater remediation: effect of activation conditions. J Colloid Interface Sci 493:228–240.

Shen ZT, Zhang YH, McMillan O, Jin F, Al-Tabbaa A (2017) Characteristics and mechanisms of nickel adsorption on biochars produced from wheat straw pellets and rice husk. Environ Sci Pollut Res 24:12809–12819.

Wang Q, Zheng C, Shen Z, Lu Q, He C, Zhang TC, Liu J (2019) Polyethyleneimine and carbon disulfide co-modified alkaline lignin for removal of Pb2+  ions from water. Chem Eng J 359:265–274.

Zhou N, Chen H, Xi J, Yao D, Zhou Z, Tian Y, Lu X (2017) Biochars with excellent Pb(II) adsorption property produced from fresh and dehydrated banana peels via hydrothermal carbonization. Bioresour Technol 232:204–210.