Supporting Information of

Green solid-state synthesis of Cu4O3/biochar composites with high antimicrobial activity

Ke Sun, Wenyi Yang, Yiheng Shen, Zihan Wang, Yindian Wang, Hongxia Chen,* and Yi Liu*

K. Sun, Y. Shen, Z. Wang, Y. Liu*

Materials Genome Institute, Shanghai Engineering Research Center for Integrated Circuits and Advanced Display Materials, Shanghai University, Shanghai 200444, China

*E-Mail: yiliu@shu.edu.cn (Y. Liu)

W. Yang, H. Chen*

School of Life Sciences, Shanghai University, Shanghai, 200444, China

*E-Mail: hxchen@shu.edu.cn (H. Chen)

Y. Wang

School of Medicine, Shanghai University, Shanghai, 200444, China

Figure S1. SEM images of copper formate. (a) untreated sample, (b) after the BM-1 process.

Figure S2. SEM images of (a) CSBC and (b-d) the copper formate/CSBC precursor.

Table S1. The mass ratio of Cu and Cu4O3 in the Cu4O3/CSBC composite. The results were determined by ICP-OES. The mass ratio of Cu4O3 was calculated according to the mass ratio of Cu element (84.1 %) relative to Cu4O3.

| Sample | Cu atomic mass ratio (wt.%) | Cu4O3 mass ratio (wt.%) |
| --- | --- | --- |
| Cu4O3/CSBC composite | 12.87 | 15.30 |

Figure S3. XRD spectra of the sintered product of copper formate/CSBC precursor after the solid-state sintering process at different sintering temperature. (a) sintering at 220 ℃ for 12 min; (b) sintering at 240 ℃ for 12 min.

Figure S4. XRD spectra of the sintered products for the CSBC supporting capacity experiments on Cu4O3. (a) support amount of 10 wt.% for Cu4O3; (b) support amount of 20 wt.% for Cu4O3.

Table S2. Optimal processing parameters for preparing Cu4O3/biochar composites from various resources: PLBC, CWBC, and BBC.

| sample | biomass resource | pyrolysis temperature of biochar (℃) | Cu4O3 mass ratio (wt.%) |
| --- | --- | --- | --- |
| Cu4O3/PLBC composite | palm leaves | 300 | 15 |
| Cu4O3/CWBC composite | cedar wood | 300 | 10 |
| Cu4O3/BBC composite | bagasse | 400 | 15 |

Table S3. Processing variables of the controlled experiments, where “√” indicates that the sample underwent the treatment and “×” indicates that the sample did not undergo the treatment.

| sample | process |  |  |
| --- | --- | --- | --- |
|  | BM-2 | removal of copper formate | solid-state sintering process |
| CSBC | × | × | × |
| BM-CSBC | √ | √ | × |
| BM-S-CSBC | √ | √ | √ |
| Cu4O3/CSBC composite | √ | × | √ |

Table S4. MIC values of the Cu4O3/CSBC composite against E. coli, S. aureus, and MRSA, respectively.

| sample | MIC (μg/mL) |  |  |
| --- | --- | --- | --- |
|  | E. coli | S. aureus | MRSA |
| Cu4O3/CSBC composite | 5 | 0.1 | 0.125 |

Figure S5. Release rate of Cu ions for the Cu4O3/CSBC composite during the 48-hour immersion experiment. The data were analyzed based on the differences in the cumulative release of Cu ions during each test period.

Figure S6. Standard curve between the absorbance of BCS at 483 nm and the concentrations of Cu ions. The linear regression equation was obtained from the standard curve as follows,

A483=0.18796 c+0.05021

where A483 is the absorbance at 483 nm, and c is the concentration of Cu ions.

Experimental procedure:

Hydroxylamine hydrochloride (20 mg) was added to six portions of the standard solution of CuSO4 (1 mM) to completely reduce Cu2+ to Cu+. Then the solution was diluted to 0.5, 1, 2, 3, 4, and 5 ppm of Cu ion concentrations with phosphate buffer solution and water, respectively. 100 μL of BCS solution (5 mM) was added to each solution, and kept for 10 min after shaking. The absorbance of the samples was then detected by UV-vis spectroscopy in the wavelength range of λ = 190-700 nm.

Figure S7. Cumulative release of Cu(I) and Cu(II) ions for the Cu4O3/CSBC composite during the 48-hour immersion experiment. The data were obtained as follows,

CCu(II)=CCu-CCu(I)

where CCu(II) is the cumulative release of Cu(II) ions, CCu is the cumulative release of Cu ions obtained from the ICP-OES test, and CCu(I) is the cumulative release of Cu(I) ions obtained from the linear regression equation: A483 = 0.18796 c + 0.05021.

Table S5. Vacancy formation energy of Cu ions on the Cu4O3 (101) surface.

| Sites | Cu-I | Cu-II-a | Cu-II-b |
| --- | --- | --- | --- |
| Edefected slab (eV) | -299.67 | -298.25 | -298.80 |
| Evacancy (eV) | 1.69 | 3.10 | 2.55 |

The vacancy formation energy is calculated by the equation as follows,

Evacancy=Edefected slab+EFCC_Cu-Eperfect slab

where Evacancy is the vacancy formation energy; Edefected slab is the total energy of surface model with a vacancy, EFCC_Cu is the total energy of FCC Cu, -1.63 eV/atom, and Eperfect_slab is the total energy of (101) surface model, -302.98 eV.

Table S6. Vacancy formation energy of Cu ions on the Cu4O3 (100) surface.

| sites | Cu-I | Cu-II |
| --- | --- | --- |
| Edefected slab (eV) | -291.53 | -289.29 |
| Evacancy (eV) | 1.83 | 4.07 |

The vacancy formation energy is calculated by the equation as follows,

Evacancy=Edefected slab+EFCC_Cu-Eperfect slab

where Evacancy is the vacancy formation energy; Edefected slab is the total energy of surface model with vacancies, EFCC_Cu is the energy of FCC Cu, -1.63 eV/atom, and Eperfect_slab is the total energy of (100) surface model, -294.99 eV.

Table S7. Intensity ratio of the (202) of Cu4O3 and CSBC based on the XRD spectra of the Cu4O3/CSBC composite during a 48-hour immersion experiment.

| Immersion time | 0 h | 6 h | 12 h | 24 h | 48 h |
| --- | --- | --- | --- | --- | --- |
| Id(202)/Id(CSBC) (%) | 1.28 | 1.18 | 1.04 | 0.91 | 0.88 |