Removal of traces of highly explosive trinitrotoluene from TNT Red water by using graphene  nanocomposites prepared from solid wastes:

An example of circular economy

Anshika Yadav1,2, Mohammad O. Aquatar1,2, Reddithota J. Krupadam1,2*

1Climate Change & Green Materials Division, CSIR-National Environmental Engineering Research Institute (NEERI), Nehru Marg, Nagpur 440020, India; 2Academy of Scientific & Innovative Research, Kamla Nehru Marg, Ghaziabad – 201 002, India

Support Information

SI-Fig.1: Schematic of graphene nanocomposites preparation using chemical exfoliation method. GN-G, graphene nanocomposite prepared from commercial graphite and GN-S, graphene nanocomposite prepared from sludge generated during chemical coagulation of TNT red water.

TNT red water

Chemical coagulation

Sludge

Chemical treatment

Filtration

KOH/150°C

organic acid mixture

Graphite

Commercial Graphite

Oxidation

Graphite oxide

Exfoliation

Fe(acac)3 +oleic acid

Reduction

NaNO3 + H2SO4       + KMnO4

GN-G

GN-S

Graphene

Support Information SI-1

Experimental Procedure of Adsorption Studies

A stock solution of TNT with concentration 100 mg L-1 was prepared by dissolution of appropriate quantity of TNT in deionised water. To prepare, TNT stock solution, TNT certified reference material (CRM) procured from AccuStandard (M-8330-11) of concentration 1000 mg L-1 was used. 50 mg of each adsorbent (Gs or GNCs) was dispersed separately in 100 mL of an aqueous TNT solution at pH 70.5 in reagent bottles. The samples were agitated at 300 rpm in temperature-controlled water bath. After fixed time intervals, TNT concentration was monitored using GC (Varian/Saturn 2000 MSD) equipped with capillary column CP-Sil8 CB/Low Bleed – MS (Dawidziuk et al. 2018). The adsorption removal efficiency (RE%) and equilibrium adsorption capacity (qe) of Gs and GNCs were calculated as per mathematical equations [1] and [2] respectively

RE%=[(Ci-Ce)/Ci]×100%                                                                                                  [1]

qe=Ci-Ce×V/Ci                                                                                                                            [2]

where Ci and Ce are initial and residual aqueous TNT concentration (mg L-1) respectively, V represents total volume of contaminant solution used (L), and m here represents adsorbent’s mass (g).

Adsorption kinetic studies were performed in 100 mL reagent bottles at solution pH 7.00.5. Each adsorbent (Gs or GNCs) was added at a quantity of 50 mg to a 100 mL TNT solution, which had a concentration of 100 mg L-1.  Following this, solutions were agitated for 1-120 min in a horizontal shaking system. The temperature of the solution was kept at 298 K throughout the experiments. The solutions after time intervals of 1, 5, 10, 15, 30, 45, 60 and 120 min were collected and centrifuged at 20,000 rpm to settle-down the particles of Gs or GNCs. The concentration of TNT in supernatant solutions was monitored using gas chromatography (GC-MS/MS).

Adsorption isotherm experiments were conducted at temperatures 298 K, 308 K and 318 K. The concentration of TNT solutions used in the isotherm experiments ranged from 1, 5, 10, 25, 50 and 100 mg L-1. The quantity of adsorbents (Gs or GNCs) used for each experiment was 50 mg. The contact time of 30 min. was used for all adsorption isotherm experiments.

Reference Cited:

Dawidziuk, B., Nawała, J., Dziedzic, D., Gordon, D., Popiel, S., 2018. Development, validation and comparison of three methods of sample preparation used for identification and quantification of 2,4,6-trinitrotoluene and products of its degradation in sediments by GC-MS/MS. Anal. Methods 10(43), 5188–5196. https://doi.org/10.1039/C8AY01939H

Support Information

SI-Table 1: Elemental composition of GNCs

| Material | Elemental Composition (wt%) |  |  |  |  | N/C* | H/C* | Feb (wt%) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Na | Ca | Oa | Ha | Others |  |  |  |
| G | 4.3 | 76.1 | 2.1 | 4.1 | 13.4 | 0.056 | 0.054 | 0.02 |
| G-G | 4.5 | 75.6 | 2.3 | 3.9 | 13.7 | 0.059 | 0.051 | 0.07 |
| G-S | 31.2 | 59.9 | 1.1 | 4.7 | 3.1 | 0.521 | 0.078 | 0.09 |
| GN-G | 4.3 | 76.2 | 1.9 | 4.4 | 13.2 | 0.056 | 0.058 | 8.47 |
| GN-S | 16.9 | 70.5 | 1.6 | 2.1 | 8.9 | 0.239 | 0.029 | 8.15 |

acalculated through organic elemental analysis; bcalculated through XRF; *weight ratios.

Support Information

SI-Table 2: Comparison of adsorption capacity of prepared GNC with reported adsorbents.

| Adsorbent | Maximum adsorption capacity qmax (mg g-1) | Adsorption conditions [Contact time/Temp./solution pH] | References |
| --- | --- | --- | --- |
| 4-AING | 168.6 | 8 h/298K/ pH 7.0 | (Wang et al., 2022) |
| nZVI-rGO | 41.9 | 303K/pH 6.0 | (Bharti et al., 2018) |
| AP-SiO2 + Fe/Co | 74 | 8 h/298K/ pH 6.0 | (Mangal et al., 2017) |
| AP-SiO2 + Fe | 57.8 | 8 h/298K/ pH 6.0 |  |
| HINFA | 117.5 | 1.5h/293K | (Wang et al., 2020) |
| Fe@SiO2-NH2 | 6.71 | 293K | (Li et al., 2021) |
| Isoxazoline based porous polymer | 177.3 | 4 h/298K | (Deng et al., 2020) |
| PAIN | 163.8 | 10 h | (Wang et al., 2019) |
| Fe3O4 NHS | 70 | 298K/pH 6.5 | (Rehman et al., 2022) |
| GO | 62.7 | 10 h/298K | (Raad et al., 2017) |
| rGO | 67.8 | 10 h/298K |  |
| rGO/SiO2 | 76.7 | 10 h/298K |  |
| GN-G | 116.2 | 0.5 h/298K | This work |
| GN-S | 151.6 | 0.5 h/298K |  |

4-AING, 4-aminoindole-based aerogel; nZVI-rGO, nano zerovalent iron impregnated reduced graphene oxide; AP-SiO2 + Fe/Co, silica nanoparticles prepared using aerogel process impregnated with bimetallic Fe/Co; AP-SiO2 + Fe, silica nanoparticles prepared using aerogel process impregnated with Fe; PCR, porous carbon rods; Fe-PCR, iron containing porous carbon rods; HINFA, hybrid hierarchically porous indole based aerogel; Fe@SiO2-NH2; amino-modified nanosized zero valent iron; PAIN, indole based polymer with amine units; Fe3O4NHS, magnetic nano hollow spheres; GO, graphene oxide; rGO, reduced graphene oxide; rGO-SiO2, reduced graphene oxide coated silica nanoparticles..