Degradation of enrofloxacin by Fe0 activated PDS

Yaru Zhang  Zhenguo Li  Wenlong Bi*  Bo Sun  Huanhuan Pei  Junmei Qin  Liu Fenwu

College of Resources and Environment, Shanxi Agricultural University, Taigu 030801, PR China

*Corresponding author. E-mail: jiayangbihu@126.com

Supplementary Material

- The standard curve for enrofloxacin

Figure S1 The standard curve for enrofloxacin

- Before and after pH of ENR degradation in different systems

Table S1 The pH before and after the degradation of ENR with Fe0/PS under optimal

conditions ([ENR] =20 μmol/L, [Fe0] = 0.15 g/L, [PS] =0.4 mM).

| Condition | Fe0 | PS | Fe0/PS |
| --- | --- | --- | --- |
| Before | 6.35 | 6.35 | 6.35 |
| After | 6.66±0.02 | 6.11±0.01 | 5.84±0.02 |

- EPR Detection Mapping

Figure S2 EPR Detection Mapping

([ENR] =20 μmol/L, [Fe0] = 0.15 g/L).

- Ultraviolet spectrum of ENR degraded at different time points in Fe0/PS system

Figure S3 Ultraviolet spectrum of ENR degraded at different time points in Fe0/PS system

([ENR] =20 μmol/L, [Fe0] = 0.15 g/L, [PS] =0.4 mM).

- Table S2 The pH before and after free radical contribution in Fe0/PS system

([ENR] =20 μmol/L, [Fe0] = 0.15 g/L, [PS] =0.4 mM).

| Condition | MeOH | TBA | Control |
| --- | --- | --- | --- |
| Before | 6.35 | 6.35 | 6.35 |
| After | 5.93 | 5.77 | 5.88 |

6. pH in the degradation of ENR in Fe0/PS system

Figure S4. pH in the degradation of ENR in the FeS2/PS system with time

([ENR] =20 μmol/L, [Fe0] = 0.15 g/L, [PS] =0.4 mM).

- Changes in iron ion concentration during ENR removal by Fe0/PDS system

Figure S5. Variation of Fe2+ and  Fe3+ concentration in the Fe0/PDS system ([ENR]=20 μmol/L, [Fe0]=0.15 g/L, [PDS]=0.4 mmol/L)

- TOC change after reaction

Figure S6. Determination of TOC after ENR degradation in Fe0/PDS system ([ENR]=20 μmol/L, [Fe0]=0.15 g/L, [PDS]=0.4 mmol/L)

- The pH before and after the degradation of ENR by Fe0/PS system under different pH conditions

Table S3 The pH before and after the degradation of ENR by Fe0/PS system under different pH conditions ([ENR] =20 μmol/L, [Fe0] = 0.15 g/L, [PS] =0.4 mM)

| Condition | pH = 2 | pH = 4 | pH = 6 | pH = 8 | pH = 10 | Control |
| --- | --- | --- | --- | --- | --- | --- |
| Before | 1.98 | 4.00 | 5.98 | 7.98 | 10.01 | 6.35 |
| After | 2.38 | 5.95 | 6.24 | 6.01 | 6.08 | 5.88 |

- The pH before and after the reaction of different anions

Table S4 After adding different concentrations of Cl–, HCO3–, NO3–, the Fe0/PS system degrades the pH before and after the methyl orange reaction ([ENR] =20 μmol/L, [Fe0] = 0.15 g/L, [PS] =0.4 mM)

| Anion/ENR | Cl– |  | HCO3– |  | NO3– |  |
| --- | --- | --- | --- | --- | --- | --- |
| Reaction | Before | After | Before | After | Before | After |
| 0 | 6.35 | 5.88 | 6.35 | 5.88 | 6.35 | 5.88 |
| 0.1 | 6.30 | 6.16 | 6.53 | 5.66 | 6.54 | 5.55 |
| 1 | 6.18 | 6.02 | 6.74 | 5.72 | 7.05 | 5.53 |
| 10 | 6.08 | 5.99 | 7.78 | 5.55 | 7.11 | 5.50 |
| 100 | 6.05 | 5.92 | 7.98 | 7.71 | 7.45 | 5.60 |

- Basic physical and chemical properties of different water substrates

Table S5 Physical and chemical properties of different water substrates.

| Physicochemical property | Tap water | River water |
| --- | --- | --- |
| Water temperature | 20.3ºC | 21.6ºC |
| pH | 7.90 | 8.02 |
| Electrical conductivity | 535 μS/cm | 655 μS/cm |
| TOC | 11.12 mg/L | 18.65 mg/L |
| Na+ | 4.02 mg/L | 7.69 mg/L |
| K+ | 0.11 mg/L | 1.021 mg/L |
| Ca2+ | 24.16 mg/L | 15.09 mg/L |
| Mg2+ | 80.15 mg/L | 60.25 mg/L |
| Cl– | 59.32 mg/L | 23.45 mg/L |
| HCO3– | 265.16 mg/L | 254.63 mg/L |

Note: The river water was taken from the Wuma River, Taigu, Jinzhong City, Shanxi Province on April 25, 2024 ( 37°2711N, 112°3318E )