Supplementary Information

Effect of spraying and stirring on the formation and decomposition of CH4 hydrates in the presence of copper foam and 1,3-DIOX

Xinwei Mi1, Yao Li1, Lanyun Wang1,2*, Yongliang Xu1,2, Yibo Gao1, Zecheng Lv1，Zhengyan Wu 3, Kun Zhang 4

1 School of Safety Science and Engineering, Henan Polytechnic University, Jiaozuo, 454003, Henan, China.

2 School of Safety Science and Engineering, Changzhou University, Changzhou 213164, Jiangsu, China.

3 School of Safety Engineering, China University of Mining & Technology, Xuzhou, 221116, Jiangsu, China.

4 Department of System Safety Engineering, Nagaoka University of Technology, 1603-1Kamitomioka-machi, Nagaoka-shi, Niigata 940-2188, Japan

CH4 hydrates formation

Table S1. The induction times of CH4 hydrates formation in pure water and copper foam systems

under 3.0MPa and 4.0MPa (in min)

| pressure |  | Spraying method | Stirring method | Stirring+ spraying | Static condition |
| --- | --- | --- | --- | --- | --- |
| 3.0MPa | Pure water | 517.4 | 361.8 | 456.7 | 579.8 |
|  | 30PPI copper foam | 622 | 468 | 406.4 | 630.3 |
|  | 60PPI copper foam | 493.6 | 394.5 | 385.3 | 550.6 |
|  | 130PPI copper foam | 519.5 | 496.7 | 279.2 | 591.9 |
| 4.0MPa | Pure water | 598.1 | 354 | 559.5 | 593 |
|  | 30PPI copper foam | 614.4 | 475.2 | 460.3 | 507.8 |
|  | 60PPI copper foam | 584.2 | 442.8 | 399 | 418.3 |
|  | 130PPI copper foam | 553.8 | 118.6 | 325 | 479.9 |

Table S2. The gas consumption of CH4 hydrates formation in pure water and copper foam systems

under 3.0MPa and 4.0MPa (in mol CH4 /mol H2O)

| pressure |  | Spraying method | Stirring method | Stirring+ spraying | Static condition |
| --- | --- | --- | --- | --- | --- |
| 3.0MPa | Pure water | 0.0156 | 0.0482 | 0.048 | 0.0177 |
|  | 30PPI copper foam | 0.0145 | 0.06025 | 0.0498 | 0.0206 |
|  | 60PPI copper foam | 0.0122 | 0.0536 | 0.0732 | 0.0218 |
|  | 130PPI copper foam | 0.0463 | 0.0945 | 0.01013 | 0.0215 |
| 4.0MPa | Pure water | 0.0326 | 0.0602 | 0.04 | 0.0307 |
|  | 30PPI copper foam | 0.0438 | 0.0764 | 0.0579 | 0.0337 |
|  | 60PPI copper foam | 0.0275 | 0.1007 | 0.0726 | 0.04 |
|  | 130PPI copper foam | 0.0627 | 0.1154 | 0.1086 | 0.0508 |

Table S3. The induction times and growth times of CH4 hydrates formation in 1,3-dioxolane system (in min)

|  | Spraying method |  | Stirring method |  | Stirring+ Spraying |  | Static condition |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | induction time | growth time | induction time | growth time | induction time | growth time | induction time | growth time |
| 1,3-dioxolane (2.0MPa) | 33.4 | 77.9 | 32.3 | 107.2 | 22.1 | 65.9 | 26 | 26 |
| 1,3-dioxolane (3.0MPa) | 43.5 | 151.6 | 20.9 | 398.9 | 37.5 | 227 | 35.7 | 77.1 |
| 1,3-dioxolane (4.0MPa) | 22.5 | 79.1 | 9.8 | 214 | 35.7 | 82 | 10.3 | 111.6 |

Table S4. The gas consumption of CH4 hydrates formation in 1,3-dioxolane system (in mol CH4 /mol H2O)

|  | Spraying method | Stirring method | Stirring+ Spraying | Static condition |
| --- | --- | --- | --- | --- |
| 1,3-dioxolane (2.0MPa) | 0.0471 | 0.0426 | 0.0268 | 0.0108 |
| 1,3-dioxolane (3.0MPa) | 0.098 | 0.0848 | 0.0996 | 0.0448 |
| 1,3-dioxolane (4.0MPa) | 0.0552 | 0.064 | 0.0644 | 0.055 |

Table S5. The induction times of CH4 hydrates in copper foam + 1,3-dioxolane systems (in min)

| pressure | systems | Spraying method | Stirring method | Stirring+ spraying | Static condition |
| --- | --- | --- | --- | --- | --- |
| 2.0MPa | 1,3-dioxolane + 30PPI copper foam | 22.5 | 19.7 | 26.5 | 19.3 |
|  | 1,3-dioxolane + 60PPI copper foam | 31.1 | 27.9 | 20 | 17.9 |
|  | 1,3-dioxolane + 130PPI copper foam | 29 | 18.1 | 32.3 | 36.4 |
| 3.0MPa | 1,3-dioxolane + 30PPI copper foam | 75.3 | 13.4 | 10.8 | 14.4 |
|  | 1,3-dioxolane + 60PPI copper foam | 43 | 15.3 | 12.45 | 9.5 |
|  | 1,3-dioxolane + 130PPI copper foam | 34.4 | 19.7 | 17.5 | 37.4 |
| 4.0MPa | 1,3-dioxolane + 30PPI copper foam | 13.9 | 5.7 | 31.01 | 9 |
|  | 1,3-dioxolane + 60PPI copper foam | 4.85 | 5.35 | 41.42 | 5.35 |
|  | 1,3-dioxolane + 130PPI copper foam | 19.5 | 9.5 | 29.1 | 7.3 |

Table S6. The gas consumption of CH4 hydrates formation in copper foam + 1,3-dioxolane systems

(in mol CH4 /mol H2O)

| pressure | systems | Spraying method | Stirring method | Stirring+ spraying | Static condition |
| --- | --- | --- | --- | --- | --- |
| 2.0MPa | 1,3-dioxolane + 30PPI copper foam | 0.039 | 0.0867 | 0.0692 | 0.0342 |
|  | 1,3-dioxolane + 60PPI copper foam | 0.0517 | 0.0513 | 0.0676 | 0.0392 |
|  | 1,3-dioxolane + 130PPI copper foam | 0.0719 | 0.0634 | 0.0715 | 0.0454 |
| 3.0MPa | 1,3-dioxolane + 30PPI copper foam | 0.0917 | 0.1061 | 0.1519 | 0.0497 |
|  | 1,3-dioxolane + 60PPI copper foam | 0.1002 | 0.0851 | 0.1733 | 0.0792 |
|  | 1,3-dioxolane + 130PPI copper foam | 0.0734 | 0.0739 | 0.062 | 0.0855 |
| 4.0MPa | 1,3-dioxolane + 30PPI copper foam | 0.0689 | 0.1118 | 0.1244 | 0.0566 |
|  | 1,3-dioxolane + 60PPI copper foam | 0.1291 | 0.1179 | 0.1198 | 0.0536 |
|  | 1,3-dioxolane + 130PPI copper foam | 0.0937 | 0.1256 | 0.0799 | 0.0876 |

(a) 2.0MPa, spraying method

(b) 2.0MPa, stirring method

(c) 2.0MPa, stirring + spraying method

(d) 2.0MPa, static condition

(e) 3.0MPa, spraying method

(f) 3.0MPa, stirring method

(g) 3.0MPa, stirring + spraying method

(h) 3.0MPa, static condition

(i) 4.0MPa, spraying method

(j) 4.0MPa, stirring method

(k) 4.0MPa，stirring + spraying method

(l) 4.0MPa，static condition

Figure S1. The experimental P-T-t curve of CH4 hydrates formation with different mechanical methods in the presence of CF+1,3-DIOX

CH4 hydrates decomposition

Table S7. Decomposition temperatures and times of CH4 hydrates in copper foam + 1,3-dioxolane systems

| Condition | Systems | Starting decomposition temperature（K） | Complete decomposition temperature（K） | decomposition time （min） |
| --- | --- | --- | --- | --- |
| 4.0MPa spraying method | 1,3-DIOX | 288.82 | 299.36 | 217.52 |
|  | 1,3-DIOX+30PPICF | 288.36 | 300.43 | 242.35 |
|  | 1,3-DIOX+60PPICF | 287.46 | 299.9 | 253.08 |
|  | 1,3-DIOX+130PPICF | 286.89 | 299.28 | 255.62 |
| 4.0MPa stirring method | 1,3-DIOX | 283.2 | 305.91 | 499.77 |
|  | 1,3-DIOX+30PPICF | 288.57 | 305.59 | 356.82 |
|  | 1,3-DIOX+60PPICF | 287.75 | 304.5 | 319.2 |
|  | 1,3-DIOX+130PPICF | 286.77 | 304.51 | 370.98 |
| 3.0MPa spraying method | 1,3-DIOX | 285.82 | 297.57 | 251.72 |
|  | 1,3-DIOX+30PPICF | 285.89 | 294.36 | 162.28 |
|  | 1,3-DIOX+60PPICF | 286.43 | 298.63 | 245.55 |
|  | 1,3-DIOX+130PPICF | 285.05 | 299 | 284.87 |
| 3.0MPa stirring method | 1，3-DIOX | 285.05 | 303.86 | 382.82 |
|  | 1,3-DIOX+30PPICF | 287.03 | 302.2 | 300.97 |
|  | 1,3-DIOX+60PPICF | 287.38 | 300.65 | 267.22 |
|  | 1,3-DIOX+130PPICF | 286.21 | 303.55 | 350.08 |

(a) 3.0MPa, stirring method

(b) 3.0MPa, spraying method

(c) 4.0MPa, stirring method

(d) 4.0MPa, spraying method

Figure S2. The experimental P-T-t curve of CH4 hydrates decomposition with spraying and stirring methods in the presence of CF+1,3-DIOX