Supplementary file

Fig. S.1 Normal probability effects for the studied outputs

Fig. S.2 pareto charts of effects for the studied outputs

Table S.1.Normalized ion release rate from different vitrified samples (mg/(cm2 d)).

| Glass sample , x 10-4 | Sr | B | Na | References |
| --- | --- | --- | --- | --- |
| ABS-Waste (17) | 4.47 | 36.02 | 28.301 | [9] |
| MABS-Waste (20) | 3.447 | 31.54 | 22.256 | [9] |
| ABS-Waste (25) | 1.226 | 20.121 | 40.363 | [9] |
| Simulated Magnox-modified | - | 130.68 | 19.42 | [61] |
| Sr-ABS | 1.95 | - | 1.25 | This study |