Supporting Information for

Photocatalytic hydrogen peroxide production with an external quantum yield of almost 500%

Yaozong Yan,1 Shin-ichi Naya,2* Hisashi Sugime,1,3 Hiroaki Tada4*                 & Tetsuro Soejima1,3*

1 Graduate School of Science and Engineering, Kindai University, 3-4-1, Kowakae, Higashi-Osaka, Osaka 577-8502, Japan.

2 Environmental Research Laboratory, Kindai University, 3-4-1, Kowakae, Higashi-Osaka, Osaka 577-8502, Japan.

3 Department of Applied Chemistry, Faculty of Science and Engineering, Kindai University, 3-4-1, Kowakae, Higashi-Osaka, Osaka 577-8502, Japan.

4 Institutes of Innovation for Future Society, Nagoya University, Furo-cho, Chikusa-ku, Nagoya, Aichi 464-8603, Japan.

* To whom correspondence should be addressed: Prof. Hiroaki Tada

E-mail: htada0409@gmail.com

Table of Contents

Supplementary Fig. 1 | Adsorption and decomposition properties of various metal oxides in dark. The decrement in H2O2 concentration of the solution (0.1 mM, 10 mL) in the presence of various metal oxide particles (100 mg) at 298 K.	S4

Supplementary Fig. 2 | Morphologies of the hybrid photocatalyst components. SEM images of ATO (a) and ZnO (b).	S4

Supplementary Fig. 3 | Morphology of ATO particles. TEM images of ATO particles observed at different magnifications.	S5

Supplementary Fig. 4 | Morphology of ht-ATO-CL/ZnO particles. TEM-EDS analysis for ht-ATO-CL/ZnO particles.	S5

Supplementary Fig. 5 | Junction state of ht-ATO-CL(100)/ZnO(50). HR-TEM image of ht-ATO-CL(100)/ZnO(50).	S6

Supplementary Fig. 6 | Optical properties of the samples. Kubelka-Munk-transformed UV-Vis-NIR absorption spectra of ZnO, ATO, and ATO-CL(100)/ZnO(50).	S6

Supplementary Fig. 7 | Band gap determination. Tauc plots for ZnO (a) and ATO (b).	S7

Supplementary Fig. 8 | Relationship between the mixing ratio of ATO-CL(x)/ZnO(50) and photocatalytic activity for H2O2 production. Plots of the H2O2 concentration generated after 12 h irradiation vs. ATO content. The values in the abscissa show the x values with the y value fixed at 50 mg.	S7

Supplementary Fig. 9 | Catalytic activity and photocatalytic activity for H2O2 decomposition. Time courses for the H2O2 concentration in the presence of Au/TiO2 and ATO-CL(100)/ZnO2(50) in dark and under UV-light irradiation ( = 365 nm) using two LED lamps (each light intensity = 120 mW cm−2).	S8

Supplementary Fig. 10 | Kinetic isotope effect of H2O2 production. Time courses for ATO-CL(100)/ZnO(50)-photocatalyzed H2O2 production in the 4 vol% C2H5OH and C2D5OD aqueous solutions at 288 K.	S8

Supplementary Fig. 1 | Adsorption and decomposition properties of various metal oxides in dark. The decrement in H2O2 concentration of the solution (0.1 mM, 10 mL) in the presence of various metal oxide particles (100 mg) at 298 K.

Supplementary Fig. 2 | Morphology of ZnO particles. TEM images of ZnO particles observed at different magnifications.

Supplementary Fig. 3 | Morphology of ATO particles. TEM images of ATO particles observed at different magnifications.

Supplementary Fig. 4 | Morphology of ht-ATO-CL/ZnO particles. TEM-EDS analysis for ht-ATO-CL/ZnO particles.

Supplementary Fig. 5 | Junction state of ht-ATO-CL(100)/ZnO(50). HR-TEM image of ht-ATO-CL(100)/ZnO(50).

Supplementary Fig. 6 | Optical properties of the samples. Kubelka-Munk-transformed UV-Vis-NIR absorption spectra of ZnO, ATO, and ATO-CL(100)/ZnO(50).

- (b)

Supplementary Fig. 7 | Optical band gaps of the samples. Tauc plots of ZnO (a) and ATO (b).

Supplementary Fig. 8 | Relationship between the mixing ratio of ATO-CL(x)/ZnO(50) and photocatalytic activity for H2O2 production. Plots of the H2O2 concentration generated after 12 h irradiation vs. ATO content. The values in the abscissa show the x values with the y value fixed at 50 mg.

Supplementary Fig. 9 | Catalytic activity and photocatalytic activity for H2O2 decomposition. Time courses for the H2O2 concentration in the presence of Au/TiO2 and ATO-CL(100)/ZnO2(50) in dark and under UV-light irradiation ( = 365 nm) using two LED lamps (each light intensity = 120 mW cm−2).

Supplementary Fig. 10 | Kinetic isotope effect of H2O2 production. Time courses for ATO-CL(100)/ZnO(50)-photocatalyzed H2O2 production in the 4 vol% C2H5OH and C2D5OD aqueous solutions at 288 K.