Chitosan modified diatomite cross-linked with sodium alginate and polyethyleneimine composite gel particles for efficient removal of copper and lead ions

Jianjun Sun1 · Zongrui Zhang1 · Mengyun Yu1 · Weiwei Xu1 · Guona Bai1 · Yixin Xiang1 · Mengqun Li1

Materials and methods

Preparation of DE/CS-PEI@SA composite gel particles

The impact of varying proportions of SA and PEI on the gel particles morphology was investigated during the preparation of composite gels. Various combinations of SA and PEI were utilized to produce composite gel samples, with the specific components detailed in Table S1.

Table S1. Components of DE/CS-PEI@SA composite gel particles

| sample | DE/CS mass (g) | PEI mass (g) | SA mass(g) |
| --- | --- | --- | --- |
| DE/CS-PEI@SA(2:1) composite gel | 0.5 | 0.5 | 0.25 |
| DE/CS-PEI@SA(1:1) composite gel | 0.5 | 0.5 | 0.5 |
| DE/CS-PEI@SA(1:1.5) composite gel | 0.5 | 0.5 | 0.75 |
| DE/CS-PEI@SA(1:3) composite gel | 0.5 | 0.5 | 1.5 |
| DE/CS-PEI@SA(1:2) composite gel | 0.5 | 0.5 | 1.0 |
| DE/CS-PEI@SA(1:2) composite gel | 0.5 | 0.25 | 1.0 |
| DE/CS-PEI@SA(1:2) composite gel | 0.5 | 0.75 | 1.0 |
| DE/CS-PEI@SA(1:2) composite gel | 0.5 | 1.0 | 1.0 |

Adsorption experiments

The standard curves for Cu(Ⅱ) and Pb(Ⅱ) absorbance are generated in Fig. S1.

Fig. S1. The standard curves of copper Cu(II) and lead Pb(II) absorbance.

Results and discussion

Chemical structural performance

Fig. S2. The (a) FT-IR, and (b) 1H NMR spectra of the composite gel DE/CS-PEI@SA and after the adsorption of Cu(II) and Pb(II).

Crystallization and thermal properties

Fig. S3. The (a) XRD, and (b) DSC spectra of the composite gel DE/CS-PEI@SA and after the adsorption of Cu(II) and Pb(II).

Thermal stability

Fig. S4. The (a) TG and (b) DTG curves of the composite gel DE/CS-PEI@SA and after the adsorption of Cu(II) and Pb(II).

Adsorption performance and kinetics

Fig. S5. The Cu(II) and Pb(II) adsorption performances of raw materials DE, CS, SA, and composite gel DE/CS-PEI@SA.

Fig. S6. The Cu(II) and Pb(II) adsorption performances of different composition of composite gel DE/CS-PEI@SA, (a) and (c) different PEI amount.