Supporting information

Fine-tuning dye adsorption capacity of UiO-66 by mixed-ligand approach

Chompoonoot Nanthamatheea, Chantamalinee Chantarangkula, Chanida Jakkrawhad a, Apirak Payakaa and Pongsathorn Dechatiwongseb*

aDepartment of Chemistry, School of Science, Walailak University, Nakhon Si Thammarat, Thailand, 80160.

bDepartment of Chemical Engineering, School of Engineering and Technology, Walailak University, Nakhon Si Thammarat, Thailand, 80160.

*Coresponding author

Figure. S1 SEM images of (a) UiO-66 (b) UiO-66-0.5ATA (c) UiO-66-0.75ATA (d) UiO-66-ATA

Figure. S2 Plots of (a) pseudo-second-order kinetics (b) pseudo-first-order kinetics of IC adsorption onto UiO-66, UiO-66-0.5ATA, UiO-66-0.75ATA and UiO-66-ATA at 303 K, 313 K and 323 K at initial concentration of 100 ppm

Figure. S3 Elovich kinetic model for IC adsorption onto UiO-66, UiO-66-0.5ATA, UiO-66-0.75ATA and UiO-66-ATA at 303 K, 313 K and 323 K at initial concentration of 100 ppm

Table S1 Kinetic parameters of the adsorption of IC on UiO-66, UiO-66-0.5ATA, UiO-66-0.75ATA and UiO-66-ATA at initial concentration of 100 ppm, temperture = 303 K.

| Pseudo first order model | UiO-66 | UiO-66-0.5ATA | UiO-66-0.75ATA | UiO-66-ATA |
| --- | --- | --- | --- | --- |
| k1 (1/min) x 103 | 2.3 | 2.3 | 2.07 | 2.76 |
| Qe(exp) (mg/g) | 86.46 | 79.55 | 89.23 | 79.67 |
| Qe(cal) (mg/g) | 53.77 | 27.35 | 16.68 | 25.96 |
| R2 | 0.9529 | 0.964 | 0.787 | 0.8183 |
| Pseudo second order model | UiO-66 | UiO-66-0.5ATA | UiO-66-0.75ATA | UiO-66-ATA |
| k2 (g/ min mg) x 10^3 | 0.21 | 0.32 | 0.28 | 0.36 |
| Qe(cal) (mg/g) | 89.28 | 81.3 | 87.72 | 80 |
| R2 | 0.9975 | 0.9982 | 0.9976 | 0.999 |
| Elovich model | UiO-66 | UiO-66-0.5ATA | UiO-66-0.75ATA | UiO-66-ATA |
| α (mg/g min) | 174.10 | 43.91 | 44.41 | 1.95 x 103 |
| β (g/mg) | 0.13 | 0.11 | 0.10 | 0.20 |
| R2 | 0.7178 | 0.8999 | 0.9068 | 0.9454 |
| Intra-particular diffusion model | UiO-66 | UiO-66-0.5ATA | UiO-66-0.75ATA | UiO-66-ATA |
| K1d (g/mg min1/2) | 2.4498 | 0.9001 | 1.4645 | 1.0018 |
| R2 | 0.9863 | 0.9618 | 0.9494 | 0.9857 |
| K2d (g/mg min1/2) | 1.101 | 0.7977 | 1.014 | 0.4152 |
| R2 | 0.9987 | 0.9644 | 0.9772 | 0.9497 |
| K3d (g/mg min1/2) | 1.2045 | 0.2123 | 0.1175 | 0.3732 |
| R2 | 0.9651 | 0.6092 | 0.6988 | 0.8862 |
| Boyd kinetic model | UiO-66 | UiO-66-0.5ATA | UiO-66-0.75ATA | UiO-66-ATA |
| B (1/s) x 103 | 2 | 3.4 | 3.3 | 2 |
| R2 | 0.9806 | 0.9785 | 0.9183 | 0.9545 |
| Di x 10-18(m2/s) | 3.58 | 6.09 | 2.63 | 3.58 |

Table S2 Kinetic parameters of the adsorption of IC on UiO-66, UiO-66-0.5ATA, UiO-66-0.75ATA and UiO-66-ATA at initial concentration of 100 mg/L, temperture = 313 K.

| Pseudo first order model | UiO-66 | UiO-66-0.5ATA | UiO-66-0.75ATA | UiO-66-ATA |
| --- | --- | --- | --- | --- |
| k1 (1/min) x 103 | 2.3 | 1.38 | 2.07 | 1.84 |
| Qe(exp) (mg/g) | 96.15 | 85.92 | 89.72 | 79.67 |
| Qe(cal) (mg/g) | 14.95 | 21.76 | 16.07 | 26.76 |
| R2 | 0.7152 | 0.6305 | 0.8945 | 0.8207 |
| Pseudo second order model | UiO-66 | UiO-66-0.5ATA | UiO-66-0.75ATA | UiO-66-ATA |
| k2 (g/ min mg) x 10^3 | 0.38 | 0.41 | 0.33 | 0.44 |
| Qe(cal) (mg/g) | 96.15 | 85.47 | 88.5 | 78.74 |
| R2 | 0.9983 | 0.998 | 0.9946 | 0.9978 |
| Elovich model | UiO-66 | UiO-66-0.5ATA | UiO-66-0.75ATA | UiO-66-ATA |
| α (mg/g min) | 2910.94 | 29.38 | 460.44 | 4.42 x 104 |
| β (g/mg) | 0.14 | 0.13 | 0.13 | 0.21 |
| R2 | 0.8842 | 0.9639 | 0.9081 | 0.963 |
| Intra-particular diffusion model | UiO-66 | UiO-66-0.5ATA | UiO-66-0.75ATA | UiO-66-ATA |
| K1d (g/mg min1/2) | 3.2294 | 1.259 | 1.638 | 1.0372 |
| R2 | 0.9089 | 0.9559 | 0.9637 | 0.9682 |
| K2d (g/mg min1/2) | 0.1465 | 0.6287 | 0.8018 | 0.432 |
| R2 | 0.6428 | 0.9072 | 0.9601 | 0.9169 |
| K3d (g/mg min1/2) | 0.4566 | 0.732 | 0.1553 | 0.4566 |
| R2 | 0.9217 | 0.8889 | 0.9669 | 0.9217 |
| Boyd kinetic model | UiO-66 | UiO-66-0.5ATA | UiO-66-0.75ATA | UiO-66-ATA |
| B (1/s) x 103 | 1.3 | 1.9 | 3.2 | 2 |
| R2 | 0.5114 | 0.9689 | 0.9596 | 0.9423 |
| Di x 10-18(m2/s) | 2.33 | 3.4 | 2.55 | 3.58 |

Table S3 Kinetic parameters of the adsorption of IC on UiO-66, UiO-66-0.5ATA, UiO-66-0.75ATA and UiO-66-ATA at initial concentration of 100 mg/L, temperture = 323 K.

| Pseudo first order model | UiO-66 | UiO-66-0.5ATA | UiO-66-0.75ATA | UiO-66-ATA |
| --- | --- | --- | --- | --- |
| k1 (1/min) x 103 | 2.76 | 2.76 | 2.53 | 2.99 |
| Qe(exp) (mg/g) | 97.12 | 85.43 | 90.45 | 79.42 |
| Qe(cal) (mg/g) | 30.75 | 18.51 | 12.02 | 22.66 |
| R2 | 0.8288 | 0.8158 | 0.8174 | 0.9761 |
| Pseudo second order model | UiO-66 | UiO-66-0.5ATA | UiO-66-0.75ATA | UiO-66-ATA |
| k2 (g/ min mg) x 10^3 | 0.48 | 0.52 | 0.42 | 0.56 |
| Qe(cal) (mg/g) | 98.04 | 86.95 | 90.91 | 80.19 |
| R2 | 0.9971 | 0.9971 | 0.9997 | 0.9997 |
| Elovich model | UiO-66 | UiO-66-0.5ATA | UiO-66-0.75ATA | UiO-66-ATA |
| α (mg/g min) | 2377.00 | 1031.02 | 10284.08 | 1.30 x 106 |
| β (g/mg) | 0.14 | 0.14 | 0.16 | 0.25 |
| R2 | 0.8668 | 0.9576 | 0.9205 | 0.9417 |
| Intra-particular diffusion model | UiO-66 | UiO-66-0.5ATA | UiO-66-0.75ATA | UiO-66-ATA |
| K1d (g/mg min1/2) | 1.0229 | 1.6995 | 1.832 | 1.1661 |
| R2 | 0.973 | 0.9579 | 0.9678 | 0.9266 |
| K2d (g/mg min1/2) | 0.4179 | 0.4046 | 0.2269 | 0.2928 |
| R2 | 0.9941 | 0.9781 | 0.9792 | 0.9376 |
| K3d (g/mg min1/2) | 0.2815 | 0.8326 | 0.2266 | 0.2638 |
| R2 | 0.9276 | 0.8981 | 0.7938 | 0.6183 |
| Boyd kinetic model | UiO-66 | UiO-66-0.5ATA | UiO-66-0.75ATA | UiO-66-ATA |
| B (1/s) x 103 | 1.8 | 1.3 | 2.9 | 0.8 |
| R2 | 0.9683 | 0.9376 | 0.9234 | 0.7827 |
| Di x 10-18(m2/s) | 3.22 | 1.33 | 2.31 | 1.43 |

Figure. S4 Plots of variation of IC adsorption kinetics onto UiO-66, UiO-66-0.5ATA, UiO-66-0.75ATA and UiO-66-ATA at IC concentration of 100 ppm according to the intra-particle diffusion

Figure. S5 The plot of Bt versus time for UiO-66, UiO-66-0.5ATA, UiO-66-0.75ATA and UiO-66-ATA at IC concentration of 50 and 100 ppm, T = 303 K

Figure. S6 Langmuir adsorption isotherms for the adsorption of IC by UiO-66, UiO-66-0.5ATA, UiO-66-0.75ATA and UiO-66-ATA at initial concentration of 100 ppm and temperature of 303 K, 313 K and 323 K.

Figure. S7 Freundlich adsorption isotherms for the adsorption of IC by UiO-66, UiO-66-0.5ATA, UiO-66-0.75ATA and UiO-66-ATA at 303 K, 313 K and 323 K

Figure. S8 Dubinin-Radushkevich (D-R) isotherms for the adsorption of IC by UiO-66, UiO-66-0.5ATA, UiO-66-0.75ATA and UiO-66-ATA at 303 K, 313 K and 323 K

Figure. S9 Temkin isotherms for the adsorption of IC by UiO-66, UiO-66-0.5ATA, UiO-66-0.75ATA and UiO-66-ATA at 303 K, 313 K and 323 K

Figure. S10 Plot of lnKd versus 1/T of IC adsorption on UiO-66, UiO-66-0.5ATA, UiO-66-0.75ATA and UiO-66-ATA

Table S4 Comparison of IC adsorption capacities of different adsorbents

| Adsorbents | Adsorption capacity (mg/g) | Reference |
| --- | --- | --- |
| CuAl-LDH/SWCNTs nanocomposites | 196.78 | 1 |
| Mg/Fe layered double hydroxide nanoparticles | 62.8 | 2 |
| activated carbon doped with Mn oxide (Bio-MnOx-C) | 45.95 | 3 |
| nanotube carbon (CNTs) | 88.5 | 4 |
| COOH-functionalized CNTs | 136 | 4 |
| Brazil nut shells | 1.09 | 5 |
| Rice husk ash | 29.28 | 6 |
| Chitin | 0.0058 | 7 |
| Chitosan | 0.0072 | 7 |
| Activated carbon (AC) prepared from peanut shell | 24.35 | 8 |

Table S5 Adsorption capacity of UiO-66, UiO-66-0.5ATA, UiO-66-0.75ATA and UiO-66-ATA at different types of dyes solution (dye concentration = 100 ppm, pH = 6.5, contact time = 24 hours, adsorbent dosage = 10.0000 mg in 10.00 mL dye solution).

| Dye | Adsorption capacity (Qe) (mg/g) |  |  |  |
| --- | --- | --- | --- | --- |
|  | UiO-66 | UiO-66-0.5ATA | UiO-66-0.75ATA | UiO-66-ATA |
| Methylene blue | 69.26 | 81.58 | 89.74 | 72.34 |
| Indigo Carmine | 75.89 | 69.55 | 84.26 | 66.67 |
| Methyl orange | 44.52 | 57.64 | 48.90 | 34.34 |
| Phenol red | 30.56 | 69.25 | 63.96 | 55.69 |
| Congo red | 35.00 | 45.34 | 52.82 | 37.30 |

| E = -8172.45410327 a.u. |  |
| --- | --- |
| [Zr6O4(OH)4(OOC-C6H4-COO)12]12– |  |
| E = -8504.21712182 a.u. | E = -8504.20809961 a.u. |
| [Zr6O4(OH)4(OOC-C6H4-COO)6(OOC-C6H6N-COO)6]12–_A | [Zr6O4(OH)4(OOC-C6H4-COO)6(OOC-C6H6N-COO)6]12–_B |
| E = -8504.21341557 a.u. | E = -8504.21320031 a.u. |
| [Zr6O4(OH)4(OOC-C6H4-COO)6(OOC-C6H6N-COO)6]12–_C | [Zr6O4(OH)4(OOC-C6H4-COO)6(OOC-C6H6N-COO)6]12–_D |
| E = -8504.21353798 a.u. | E = -8504.20949533 a.u. |
| [Zr6O4(OH)4(OOC-C6H4-COO)6(OOC-C6H6N-COO)6]12–_E | [Zr6O4(OH)4(OOC-C6H4-COO)6(OOC-C6H6N-COO)6]12–_F |
| E = -8504.20594593 a.u. | E = -8504.21363441 a.u. |
| [Zr6O4(OH)4(OOC-C6H4-COO)6(OOC-C6H6N-COO)6]12–_G | [Zr6O4(OH)4(OOC-C6H4-COO)6(OOC-C6H6N-COO)6]12–_H |
| E = -8504.20869663 a.u. | E = -8504.20789128 a.u. |
| [Zr6O4(OH)4(OOC-C6H4-COO)6(OOC-C6H6N-COO)6]12–_I | [Zr6O4(OH)4(OOC-C6H4-COO)6(OOC-C6H6N-COO)6]12–_J |
| E = -8670.10076069 a.u. | E = -8670.10152076 a.u. |
| [Zr6O4(OH)4(OOC-C6H4-COO)3(OOC-C6H6N-COO)9]12–-A | [Zr6O4(OH)4(OOC-C6H4-COO)3(OOC-C6H6N-COO)9]12–-B |
| E = -8835.74195856 a.u. |  |
| [Zr6O4(OH)4(OOC-C6H6N-COO)12]12– |  |

Figure S11. All possible structures of [Zr6O4(OH)4(OOC-C6H4-COO)12]12–, [Zr6O4(OH)4(OOC-C6H4-COO)3(OOC-C6H6N-COO)9]12–, [Zr6O4(OH)4(OOC-C6H4-COO)3(OOC-C6H6N-COO)9]12– and [Zr6O4(OH)4(OOC-C6H6N-COO)12]12– are presented optimizing at PM6 level of theory. Their structural energies were calculated at PBE1PBE/LanL2DZ level of accuracy.

| HOMO | LUMO |
| --- | --- |
| [Zr6O4(OH)4(OOC-C6H4-COO)12]12– |  |
| [Zr6O4(OH)4(OOC-C6H4-COO)6(OOC-C6H6N-COO)6]12–_A |  |
| [Zr6O4(OH)4(OOC-C6H4-COO)6(OOC-C6H6N-COO)6]12–_B |  |
| [Zr6O4(OH)4(OOC-C6H4-COO)6(OOC-C6H6N-COO)6]12–_C |  |
| [Zr6O4(OH)4(OOC-C6H4-COO)6(OOC-C6H6N-COO)6]12–_D |  |
| [Zr6O4(OH)4(OOC-C6H4-COO)6(OOC-C6H6N-COO)6]12–_E |  |
| [Zr6O4(OH)4(OOC-C6H4-COO)6(OOC-C6H6N-COO)6]12–_F |  |
| [Zr6O4(OH)4(OOC-C6H4-COO)6(OOC-C6H6N-COO)6]12–_G |  |
| [Zr6O4(OH)4(OOC-C6H4-COO)6(OOC-C6H6N-COO)6]12–_H |  |
| [Zr6O4(OH)4(OOC-C6H4-COO)6(OOC-C6H6N-COO)6]12–_I |  |
| [Zr6O4(OH)4(OOC-C6H4-COO)6(OOC-C6H6N-COO)6]12–_J |  |
| [Zr6O4(OH)4(OOC-C6H4-COO)3(OOC-C6H6N-COO)9]12–-A |  |
| [Zr6O4(OH)4(OOC-C6H4-COO)3(OOC-C6H6N-COO)9]12–-B |  |
| [Zr6O4(OH)4(OOC-C6H6N-COO)12]12– |  |

Figure S12. The HOMO and LUMO orbitals of [Zr6O4(OH)4(OOC-C6H4-COO)12]12–, [Zr6O4(OH)4(OOC-C6H4-COO)6(OOC-C6H6N-COO)6]12–, [Zr6O4(OH)4(OOC-C6H4-COO)3(OOC-C6H6N-COO)9]12– and [Zr6O4(OH)4(OOC-C6H6N-COO)12]12– are presented calculating from TD-DFT calculations at PBE1PBE/LanL2DZ level of accuracy.

References

1.	Almoisheer, N.; Alseroury, F. A.; Kumar, R.; Aslam, M.; Barakat, M. A., Adsorption and anion exchange insight of indigo carmine onto CuAl-LDH/SWCNTs nanocomposite: kinetic, thermodynamic and isotherm analysis. RSC Advances 2019, 9, (1), 560-568.

2.	Ahmed, M. A.; brick, A. A.; Mohamed, A. A., An efficient adsorption of indigo carmine dye from aqueous solution on mesoporous Mg/Fe layered double hydroxide nanoparticles prepared by controlled sol-gel route. Chemosphere 2017, 174, 280-288.

3.	Hu, Y.; Chen, X.; Liu, Z.; Wang, G.; Liao, S., Activated carbon doped with biogenic manganese oxides for the removal of indigo carmine. Journal of Environmental Management 2016, 166, 512-518.

4.	Dastgerdi, Z. H.; Meshkat, S. S.; Esrafili, M. D., Enhanced adsorptive removal of Indigo carmine dye performance by functionalized carbon nanotubes based adsorbents from aqueous solution: equilibrium, kinetic, and DFT study. Journal of Nanostructure in Chemistry 2019, 9, (4), 323-334.

5.	de Oliveira Brito, S. M.; Andrade, H. M. C.; Soares, L. F.; de Azevedo, R. P., Brazil nut shells as a new biosorbent to remove methylene blue and indigo carmine from aqueous solutions. Journal of Hazardous Materials 2010, 174, (1), 84-92.

6.	Mittal, A.; Mittal, J.; Kurup, L., Batch and bulk removal of hazardous dye, indigo carmine from wastewater through adsorption. Journal of Hazardous Materials 2006, 137, (1), 591-602.

7.	Prado, A. G. S.; Torres, J. D.; Faria, E. A.; Dias, S. l. C. L., Comparative adsorption studies of indigo carmine dye on chitin and chitosan. Journal of Colloid and Interface Science 2004, 277, (1), 43-47.

8.	Zhang, J.; Zhou, Q.; Ou, L., Removal of indigo carmine from aqueous solution by microwave-treated activated carbon from peanut shell. Desalination and Water Treatment 2016, 57, (2), 718-727.