Hierarchically porous composites containing mining tailings-based geopolymer and zeolite 13X: application for carbon dioxide sequestration

Mariana Schneider1,2, Enrique Rodríguez-Castellón2, M. Olga Guerrero-Pérez3, Dachamir Hotza1, Agenor De Noni Junior1, Regina de Fátima Peralta Muniz Moreira1*

1 Department of Chemical Engineering and Food Engineering, Federal University of Santa Catarina, 88040-900 Florianópolis, SC, Brazil

2 Department of Inorganic Chemistry Faculty of Sciences, University of Málaga, 29071 Málaga, Spain

3 Department of Chemical Engineering, Faculty of Sciences, University of Málaga, 29071 Málaga, Spain

*Corresponding author: R F P M Moreira (regina.moreira@ufsc.br)

Supplementary data

.

Figure 1S. Deconvolution spectra of the Z13X sample.

Figure 2S. Deconvolution spectra of the GP sample

Figure 3S(a). Deconvolution spectra of the Z5 sample.

Figure 3S(b). Deconvolution spectra of the Z10 sample.

Figure 3S(c). Deconvolution spectra of the Z20 sample.

Figure 3S(d). Deconvolution spectra of the Z30 sample.

Table 1S. XPS quantification of the deconvoluted peaks.

|  | Area peaks (%) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | GP |  |  |  |  | Z13X |  |  |  | x | Z5 |  |  | x | Z10 |  |  |  | Z20 |  |  |  | Z30 |  |  |
| C1s | 284.8 eV 77.59 | 286.4 eV 7.57 | 289.0 eV 3.41 | 291.3 eV 11.44 | x | 284.8 eV 72.24 | 286.9 eV 5.31 | 289.3 eV 4.82 | 291.9 eV 17.62 |  | 284.9 eV 79.33 | 286.6 eV 4.95 | 289.5 eV 15.72 |  | 284.8 eV 82.60 | 286.6 eV 7.61 | 289.2 eV 9.79 |  | 284.8 eV 86.80 | 286.6 eV 6.75 | 289.1 eV 6.45 |  | 284.8 eV 80.37 | 286.5 eV 11.09 | 289.1 eV 8.54 |
| O1s | 530.5 eV 9.63 | 531.5 eV 67.05 | 532.8 eV 23.32 | - |  | 531.6 eV 96.37 | 533.1 eV 3.63 | - | - |  | 531.4 eV 62.40 | 532.5 eV 37.60 | - |  | 531.3 eV 69.63 | 532.4 eV 30.37 |  |  | 531.4 eV 56.80 | 532.3 eV 43.20 |  |  | 531.4 eV 56.82 | 532.4 eV 43.18 |  |
| Na1s | 1072.6 eV 100 | - | - | - |  | 1072.3 eV 100 | - | - | - |  | 1072.8 eV 100 | - | - |  | 1072.2 eV 100 | - |  |  | 1072.3 eV 100 | - |  |  | 1072.4 eV 100 | - |  |
| Al2s | - | - | - | - |  | 119.1 eV 83.92 | 123.9 eV 16.08 | - | - |  |  |  | - |  |  |  |  |  |  |  |  |  |  |  |  |
| Mg1s |  |  |  |  |  |  |  |  |  |  | 1303.8 eV 100 |  |  |  | 1303.7 eV 100 |  |  |  | 1303.8 eV 100 |  |  |  | 1303.8 eV 100 |  |  |
| Si2p | 102.4 eV 100 | - | - | - |  | 102.5 eV 100 | - | - | - |  | 102.7 eV 100 | - | - |  | 102.6 eV 100 | - |  |  | 102.7 eV 100 |  |  |  | 102.7 eV 100 |  |  |
| Al2p | 74.3 eV 100 | - | - | - |  | 72.7 eV 13.83 | 74.2 eV 86.17 | - | - |  | 74.5 eV 100 |  | - |  | 74.3 eV 100 |  |  |  | 74.4 eV 100 |  |  |  | 74.4 eV 100 |  |  |
| Mg2p | - | - | - | - |  | 50.2 eV 72.08 | 55.6 eV 27.92 | - | - |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Fe2p | 711.1 eV 100 | - | - | - |  | 710.6 eV 60.09 | 713.8 eV 19.59 | 724.7 eV 20.32 | - |  |  |  |  |  |  |  |  |  | 711.4 eV 70.83 | 723.9 eV 29.17 |  |  | 712.0 eV 62.09 | 725.2 eV 37.91 |  |
| Cl2p | - | - | - | - |  | 199.0 eV 100 | - | - | - |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |