Supporting Information

Heterogeneous Catalytic Oxidation of 5-hydroxymethylfurfural (5-HMF) To 2,5-Diformoylfuran (DFF) Using Fe3O4@C Catalyst

Rama Jaiswala, Kalluri V.S. Ranganath*

a Dept. of Chemistry, Institute of Science, Banaras Hindu University, Varanasi

E-mail: ranganath.Chem@bhu.ac.in

Fig. S1: XPS of  a heterogeneous catalyst, Fe3O4@C

DFF analysis

The confirmation of DFF were done by HPLC, UV-Vis spectroscopy.

% conversion= no. of moles of product formedinitial no. of moles of substrate×100

% selectivity= no. of moles of product formedtotal no. of moles of products×100

Fig. S2 Calibration curve plotted against concentration of HMF (Using HPLC, UV-detector, 483 nm).

min

0.0

2.5

5.0

7.5

10.0

12.5

15.0

17.5

20.0

0

25

50

75

Detector A 283nm

2

.

229

2

.

634

7

.

212

12

.

127

Fig. S3 HPLC chromatogram of DFF from HMF using H2O2 as Oxidant

min

0.0

2.5

5.0

7.5

10.0

12.5

15.0

17.5

20.0

22.5

0

50

100

150

Detector A 283nm

6

.

933

11

.

495

Fig. S4 HPLC chromatogram of DFF from HMF using TEMPO as Oxidant

Fig. S5 HPLC chromatogram of DFF from HMF using molecular oxygen as Oxidant

Fig. S6 HPLC chromatogram of DFF from Glucose using H2O2 as Oxidant

In figure S10, UV-Vis graph represent lambda max. value for Glucose (A), DFF (B) i.e.  obtained from glucose and (C) also for DFF obtained from HMF.

Fig. S7 UV-Vis spectra of reaction mixture after removal of the catalysts from the reaction mixture

In summary, we developed a new heterogeneous catalyst, operable under mild conditions, for the selective oxidation of HMF to DFF using Fe3O4@C catalyst. Under optimized reaction conditions, we used water as a solvent.

Fig. S8 GC/MS of the reaction mixture.