Supplementary Information

Fig. S1. EDS N-element surface scan analysis diagram. (a) resin XRZ04B (b) enzyme-loaded XRZ04B (c) CALB@resin-CAB

Fig. S2. TGA analysis of resin XRZ04B, enzyme-loaded XRZ04B and CALB@resin-CAB.

Fig. S3. Fluorescence analysis of immobilized CALB (a) surface (b) Cross-section

Fig. S4. N2 adsorption-desorption isotherm of (a) resin XRZ04B (b) enzyme-loaded XRZ04B (c) CALB@resin-CAB

Fig. S5. Pore size distribution curves of resin XRZ04B (Black square■), enzyme-loaded resin XRZ04B (Red circle●) and CALB@resin-CAB (Blue Triangles▲).

Fig. S6. Optimization of enzyme-catalyzed biodiesel production (a) Temperature (b) Types of organic solvents (c) Organic solvent content

Fig. S7. Batch stability of CALB@resin-CAB catalyzed biodiesel production.

Fig. S8. CALB@resin-CAB catalyzed production of biodiesel in flow reaction, flow rate: 1-20 Bv/h

Table S1. Esterification activity and protein leakage rates of different immobilized enzymes.

| Immobilized enzyme | Specific enzyme activity（PLU/g） | Protein leakage rate（%） |
| --- | --- | --- |
| enzyme-loaded resin | 13214.1±2.3 | 8.4±0.6 |
| CALB@resin-CAB | 12685.5±2.6 | 2.1±0.1 |
| Novozym 435 | 10067.9±3.2 | 8.5±0.4 |
| coated Novozym 435 | 9665.2±2.5 | 2.2±0.2 |

Table. S2 The physical properties of as-prepared samples.

| Sample | SBET (m2·g-2) | Pore capacity (cm3·g-1) |  | Average pore size (nm) | most probable pore size (nm) |
| --- | --- | --- | --- | --- | --- |
| resin XRZ04B | 161.17 | 0.44 | 17.73 |  | 22.49 |
| enzyme-loaded resin XRZ04B | 3.24 | 0.01 | 15.77 |  | 16.04 |
| CALB@resin-CAB | 34.00 | 0.09 | 18.39 |  | 21.13 |

Table S3. Effect of molar ratio of Oil and methanol on conversion of Palm acidification oil.

| Molar ratio of oil to alcohol (mol:mol) | Actual conversion rate (%) |  | Theoretical Conversion Rate (%) | Actual/Theoretical Relative Conversion Rate (%) |
| --- | --- | --- | --- | --- |
| 1:1 | 32.1 | 33.3 |  | 96.4 |
| 1:2 | 62.4 | 66.7 |  | 93.6 |
| 1:3 | 92.1 | 100 |  | 92.1 |
| 1:4 | 92.0 | 100 |  | 92.0 |
| 1:5 | 90.4 | 100 |  | 90.4 |
| 1:6 | 88.6 | 100 |  | 88.6 |