Supporting Information

Polycaprolactone Electrospun Nanofibers Embedded with Phosphorus-Doped g-Carbon Nitride for Rapid Detection of Xanthine

Hafsah Akhtara, Sehrish Hanifb, Fahad Hussain Alhamoudic, Anam Zulfiqard, Ather Farooq Khana, Naeem Akhtarb,e*, Hamad Khalid**a, Nosherwan Adild, Cong Yu***e

aInterdisciplinary Research Centre in Biomedical Materials (IRCBM), COMSATS University Islamabad, Lahore Campus 54000, Pakistan

bInstitute of Chemical Sciences, Bahauddin Zakariya University (BZU), Multan 60800, Pakistan

cDental Technology Department, Applied Medical Sciences, King Khalid University, Abha 62529, Kingdom of Saudi Arabia.

dDepartment of Biochemistry, Bahauddin Zakariya University (BZU), Multan 60800, Pakistan

eState Key Laboratory of Electroanalytical Chemistry, Changchun Institute of Applied Chemistry, Chinese Academy of Sciences, Changchun 130022, China

Corresponding author:

Dr. Naeem Akhtar: naeemakhtar@bzu.edu.pk

Dr. Hamad Khalid: hamakhalid@cuilahore.edu.pk

Dr. Cong Yu: congyu@ciac.ac.cn

- Instrument Details

The surface morphological analyses of PCL-P@gC3N4 were analyzed using TESCAN Vega LMU-Variable Pressure Scanning Electron Microscope (SEM) and compositional analysis was characterized by using scanning electron microscopy (FEI NOVA Nano SEM 450). Fourier transform infrared spectroscopy (FTIR) was conducted using an IRA affinity-1S spectrophotometer-USA to obtain FTIR spectra of PCL-P@gC3N4, P@gC3N4 and gC3N4. X-ray diffraction (XRD) analysis was performed using a Rigaku Miniflex-II (600-c, made in Japan) with Cu Kα radiation. The scan angle ranged from 5⁰ to 80⁰, step size 0.02⁰, scan speed 10⁰/min and the X-ray source operated at 40 kV and 40 mA. Electrochemical characterizations were investigated using potentiostat (Metrohm DropSens, Software: DropView 8400). This potentiostat instrument contains three electrodes: a working electrode, a reference electrode, and an auxiliary electrode. In this work, the synthesized electrode PCL-P-gC3N4@NF was used as the working electrode, Ag/AgCl as the reference electrode, and platinum wire as the auxiliary electrode.