Table 1 Six Types of Intersection Modes between Joints

| Node | Parallel crack penetration | Parallel crack penetration Type |
| --- | --- | --- |
| P1 |  | The internal endpoints of parallel cracks produce shear cracks and are connected by secondary tensile cracks |
| P2 |  | The internal endpoints of parallel cracks are connected by secondary tensile cracks |
| P3 |  | The endpoint of the crack and the middle part of another crack are connected by a tensile wing crack |
| P4 |  | Two cracks on the same side are connected by a tensile crack at the end |
| P5 |  | Two cracks with opposite side ends connected by reverse tensile cracks |
| P6 |  | Two coplanar cracks with different ends connected by shear cracks |

Table 2 Probability distribution types of structural plane parameters

| Structural plane grouping number | Number of joints | Dip angle α/° | Dip direction β/° | Trace length L/mm | Joint density P32 (m2/m3) |
| --- | --- | --- | --- | --- | --- |
|  | 8 | 30 | 0 | 20 | 12.5 |
|  |  | 45 |  |  |  |
|  |  | 60 |  |  |  |
|  |  | 75 |  |  |  |
|  | 8 | 30 | 0 | 20 | 12.5 |
|  |  | 45 |  |  |  |
|  |  | 60 |  |  |  |
|  |  | 75 |  |  |  |
|  | 8 | 30 | 0 | 20 | 12.5 |
|  |  | 45 |  |  |  |
|  |  | 60 |  |  |  |
|  |  | 75 |  |  |  |

Table 3 Results of Whole Rock Element Analysis of Marble

| element | Weight percentage（wt%） | The total confidence value of the analysis（wt% Sigma） |
| --- | --- | --- |
| O | 38.27 | 0.20 |
| Mg | 2.14 | 0.05 |
| Al | 9.3 | 0.09 |
| Si | 31.83 | 0.16 |
| Nb | 18.45 | 0.29 |
| total | 100 |  |

Table 4 Strength parameters of fractured network rock mass

|  | Peak stress σc/MPa | Strength ratio n | Elastic modulus Es/GPa | Poisson's ratio ν |
| --- | --- | --- | --- | --- |
| a-30 | 15.04 | 0.28 | 17.1 | 0.289 |
| a-45 | 24.93 | 0.46 | 18.4 | 0.325 |
| a-60 | 27.73 | 0.52 | 19.1 | 0.308 |
| a-75 | 51.08 | 0.95 | 21.5 | 0.317 |
| b-30 | 30.23 | 0.56 | 18.7 | 0.312 |
| b-45 | 31.85 | 0.59 | 19.9 | 0.321 |
| b-60 | 42.63 | 0.79 | 21.2 | 0.315 |
| b-75 | 48.56 | 0.91 | 22.9 | 0.303 |
| c-30 | 23.53 | 0.44 | 17.7 | 0.300 |
| c-45 | 24.65 | 0.46 | 21.8 | 0.301 |
| c-60 | 36.77 | 0.69 | 23.0 | 0.325 |
| c-75 | 40.69 | 0.76 | 22.7 | 0.306 |

Table 5 Process and failure diagram of rock mass fracture in a series of fracture networks

| Node | Failure process |  |  | Test failure figure | Failure mode |
| --- | --- | --- | --- | --- | --- |
| a-30 |  |  |  |  | Tensile failure, Stepped and rotation mode |
|  | 11.24MPa | 14.0MPa | 10.5 MPa |  |  |
| a-45 |  |  |  |  | Tensile and shear failure, Stepped and rotation mode |
|  | 21.01 MPa | 24.5MPa | 19.5 MPa |  |  |
| a-60 |  |  |  |  | Tensile failure, Stepped mode |
|  | 24.35 MPa | 27.5MPa | 2.0 MPa |  |  |
| a-75 |  |  |  |  | Shear failure, Stepped mode |
|  | 45.95 MPa | 50.5MPa | 29.9 MPa |  |  |

Table 6 Process and failure diagram of rock mass fracture in the b series fracture network

| Node | Failure process |  |  | Test failure figure | Failure mode |
| --- | --- | --- | --- | --- | --- |
| b-30 |  |  |  |  | Tensile failure, Stepped mode |
|  | 25.93 MPa | 30.0 MPa | 10.5 MPa |  |  |
| b-45 |  |  |  |  | Tensile failure, Stepped mode |
|  | 25.28 MPa | 31.5 MPa | 20.5 MPa |  |  |
| b-60 |  |  |  |  | Tensile failure, Stepped mode |
|  | 38.34 MPa | 42.0 MPa | 28.5 MPa |  |  |
| b-75 |  |  |  |  | Shear failure, Through a plane mode |
|  | 43.06 MPa | 48.0 MPa | 3.68 MPa |  |  |

Table 7 Process and failure diagram of rock mass fracture in the c-series fracture network

| Node | Failure process |  |  | Test failure figure | Failure mode |
| --- | --- | --- | --- | --- | --- |
| c-30 |  |  |  |  | Tensile failure, Stepped mode |
|  | 18.67MPa | 23.0 MPa | 10.0 MPa |  |  |
| c-45 |  |  |  |  | Tensile and shear failure, Through a plane mode |
|  | 18.83MPa | 24.0 MPa | 6.43 MPa |  |  |
| c-60 |  |  |  |  | Tensile and shear failure, Through a plane mode |
|  | 32.94MPa | 36.0 MPa | 5.0 MPa |  |  |
| c-75 |  |  |  |  | Tensile and shear failure, Stepped and rotation mode |
|  | 34.63MPa | 40.0 MPa | 5.0 MPa |  |  |

Table 8 PFC3D microscopic parameters

| Particle parameters |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Minimum particle size/mm | Particle size multiplier |  | Young's modulus/GPs |  | Stiffness ratio |  |  | friction coefficient |  | density/(kg·m-3) |
| 1.0 | 1.66 |  | 22 |  | 2.5 |  |  | 0.5 |  | 2700 |
| Adhesive parameters |  |  |  |  |  |  |  |  |  |  |
| Parallel bonding radius |  | Parallel contact/GPa |  | Stiffness ratio |  | Adhesive tensile strength/MPa |  |  | Adhesive shear strength/MPa |  |
| 1 |  | 3 |  | 3 |  | 40±6.4 |  |  | 40±6.4 |  |
| Smooth joint model parameters |  |  |  |  |  |  |  |  |  |  |
| Normal stiffness/GPa |  |  |  | Tangential stiffness/GPa |  |  | friction coefficient |  |  |  |
| 2 |  |  |  | 2 |  |  | 0.7 |  |  |  |

Table 9 Macro mechanical parameters of rock specimens

|  | Peak intensity/MPa | Elastic modulus/Gpa |
| --- | --- | --- |
| PFC3Dcomplete | 53.82 | 24.87 |
| Complete experiment | 54.57 | 24.65 |

Table 10 PFC3D numerical simulation of fracture network rock mechanics parameters

| a-series |  |  | b-series |  |  | c-series |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Dip/° | Peak intensity/MPa | Elastic modulus/GPa | Dip/° | Peak intensity/MPa | Elastic modulus/GPa | Dip/° | Peak intensity/MPa | Elastic modulus/GPa |
| 30 | 32.11 | 17.63 | 30 | 27.20 | 17.19 | 30 | 28.58 | 16.93 |
| 45 | 34.02 | 18.54 | 45 | 31.64 | 18.49 | 45 | 31.80 | 17.37 |
| 60 | 36.77 | 19.71 | 60 | 35.66 | 19.39 | 60 | 36.74 | 18.25 |
| 75 | 41.46 | 20.33 | 75 | 41.87 | 20.27 | 75 | 44.21 | 19.25 |

Table 11 PFC failure mode diagram of a series of rock masses

| Node | Test crack distribution | PFC crack distribution | Particle displacement magnitude | Particle displacement direction | Joint propagation | Failure mode |
| --- | --- | --- | --- | --- | --- | --- |
| a-30 |  |  |  |  | The joints 2, 3, 4, and 6 are connected and damaged. | Stepped |
| a-45 |  |  |  |  | The joints 2, 3, 4, and 6 are connected and damaged. | Stepped |
| a-60 |  |  |  |  | The joints 2, 3, 4, 6 and 8 are connected and damaged. | Stepped |
| a-75 |  |  |  |  | The joints 2, 3, 4, and 6 are connected and damaged. | Stepped |

Table 12 PFC failure mode diagram of b series rock mass

| Node | Test crack distribution | PFC crack distribution | Particle displacement magnitude | Particle displacement direction | Joint propagation | Failure mode |
| --- | --- | --- | --- | --- | --- | --- |
| b-30 |  |  |  |  | The joints 1, 2, 4, and 5 are connected and damaged. | Stepped and rotation |
| b-45 |  |  |  |  | The joints 1, 2, 4, 5 and 7 are connected and damaged. | Stepped and rotation |
| b-60 |  |  |  |  | The joints 1, 2, 4, and 5 are connected and damaged. | Stepped |
| b-75 |  |  |  |  | The joints 1, 2, 4, and 5 are connected and damaged. | Through a plane |

Table 13 PFC failure mode diagram of c series rock mass

| Node | Test crack distribution | PFC crack distribution | Particle displacement magnitude | Particle displacement direction | Joint propagation | Failure mode |
| --- | --- | --- | --- | --- | --- | --- |
| c-30 |  |  |  |  | The joints 1, 3 and 5 are connected and damaged. | Stepped |
| c-45 |  |  |  |  | The joints 1, 3 and 5 are connected and damaged. | Through a plane |
| c-60 |  |  |  |  | The joints 1, 3, 5, and 7 are connected and damaged. | Through a plane |
| c-75 |  |  |  |  | The joints 1, 3, 5, and 7 are connected and damaged. | Rotation |

Table 14 Statistical table of main mechanical parameters of discrete marble fractured rock mass

|  | σf/MPa | εf/% | E* /GPa | m | ε0/% | D0 |
| --- | --- | --- | --- | --- | --- | --- |
| a-30 | 15.04 | 0.136 | 17.1 | 2.294368 | 0.195314 | 0.312397 |
| a-45 | 24.93 | 0.196 | 18.4 | 2.708389 | 0.283154 | 0.260123 |
| a-60 | 27.73 | 0.218 | 19.1 | 2.460035 | 0.314321 | 0.231976 |
| a-75 | 51.08 | 0.34 | 21.5 | 2.789904 | 0.491127 | 0.13547 |
| b-30 | 30.23 | 0.23 | 18.7 | 2.836092 | 0.332167 | 0.24806 |
| b-45 | 31.85 | 0.241 | 19.9 | 2.443141 | 0.347382 | 0.199807 |
| b-60 | 42.63 | 0.3 | 21.2 | 2.499655 | 0.432808 | 0.147533 |
| b-75 | 48.56 | 0.347 | 22.9 | 2.030492 | 0.491836 | 0.079175 |
| c-30 | 23.53 | 0.202 | 17.7 | 2.390138 | 0.290856 | 0.288271 |
| c-45 | 24.65 | 0.198 | 21.8 | 1.784981 | 0.273929 | 0.123407 |
| c-60 | 36.77 | 0.229 | 23.0 | 2.782696 | 0.330796 | 0.075154 |
| c-75 | 40.69 | 0.244 | 22.7 | 3.242746 | 0.350708 | 0.087217 |