BiVO4 photoanode synergistically with persulfate to degrade antibiotics: degradation mechanism and pathway

Yun Chena, Jinquan Wana,b,*, Yongwen Maa,b, Yan Wanga, Zhicheng Yana, Shou Yang

a College of Environment and Energy, South China University of Technology, Guangzhou 510006, Guangdong, China

b Sino-Singapore International Joint Reasearch Institute, Guangzhou 510640, Guangdong, China

*Corresponding author: Tel: -86 13660539751

E-mail: jquan_wan@163.com (Jinquan Wan)

(b)

(a)

Fig.S1. (a) SEM image of BiVO4 photoanode;(b) XRD patterns of BiVO4 photoanode;

FigS2 UV-Vis spectra of BiVO4 photoanode.

Text 1

The band gap energy of prepared electrodes can be calculated by:

(αhν)n=A(hν-Eg)

Where α is the absorption coefficient, h is the Planck constant，ν is the light frequency, A is a constant and Eg is band gap. The index n depends on the type of optical transition in the semiconductor, n=2 or 1/2 indicating the type of semiconductor is direct-gap or indirect-gap, respectively.

Fig. S3 the degradation efficiency of SMX with different initial pH

Fig. S4 Changes of pH during degradation process

Fig.S5 The kinetic rate constant of TC in DI water and natural water

Fig.S6 Degradation efficiency of SMX after 4 cycles

Fig S7 XRD patterns of BiVO4 photoanode before and after reaction.

Table S1. The detective methods of three organic contaminants by HPLC.

| Organic Contaminants | Mobile Phase | Flow Rate | λmax/nm |
| --- | --- | --- | --- |
| SMX | acetonitrile : 0.2% Formic acid =30:70 | 1 mL/min | 278 |
| CIP | methanol : 5% Glacial acetic acid =68:32 | 1 mL/min | 278 |
| TC | 0.01M oxalic acid: acetonitrile =75:25 | 1 mL/min | 365 |

Table S2 the kinetic rate constants of different degradation systems

| Rate constant | PEC | PC/PS | EC/PS | PEC/PS |
| --- | --- | --- | --- | --- |
| k` min-1 | 0.0058 | 0.0069 | 0.0012 | 0.00948 |
| R2 | 0.9938 | 0.9996 | 0.9351 | 0.9990 |

Table S3 the kinetic rate constants of different degradation systems

|  | R1 | CPE1-T | CPE2-P | R2 | Error% |
| --- | --- | --- | --- | --- | --- |
| BVO | 23.38 | 8.69E-05 | 0.80827 | 483.9 | 0.9051 |
| BVO/PS | 13.11 | 4.33 E-04 | 0.79621 | 167.9 | 0.61858 |
| BVO/SMX | 14.28 | 3.28 E-04 | 0.81068 | 221.2 | 0.33753 |
| BVO/PS/SMX | 12.45 | 3.76 E-04 | 0.78076 | 126 | 0.30164 |

Table S3 The molecular formulae, molecular masses, and proposed structures of the TPs of SMX

| Products | m/z | Molecular formula | Structural formula |
| --- | --- | --- | --- |
| SMX | 254 | C10H11N3O3 |  |
| TP1 | 190 | C10H11N3O |  |
| TP2 | 99 | C4H6N2O |  |
| TP3 | 209 | C8H8N4O3 |  |
| TP4-1 | 284 | C10H9N3O5S |  |
| TP4-2 | 284 | C10H9N3O5S |  |
| TP5 | 254 | C10H11N3O3S |  |
| TP6 | 299 | C10H9N3O6S |  |
| TP7 | 219 | C6H5NO6S |  |
| TP8 | 504 | C20H20N6O6S2 |  |

Table S5 The molecular formulae, molecular masses, and proposed structures of the TPs of SMX

| Products | m/z | Molecular formula | Structural formula |
| --- | --- | --- | --- |
| CIP | 332 | C17 H18 F N3 O3 |  |
| TP1 | 347 | C17 H18 F N3 O4 |  |
| TP2 | 345 | C17H19N3O5 |  |
| TP3 | 317 | C16H19N3O4 |  |
| TP4 | 301 | C16H19N3O3 |  |
| TP5 | 362 | C17H16FN3O5 |  |
| TP6-1 | 334 | C16H16FN3O4 |  |
| TP6-2 | 334 | C16H16FN3O4 |  |
| TP7 | 306 | C15H16FN3O3 |  |
| TP8 | 290 | C15H16FN3O2 |  |
| TP9 | 263 | C13H11FN2O3 |  |
| TP10 | 280 | C13H13FN2O4 |  |
| TP11 | 207 | C11H12FN2O |  |

Table S6 The molecular formulae, molecular masses, and proposed structures of the TPs of SMX

| Products | m/z | Molecular formula | Structural formula |
| --- | --- | --- | --- |
| TC | 445 | C22H24N2O8 |  |
| TP1 | 461 | C22H24N2O9 |  |
| TP2 | 474 | C22H22N2O10 |  |
| TP3 | 477 | C22H24N2O10 |  |
| TP4 | 459 | C22H22N2O9 |  |
| TP5 | 432 | C20H20N2O9 |  |
| TP6 | 427 | C22H22N2O7 |  |
| TP7 | 383 | C21H21NO6 |  |
| TP8 | 431 | C21H22N2O8 |  |
| TP9 | 413 | C21H20N2O7 |  |
| TP10 | 416 | C21H21NO8 |  |
| TP11 | 363 | C18H21NO7 |  |
| TP12 | 376 | C18H17NO8 |  |
| TP13 | 338 | C16H19NO7 |  |
| TP14 | 241 | C12H19NO4 |  |
| TP15 | 403 | C21H25NO7 |  |
| TP16 | 360 | C19H20O7 |  |
| TP17 | 317 | C17H17O6 |  |
| TP18 | 279 | C15H18O5 |  |
| TP19 | 273 | C15H12O5 |  |