Supplementary Materials of “Two-dimensional oxygen crystal with a honeycomb lattice on an ultraflat Cu(111)”

Note 1: Theoretical analysis of magnetic multipoles in oxylene

Note 2: Theoretical analysis of symmetry-allowed linear responses in oxylene

Note 1. Theoretical analysis of magnetic multipoles in oxylene

Figure S1. Spin densities of the upper oxygen layer in a unit cell of oxylene, projected onto the xy plane. Each oxygen atom has its own atomic multipole Oi (i=1,…, 6). Black and white circles represent + (-) spins, respectively, aligned along the z quantization axis. Solid lines indicate the mirror planes normal to the xy plane. A triangle indicates the origin of the three-fold axis normal to the xy plane. For O4, O5, and O6, an additional white circle is located beneath each depicted white circle.

Since symmetry governs physical phenomena, it can be used to predict them. Specifically, physical phenomena can be systematically analyzed by reducing them to symmetry-invariant multipoles. In this section, we analyze the multipoles in oxylene, following the definitions of symbols and methods described in Refs. 1 and 2. We focus on the upper oxygen layer (Fig. S1) as it primarily responds to external stimuli from the top surface.

The atomic multipole of O1 in Fig. S1 corresponds to the magnetic octupole Mzβx,y,z≡Szx2-y2/2 because the spin Sz has a spatial distribution of x2-y2. The atomic multipoles of O2 and O3 are magnetic octupoles derived by rotating O1 by 120 degrees and 240 degrees around the z axis, respectively. As a result, O2 and O3 can be expressed as linear combinations of Mzβx,y,z and Mxyzx,y,z≡Szxy: O2=-32Mxyz-12Mzβ and O3=32Mxyz-12Mzβ.

The atomic multipoles of O4, O5, and O6 can be obtained similarly. The atomic multipole of O4 corresponds to the magnetic octupole of Szx2-z2/2 because Sz has a spatial distribution of x2-z2. Note that O4= Szx2-y2/4-Sz(3z2-r2)/4 = O1/2-Sz(3z2-r2)/4. As the second term remains unaffected with rotation around the z axis, O5 and O6 can be expressed as: O5=O2/2-Sz(3z2-r2)/4 and O6=O3/2-Sz(3z2-r2)/4.

Since the unit cell of oxylene includes all of Oi (i= 1, …, 6) (Fig. S1), it is necessary to define a cluster multipole O(c) as the macroscopic order parameter that encompasses all six atomic multipoles:

O(c)=O1, O2, O3, O4, O5, O6=MxyzAx+MzβAy-Sz3z2-r2A1/4,

where Ax is 0,-32,32,0,-34,34, Ay is 1,-12,-12, 12,-14,-14, and A1 is 0, 0, 0, 1, 1, 1.

We note that the spatial distribution of Oi (i= 1, …, 6) is classified as the magnetic point group 3m', where ‘3’ denotes three-fold rotation symmetry and m' denotes a combined symmetry of time-reversal symmetry and mirror symmetry relative to three mirror axes denoted by solid lines in Fig. S1. Within the symmetry group 3m', Ax and Ay can be treated as x and y, respectively, since they undergo the same transformations for 3m'. On the other hand, A1 functions as a scalar 1.

Therefore, O(c) of oxylene is given as:

O(c)=Mxyzx+Mzβy-Sz3z2-r2/4= Szy3x2-y2-Sz3z2-r2/4,

where Szy3x2-y2 is the magnetic hexadecapole and Sz3z2-r2 is the magnetic octupole2. Considering the lowest order multipole, thus, O(c) of oxylene may be referred to as the cluster magnetic octupole. Note that Sz3z2-r2 of O(c) is indistinguishable from Sz in 3m', implying that, from a symmetry perspective, O(c) is equivalent to Sz and behaves similarly to collinear ferromagnets or ferrimagents. In fact, according to the classification in the spin space group of collinear magnets3, we find that oxylene belongs to the type 1 phase, which includes both ferromagnet and ferrimagnet. As explained in the main text, the magnetization density at the hcp and fcc sites differs in magnitude, indicating that oxylene behaves like a ferrimagnet.

It is important to note that the noncollinear antiferromagnet Mn3Z (Z = Sn, Ge) also exhibits macroscopic cluster magnetic octupole order4. This macroscopic order parameter of Mn3Z is responsible for a range of effects, including the large anomalous Hall effect5,6, anomalous Nernst effect7,8, magneto-optical Kerr effect9,10, magnetic spin Hall effect11, and piezomagnetism12. Despite the difference in their magnetic point groups (3m' for oxylene and m'm'm for Mn3Sn), the presence of cluster magnetic octupole O(c) in oxylene suggests that oxylene may exhibit similar linear responses to those observed in Mn3Z. In the next section, we analyze symmetry-allowed linear responses in oxylene.

Note 2. Theoretical analysis of symmetry-allowed linear responses in oxylene

In this section, we analyze symmetry-allowed linear responses in oxylene, following the definitions of symbols and methods described in Ref. 1. The linear response tensor χij[nB⨯nF] can be represented as Bi[nB]=χij[nB⨂nF]Fj[nF], where B is the rank-nB response and F is the rank-nF external field. When χ[nB⨯nF] has the parity P=-1nB+nF P=-1nB+nF+1, it is called a polar (axial) tensor.

Symmetry-allowed linear responses satisfy two conditions. The first condition is that χij[nB⨂nF] remains invariant under the rotation R associated with the system’s symmetry. We define DXR as the representation matrix of R with the observable X. In the rotated frame, the linear response equation becomes: BinB=DBR-1ijχjknB⨂nFDFRklFlnF. As a result, symmetry-allowed linear responses can be identified by verifying if the following equation is satisfied:

χilnB⨯nF=DBR-1ijχjknB⨂nFDFRkl.                              (S1)

The second condition considers time-reversal symmetry. To describe this condition, we use the Kubo formula13 for the linear response of B under a perturbation Hamiltonian Hpert=AF. Depending on the time-reversal property, χij is decomposed into χijJ and χijE, where χijJ includes the intraband contribution and χij(E) is the interband one1. When the antiunitary operation θR, where θ is the time-reversal operation, preserves the system’s symmetry, χijJ and χijE are transformed as follows:

χilJ=-tBtADBR-1ijχjkJDFRkl,                              (S2)

χilE=tBtADBR-1ijχjkEDFRkl,                                 (S3)

where θ†Xθ=tXX,tX=±1 for X=A, B. When tBtA=1, χJ (χE) can be represented by a time-reversal odd (even) multipole, and vice versa. To satisfy the symmetry conditions [Eqs. (S2) and (S3)], χJ/E should consist of active multipoles that are invariant under the symmetry operations of the magnetic point group corresponding to the system1.

The parity P and time-reversal property T classify multipoles into four types: electric multipole Q, electric toroidal multipole G, magnetic multipole M, and magnetic toroidal multipole T (Table S1)2. The above two conditions directly depend on P and T, making it natural to describe χij based on Q, G, M, and T.

From now on, we show the symmetry-allowed linear responses for χ[1⨂1] and χ[2⨂1]  in oxylene. The active multipoles required to determine χ for 3m' are listed in Table S21. χ[1⨂1] includes the electric conductivity tensor, the magnetoelectric tensor, the magnetic susceptibility tensor, and the electric-field induced rotation. As shown in Table S3, χ[1⨂1] can be classified based on tBtA and parity. According to the Wigner-Eckart theorem14, χ[1⨂1] for 3m' can be represented as:

χ[1⨂1],t=X0-XuYz0-YzX0-Xu000X0+2Xu,                              (S4)

where t, X, and Y are defined in Table S4. Here, the row and column correspond to Bx,By,Bz and Fx,Fy,Fz, respectively.

As an example, let us consider the conductivity tensor where B is the electrical current and F is the electric field or temperature gradient. According to Table S4, this tensor corresponds to tBtA=-1 and is a polar tensor. When  t=E, Yz of Eq. (S4) is Mz, which corresponds to the magnetic dipole along z direction. The presence of Mz as off-diagonal components of χ[1⨂1],t indicates that oxylene exhibits the anomalous Hall effect, anomalous Nernst effect, and magneto-optical Kerr effect. As another example, let us consider the magnetoelectric tensor where B is the magnetization and F is the electric field. According to Table S4, this tensor corresponds to tBtA=-1 and is an axial tensor. When  t=E,  X0 and Xu of Eq. (S4) are M0 (magnetic monopole) and Mu (magnetic quadrupole), respectively. This indicates that oxylene has the symmetry of M0 and Mu, enabling oxylene to exhibit the magnetoelectric effect.

Next, we discuss χ[2⨂1], which includes the piezoelectric tensor, the piezomagnetic tensor, and spin conductivity tensor (See Table S5). χ[2⨂1] can be represented as:

χt=X3aX3bXz'+2Xz-2Xzα-X3a-X3bXz'+2Xz-2Xzα00Xz'-4Xz+4XzαYu-3Xz-2Xzα0-3Xz-2Xzα-Yu02X3b-2X3a0,                  (S5)

where Xz' is independent of Xz. The row corresponds to Bxx,Byy,Bzz,Byz,Bzx,Bxy, and the column corresponds to Fx,Fy,Fz.

As an example, let us consider the piezomagnetic tensor where B is the magnetization and F is the mechanical stress. According to Table S4, this tensor corresponds to tBtA=-1 and is an axial tensor. When  t=E, all X terms of Eq. (S5) are M. As a result, oxylene exhibits the piezomagnetic effect. Similarly, one can show that oxylene also exhibits the piezoelectric effect and the magnetic spin Hall effect by considering the relevant symmetry-allowed terms.

Table S1. Classification of rank-l multipole according to parity P and time-reversal property T.

| Electric multipole Q | Electric toroidal multipole G | Magnetic multipole M | Magnetic toroidal multipole T |
| --- | --- | --- | --- |
| (P,T)=(-1l,1) | (P,T)=(-1l+1,1) | (P,T)=(-1l+1,-1) | (P,T)=(-1l,-1) |

Table S2. Active multipoles in the magnetic point group 3m' up to third order. Here, X0X=Q,G,M,T is the monopole, and Xx,y,z are the dipoles corresponding to x, y, and z, respectively. Xu is the quadrupole of 1233z2-r2, and X3a, X3b and Xzα are the octupoles of 104xx2-3y2, 104y-y2+3x2, and 12z5z2-3r2, respectively.

| Q | G | M | T |
| --- | --- | --- | --- |
| Q0,Qz,Qu,Qzα,Q3b | G3a | M0,Mz,Mu,Mzα,M3b | T3a |

Table S3. Classification of χ[1⨂1].

|  | tBtA=1 | tBtA=-1 |
| --- | --- | --- |
| Polar tensor | Magnetic susceptibility tensor, | Electric conductivity tensor |
| Axial tensor | Electric-field induced rotation Rotation-electric field induced electric dipole6 | Magnetoelectric tensor |

Table S4. Detailed information of χ.

|  | tBtA=1, t=Jt=E | tBtA=-1, t=Jt=E |
| --- | --- | --- |
| Polar tensor | X=TQ,Y=MG | X=QT,Y=GM |
| Axial tensor | X=MG,Y=TQ | X=GM,Y=QT |

Table S5. Classification of χ[2⨂1].

|  | tBtA=1 | tBtA=-1 |
| --- | --- | --- |
| Polar tensor | Piezoelectric tensor |  |
| Axial tensor | Spin conductivity tensor | Piezomagnetic tensor |

References

- Yatsushiro, M., Kusunose, H. & Hayami, S. Multipole classification in 122 magnetic point groups for unified understanding of multiferroic responses and transport phenomena. Phys. Rev. B 104, 054412 (2021).

- Hayami, S., Yatsushiro, M., Yanagi, Y. & Kusunose, H. Classification of atomic-scale multipoles under crystallographic point groups and application to linear response tensors. Phys. Rev. B 98, 165110 (2018).

- Šmejkal, L., Sinova, J. & Jungwirth, T. Beyond conventional ferromagnetism and antiferromagnetism: a phase with nonrelativistic spin and crystal rotation symmetry. Phys. Rev. X 12, 031042 (2022).

- Suzuki, M.-T., Koretsune, T., Ochi, M. & Arita, R. Cluster multipole theory for anomalous Hall effect in antiferromagnets. Phys. Rev. B 95, 094406 (2017).

- Nakatsuji, S., Kiyohara, N. & Higo, T. Large anomalous Hall effect in a non-collinear antiferromagnet at room temperature. Nature 527, 212 (2015).

- Nayak, A. K. et al. Large anomalous Hall effect driven by a nonvanishing Berry curvature in the noncolinear antiferromagnet Mn3Ge. Sci. Adv. 2, e1501870 (2016).

- Ikhlas, M. et al. Large anomalous Nernst effect at room temperature in a chiral antiferromagnet. Nat. Phys. 13, 1085 (2017).

- Hong, D. et al. Large anomalous Nernst and inverse spin-Hall effects in epitaxial thin films of kagome semimetal Mn3Ge. Phys. Rev. Mater. 4, 094201 (2020).

- Higo, H. et al. Large magneto-optical Kerr effect and imaging of magnetic octupole domains in an antiferromagnetic metal. Nat. Photon. 12, 73 (2018).

- Wu, M. et al. Magneto-optical Kerr effect in a non-collinear antiferromagnet Mn3Ge. Appl. Phys. Lett. 116, 132408  (2020).

- Kimata, M. et al. Magnetic and magnetic inverse spin Hall effects in a non-collinear antiferromagnet. Nature 565, 627 (2019).

- Ikhlas, M. et al. Piezomagnetic switching of the anomalous Hall effect in an antiferromagnet at room temperature. Nat. Phys. 18, 1086 (2022).

- Kubo, R. Statistical-mechanical theory of irreversible processes. I. General theory and simple applications to magnetic and conduction problems. J. Phys. Soc. Jpn. 12, 570-586 (1957).

- Sakurai, J. J. Modern quantum mechanics (Massachusetts, 1994, Addison-Wesley).

- Oiwa, R. & Kusunose, H. Rotation, Electric-field responses, and absolute enantioselection in chiral crystals. Phys. Rev. Lett. 129, 116401 (2022).