Supplementary Materials for

Horizontally Arranged Zinc Platelet Electrodeposits Modulated by Fluorinated Covalent Organic Framework Film for High-Rate and Durable Aqueous Zinc Ion Batteries

Zedong Zhao§1, Rong Wang§1, Chengxin Peng*2, Wuji Chen1, Tianqi Wu1, Bo Hu1, Jiaxi Zeng1, Peiying Liu1, Yicheng Liu1, Jia Guo*1, Hongbin Lu* and Zaiping Guo*3

1State Key Laboratory of Molecular Engineering of Polymers, Department of Macromolecular Science

Fudan University, 2005 Songhu Road, Shanghai 200438, China;

2School of Materials Science & Engineering, University of Shanghai for Science and Technology, Shanghai 200093, China

3Chemical Engineering & Advanced Materials, The University of Adelaide, Adelaide, SA 5005, Australia

§Both these authors contributed equally to this work

Supplementary Figures

Supplementary Fig. 1:  Comparison of the synthesis conditions of the FCOF films. a: Photos of the solvothermal glass tubes with different reaction conditions and b: Corresponding details of the ingredients and obtained products.

Supplementary Fig. 2: Product comparison after reaction. a: Photos of the solvothermal glass tubes showing the obtained FCOF films from different reaction conditions. b: the solutions taken out of the tubes after reaction. c: FESEM image showing uniform-size nano spheres in a typical suspension.

Supplementary Fig. 3: FESEM images of the FCOF films prepared with different D/M ratios. The results show that increasing the D/M ratio is important to achieve a high quality film.

Supplementary Fig. 4: FESEM images of the FCOF film grown on silicon substrate at different reaction times. The results show that the growth mechanism of the FCOF film assembly and fusion of the nano-spheres suspended in the reaction solution.

Supplementary Fig. 5: The transferring process of the FCOF film from the glass tubes.

Supplementary Fig. 6: Photos and FESEM images of the FCOF films grown on various substrates including Cu, Si, Ni, Stainless Steel (SS), Ti and SS grid.

Supplementary Fig. 7: TEM image of the FCOF film and the corresponding EDX results of C, F, and N elements.

Supplementary Fig. 8: XPS full energy spectrum of FCOF film and atomic ratio of C, N, and F elements.

Supplementary Fig. 9: AFM results of the FCOF films. Three different thickness: a ~100nm, b ~250nm and c ~500nm of the films are prepared.

Supplementary Fig. 10: Characterization of Zn2+ ion transport behavior of the FCOF films. a EIS results of the symmetric cells in SS/FCOF@GF or bare GF /SS configurations (immersed in 2M ZnSO4). b Calculated ion conductivity based on the EIS results. c The EIS results of the symmetric cells in FCOF@Zn/FCOF@Zn configurations. d Simulated Rct of the symmetric cells according to the equivalent circuit (inset).

Supplementary Fig. 11: Calculation of Zn2+ transference number (ZTN) based on the chronoamperometric tests (I-t tests) under a polarization of 20 mV. a The calculated ZTN for the FCOF@Zn or bare Zn symmetric cells. The EIS results of the b FCOF@Zn or c bare Zn symmetric cells before and after polarization (I-t test). Note that the symmetric cells are rested for 2-3h to ensure the accuracy of the test, therefore the impedance is higher than the that of Supplementary Fig. 10c. The I-t curves of the of the d FCOF@Zn or e bare Zn symmetric cells. Considering the EIS results remain nearly unchanged before and after polarization, the ZTN can be calculated by using the simplified equation I/I0, where I0 represents the initial current and I represents the equilibrium current.

Supplementary Fig. 12: Comparison of the electrolyte anticorrosion property of the FCOF@Zn and bare Zn anodes. Time-dependent EIS results of the a FCOF@Zn or b bare Zn symmetric cells. c Time-dependent XRD patterns of the FCOF@Zn and bare Zn anodes after immersing in 2M ZnSO4.

Supplementary Fig. 13: The calculated texture coefficients of different crystal planes of Zn.

The preferred orientations of Zn deposits can be determined calculating the texture coefficient (Tc) according to equation:

Tc=Ihkl/I0(hkl)1n(Ihkl/I0(hkl))

where 𝐼(ℎ𝑘𝑙) is the peak intensity of zinc electrodeposits and ∑ I is the sum of the intensities of independent peaks. The index 0 refers to the intensities for the standard Zn sample taken from a powder diffraction file (PDF) card (PDF# 99-0110). n is the number of diffraction planes considered in the analysis.

Supplementary Fig. 14: The EDX results of a Zn platelet after stripping off the FCOF film under HRTEM test.

Supplementary Fig. 15: The electrochemical performance of Zn anodes. a: CE of Zn plating/stripping on FCOF film- coated Ti and bare Ti at 1 mAh/cm2, 5 mA/cm2. b-e: The voltage profiles at selected cycles. The insets are enlarged voltage profiles. f: Cycling performance of Zn symmetric cells with or without FCOF film protection at g: 1 mAh/cm2 and 8 mA/cm2.

Supplementary Fig. 16: AFM characterization of Zn deposits after cycling (100 cycles at 1mAh/cm2, 5mA/cm2). a-b Phase and c-d height imaging of Zn deposits on FCOF film coated or bare Ti. (C) Height profiles along X (blue) and Y(red) axis of Zn deposits on e: FCOF film coated or f: bare Ti.

Supplementary Fig. 17: Raman spectra of the Zn deposits after cycling on a: bare Ti and b: FCOF coated Ti. The dominant peak at 967 cm-1 is chosen to show the Raman mapping.

| Ref (Ti/Zn asymmetric cell) | Capacity | Current Density | Cycle number |
| --- | --- | --- | --- |
| Angew. Chem. Int. Ed. 2021, 60, 2–9 | 1 mAh/cm2 | 0.5 mA/cm2 | 50 |
| Angew.Chem. Int. Ed. 2020, 59,19292 –19296 | 0.5 mAh/cm2 | 1 mA/cm2 | 300 |
| J. Mater. Chem. A, 2021, 9, 5597-5605 | 0.5 mAh/cm2 | / | 300 |
| Nano-Micro Lett. (2021) 13:79 | 5 mAh/cm2 | 5 mA/cm2 | 14 |
| Energy Environ. Sci., 2019, 12, 1938-1949 | 0.4 mAh/cm2 | 0.4 mA/cm2 | 300 |
| Advanced Functional Materials, 2020, 30(13): 1908528. | 1 mAh/cm2 | 5 mA/cm2 | 210 |
| Materials Today Energy 18 (2020) 100563 | 2.5 mAh/cm2 | 2.5 mA/cm2 | 60 |
| Advanced Functional Materials, 2021, 31(2): 2001867. | 0.885 mAh/cm2 | 1.77 mA/cm2 | 1000 |
| J. Am. Chem. Soc. 2020, 142, 21404−21409 | 0.5 mAh/cm2 | 1 mA/cm2 | 400 |
| Energy Storage Materials 27 (2020) 1–8 | 0.5 mAh/cm2 | 0.5 mA/cm2 | 50 |
| Advanced Materials, 2020, 32(33): 2003425. | 1 mAh/cm2 | 2 mA/cm2 | 20 |
| Journal of Materials Chemistry A, 2020, 8(34): 17725-17731. | / | 1 mA/cm2 | 300 |
| Nature communications, 2019, 10(1): 1-12. | 1 mAh/cm2 | 0.5 mA/cm2 | 45 |
| Present work | 1 mAh/cm2 | 5 mA/cm2 | 480 |
| Present work | 1 mAh/cm2 | 80 mA/cm2 | 320 |
| Present work | 2 mAh/cm2 | 40 mA/cm2 | 260 |

Supplementary Table 1: Cycle number and current density comparison of CE of Zn plating/stripping for the reported Zn aqueous batteries.

| Ref (symmetric cell) | Capacity | Current Density | Cycle life |
| --- | --- | --- | --- |
| ACS Energy Letters, 2020, 5(9): 3012-3020. | 2 mAh/cm2 | 10 mA/cm2 | 400 h |
| ACS Energy Lett. 2021, 6, 395−403 | 0.067 mAh/cm2 | 0.2 mA/cm2 | 170 h |
| ACS Energy Lett. 2021, 6, 675−683 | 0.1 mAh/cm2 | 5 mA/cm2 | 370 h |
| Adv. Energy Mater. 2021, 11, 2003419 | 1 mAh/cm2 | 4 mA/cm2 | 116 h |
| Adv. Funct. Mater. 2021, 31, 2006495 | 0.1 mAh/cm2 | 0.1 mA/cm2 | 200 h |
| Adv. Mater. 2021, 33, 2007497 | 1 mAh/cm2 | 4 mA/cm2 | 300 h |
| Adv. Mater. 2021, 2007416 | 1 mAh/cm2 | 5 mA/cm2 | 220 h |
| Adv. Mater. 2021, 2007388 | 1 mAh/cm2 | 1 mA/cm2 | 800 h |
| Adv. Mater. 2021, 2007406 | 1 mAh/cm2 | 5 mA/cm2 | 2500 h |
| Energy Storage Materials 36 (2021) 132–138 | 1 mAh/cm2 | 2 mA/cm2 | 400 h |
| Journal of Energy Chemistry 55 (2021) 549–556 | 0.5 mAh/cm2 | 0.5 mA/cm2 | 240 h |
| Nano-Micro Lett. (2021) 13:79 | 1 mAh/cm2 | 1 mA/cm2 | 2000 h |
| Nano Energy 80 (2021) 105478 | 0.5 mAh/cm2 | 5 mA/cm2 | 800 h |
| Angew. Chem. Int. Ed. 2021, 60, 2–9 | 0.2 mAh/cm2 | 1 mA/cm2 | 800 h |
| Nature communications, 2020, 11(1): 1-9. | 1 mAh/cm2 | 0.5 mA/cm2 | 2000 h |
| Nature communications, 2020, 11(1): 1-7. | 1 mAh/cm2 | 1 mA/cm2 | 460 h |
| Energy & Environmental Science, 2020, 13(2): 503-510. | 1.25 mAh/cm2 | 5 mA/cm2 | 500 h |
| Nature materials, 2018, 17(6): 543-549. | 0.033 mAh/cm2 | 0.2 mA/cm2 | 170 h |
| Present work | 1 mAh/cm2 | 5 mA/cm2 | 1700 h |
| Present work | 1 mAh/cm2 | 40 mA/cm2 | 700 h |

Supplementary Table 2: Cycle life comparison of symmetric Zn cells in reported Zn aqueous batteries.

Supplementary Fig. 18: FESEM images of the Zn anode surface after long cycling. The morphologies of a FCOF@Zn and b bare Zn anode.

Supplementary Fig. 19: The characterization of the FCOF film after cycling. a HRTEM image clearly shows the interlayer spacing of 0.34nm, indicating the well-maintained 2D stacked structure. b FTIR results before and after cycling show the obvious peak density of the C=N bond, demonstrating the strong stability of the covalent linked chemical structure in FCOF films.

Supplementary Fig. 20: Electrochemical results of the full cells. a 1st and 2nd CV curves of FCOF@Zn-MnO2 and Zn-MnO2 full cells. b 1st and 2nd charge/discharge profiles of the FCOF@Zn-MnO2 and Zn-MnO2 full cells. c EIS results of FCOF@Zn-MnO2 and Zn-MnO2 full cells. The 50th, 250th, 500th and 750th charge/discharge profiles of e FCOF@Zn-MnO2 and d Zn-MnO2 full cells

Supplementary Fig. 21: Electrochemical results of the FCOF@Zn-MnO2 full cells at depth of discharge (DOD) of 10% and 20%, respectively. The charge/discharge profiles and FESEM images of the FCOF@Zn anodes after long cycling at N/P ratio of a, b 10:1 and c, d 5:1.

Supplementary Fig. 22: Pictures of the flexible transparent battery.

Supplementary Fig. 23: EIS results of the flexible battery at different bending angles.

Supplementary Fig. 24: XPS results of the F 1s and Zn 2p at the FCOF-Zn interface.