Supplementary Information

Development of Intervertebral Disc Organoids through Directed Differentiation of Mesenchymal Stem Cells and Hierarchical Bioprinting

Di Wu1#, Dingchao Zhu1#, Xingyu Zhou1#, Gaocai Li1#, Xiaoguang Zhang1, Liang Ma1, Huaizhen Liang1, Bide Tong1, Jie Lei1, Hongchuan Wang1, Xiaobo Feng1, Kun Wang1, Lei Tan1*, Yunsong Shi2*, Cao Yang1*, Bingjin Wang1*

Affiliations

1 Department of Orthopaedics, Union Hospital, Tongji Medical College, Huazhong University of Science and Technology, Wuhan 430022, China.

2 Department of Stomatology, Union Hospital, Tongji Medical College, Huazhong University of Science and Technology, Wuhan 430022, China.

Figure S1. a) Principal component analysis between different groups. b) Heatmap showing DEGs between each group. c) DEGs associated with secondary NP differentiation genes. d) DEGs associated with AF-specific genes and inflammatory markers. e) DEGs associated with the secretion of ECM. n=3 independent experiments per group.

Figure S2. Preparation of GelMA with modification by Folic acid and HAMA with modification by β-CD. a) 1H NMR (400MHz, DMSO-d6,) spectra of GelMA and GelMA-FA. The new resonance peaks in the folate region (blue) of the GelMA-FA spectrum indicated successful conjugation of the folic acid motifs. b) 1H NMR (400MHz, D2O) spectra of HAMA and HAMA-βCD. The new resonance peaks in the βCD region (yellow) of HAMA-βCD. The spectrum indicated successful conjugation of the β-CD motif.

Figure S3. Immunofluorescence staining for CD24, IBSP, and NCAM1 indicated that the HG and SilMA hydrogels and the NP and AF differentiation media had synergistic effects on the ECM secretion of NPOs and AFOs at 7,14,21 days. Scale bar: 50 μm.

Figure S4. Cell viability test of a) HG and c) SilMA hydrogels for 3D bioprinted organoids. Live-dead assay of hMSCs in b) the HG hydrogel and d) SilMA after culturing for 1, 4, 7, or 14 days (live cells: green fluorescence; dead cells: red fluorescence). Scale bar: 400 μm. n=3 independent experiments per group.

Figure S5. a) Morphology and shape parameters of IVDs obtained from MR images. Photographs of 3D-printed b) AF scaffolds and c) NP scaffolds taken from different views. Scale bars: 5mm. d) Photographs of freeze-dried IVD scaffolds. Scale bars: 5mm. e) Scanning electron microscopy of freeze-dried IVD scaffolds revealed a porous structure. Scale bars: 60μm.

Figure S6. a) Representative mid-sagittal T2 MR images showing differences in the IVD across treatment groups. b) Reconstruction results of CT images showing the formation of vertebral osteophytes.

Table S1. PCR primer sequences

| Genes | Forward primer | Reverse primer |
| --- | --- | --- |
| GAPDH | AATCCCATCACCATCTTCCAG | GAGCCCCAGCCTTCTCCAT |
| COL2A1 | TGTCCATTCATCCCACCCT | CACCAGTTAGTTTCCTGCCTCT |
| CD24 | AATTTCCCCATCTTCTAAACCC | TTGGCATCCATCATCTAGTCAA |
| ACAN | ACCACTTTACTCTGGGTTTTCG | ACACGGCTCCACTTGATTCTT |
| NCAM1 | GTGGATAAGAACGACGAGG | CGGAGGCTTCACAGGTAA |
| COL1A1 | GATTGACCCCAACCAAGGC | GAATCCATCGGTCATGCTCT |
| COL5A1 | CCGATTGGCTACCCAGGTC | CACCCTTGATGCCCATGTCT |
| IBSP | AGGGCAGTAGTGACTCATCCG | AGCCCAGTGTTGTAGCAGAAAG |
| TNMD | TTGGTATCCTGGCCCTAA | CAGTGCCATTTCCGCTTC |
| BGLAP | GACAAGTCCCACACAGCAACT | GGACATGAAGGCTTTGTCAGA |

Table S2. Antibody list

| Antibody | Cat No. | Manufacturer |
| --- | --- | --- |
| Col2A1 | 28459-1-AP | Proteintech |
| KRT19 | 10712-1-AP | Proteintech |
| GAPDH | 60004-1-Ig | Proteintech |
| β-actin | 66009-1-Ig | Proteintech |
| α-tubulin | 66031-1-Ig | Proteintech |
| Col1A1 | 14695-1-AP | Proteintech |
| CD24 | 10600-1-AP | Proteintech |
| Col5A1 | DF3551 | Affinty |
| TNMD | DF13715 | Affinty |
| IBSP | DF7738 | Affinty |
| FBLN1 | DF9516 | Affinty |