Synthesis, Characterisation and Cytotoxicity of Gold Nanowires for Ultra-Sensitive Biosensor Development

# 1Nurul Akmal Che Lah, 2Robert Gray & 3*Sonia Trigueros

1Innovative Manufacturing, Mechatronics and Sports Lab (iMAMS), Faculty of Manufacturing and Mechatronics Engineering Technology, University Malaysia Pahang, 26600, Pekan, Pahang, Malaysia.

2University College London, Gower St, Bloomsbury, London, WC1E 6BT, United Kingdom.

3.Department of Zoology, University of Oxford, OX1 3PS, Oxford, United Kingdom.

*Correspondence: Sonia Trigueros

email: sonia.trigueros@zoo.ox.ac.uk

Assembly on Cantilever

AuNWs were assembled onto a cantilever surface by AuNWs-ethanol droplets evaporation method. Aluminium-coated cantilevers (Concentric GmbH-Switzerland) with 400 μm long, 1 μm thick and 100 μm wide were used in the process. 20 µl of the colloidal solution was sonicated using an ultrasonic bath for 15 min. A 5 μl drop of the solution was added onto the cantilever surface. After letting the dropping air dry for 24 h, AuNWs adhered to the surface. The AuNWs assembly was imaged using FESEM.

Integrating AuNWs onto a cantilever is crucial for the exploration of a multifunctional MC biosensor. To functionalise the cantilever, AuNWs were attached to an aluminum coated AFM cantilever surface. The surface of the cantilever was covered with AuNWs solution, and the nanowires on the surface repel each other and assemble. In this case, for the functionalisation process, we used commercial AuNWs and the evaporation process described in material and methods. The resulting attachment between the surface of the cantilever and AuNWs is shown in Figure S1. This assembly is adequate for MC biosensor functionalisation viability. Here, we demonstrated a direct depositing of AuNWs and its binding tendency onto the cantilever.

Figure S1: FESEM micrograph of commercial AuNWs deposited on the aluminium-coated AFM cantilever surface. The formation of the scaffold is due to the coffee-ring effect during the evaporation process. AuNWs are deposited along the solid-liquid contact line.

The undoubted benefit of the MC surface Au nano-structuration is the expansion of the cantilever limited sensitive range. It is well-known that one of the utmost drawbacks of micro or nanoscale sensors is their low dynamic range. A higher-performance functional surface of AuNWs could increase the binding capacity, and therefore, increasing the sensor detection to a broader range of molecule type and concentrations.

Minimising the thickness and width of the sensing element is also essential to retain an excellent signal efficiency from a strain-sensing component of MC sensor. The thickness of the AuNWs is in the range of 80 – 100 nm and width of 2.47 mm, which rules out the employment of sensors made of conventional self-sensing elements including Si and PZT. The small diameter with a much longer length of AuNWs permits the fabrication of strain sensors on small MCs without significantly affecting their dynamic properties. Also, the achievable wider sensor length is crucial in maintaining low resistance and a very high sensitive detection bandwidth. Altogether, the fabrication example in this study highlights the potential multifunctional design of AuNWs-based MC probes. Also, take into account that bulk fabrication of the MC probe at the larger scale could be possible.

Although, the thinner AuNWs the better to increase the nanosensor sensitivity, commercial AuNWs are ideal for the MC deposition. Therefore, more studies need to be undertaken to elucidate the synthesis of thinner and stable AuNWs with both high defect characteristic and intrinsic quality to allow better operation and function at a higher temperature.