Table S1: Constant compositional expansion (CCE) analysis of used oil

| Components | Reservoir oil (Mol %) |
| --- | --- |
| H2S | 0.13 |
| N2 | 0.30 |
| CO2 | 3.33 |
| C1 | 26.50 |
| C2 | 7.37 |
| C3 | 4.51 |
| iC4 | 0.60 |
| nC4 | 2.03 |
| iC5 | 2.49 |
| nC5 | 2.96 |
| C6 | 7.56 |
| C7 | 4.44 |
| C8 | 3.77 |
| C9 | 2.82 |
| C10 | 3.35 |
| C11 | 3.29 |
| C12* | 24.53 |
| Total | 100.00 |
| GOR, SCF/STB | 323 |

Table S2: Used crude oil specification

| Components | Weight Percent |
| --- | --- |
| Saturations | 49.5 % |
| Aromatics | 30 % |
| Asphaltene | 11.4 % |
| Resin | 9.1 % |

Figure S1: TEM image (left), HR-TEM image (right), and lattice spacing of the E5_L CDs sample.

Figure S2: XRD spectra of CD samples (E5_L, U5_L, and T5_L)

|  |  | E5_L CDs |
| --- | --- | --- |
|  |  | U5_L CDs |
|  |  | T5_L CDs |

Figure S3: UV-Vis spectrum (first column), photoluminescence at 360 nm (second column) spectra, and solution under UV light (third column) for E5_L, U5_L, and T5_L CDs

Figure S4: FTIR spectra of E5_L, U5_L and T5_L CDs

|  |  |  |  | C1s |
| --- | --- | --- | --- | --- |

Figure S5: XPS spectra of E5_L, U5_L, and T5_L CDs. The first row presents the full scan survey, and the second, third, and fourth rows display the high-resolution spectra for E5_L, U5_L, and T5_L CDs, respectively. The first, second, and third columns correspond to the high-resolution C1s, N1s, and O1s XPS spectra.

Figure S6: High-resolution XPS spectra of the S2p region for T5_L CDs.

Figure S7: IFT value of crude oil and different NaCl concentrations with 1000 ppm of T5_L and T10_L CDs

Figure S8: IFT value of crude oil and various NaCl concentrations in the presence of 1000 ppm T5_L and T5_M CDs

Figure S9: IFT value of crude oil and different MgCl2 concentrations with 1000 ppm of U5_L, U5_M, and U5_H CDs

Figure S10: IFT value of crude oil and different CaCl2 concentrations with 1000 ppm of T5_L and T5_M CDs