Supplementary Materials for

Shear Strain Control of Multiferroic Magnetic Ordering for Giant Ferromagnetism

Guoqiang Xi1†, Yue-Wen Fang2,3†, Dongxing Zheng4†, Shuai Xu5, Hangren Li1, Jie Tu1, Fangyuan Zhu6, Xudong Liu1, Xiuqiao Liu1, Xixiang Zhang4, Kuijuan Jin5, Jianjun Tian1, Linxing Zhang1*

1Institute for Advanced Materials Technology, University of Science and Technology Beijing, Beijing 100083, China

2Fisika Aplikatua Saila, Gipuzkoako Ingeniaritza Eskola, University of the Basque Country (UPV/EHU), Europa Plaza 1, 20018 Donostia/San Sebastián, Spain

3Centro de Física de Materiales (CSIC-UPV/EHU), Manuel de Lardizabal pasealekua 5, 20018 Donostia/San Sebastián, Spain

4Physical Science and Engineering Division, King Abdullah University of Science and Technology (KAUST), Thuwal 23955–6900, Saudi Arabia

5Beijing National Laboratory for Condensed Matter Physics, Institute of Physics, Chinese Academy of Sciences, Beijing 100190, China

6Shanghai Synchrotron Radiation Facility, Shanghai Advanced Research Institute, Chinese Academy of Sciences, Shanghai 201204, China

†These authors contributed equally.

*Correspondence to: linxingzhang@ustb.edu.cn

Figure S1 (a, b) Synchrotron X-ray total reflection (XRR) of T’-BFO and O-BFOS thin films.

The film thicknesses were measured using XRR, determining the T’-BFO and O-BFOS film thicknesses to be 78 nm and 80 nm, respectively. The thickness d had been calculated by the equation of d = λ/2sinΔθ, where λ = 1.5466 Å, Δθ is half of the average width of the peak obtained by the XRR measurement.

Figure S2 (a) Cross-sectional TEM image of T’-BFO thin film. (b) HAADF-STEM image at the interface between T’-BFO thin film and LAO substrate (a-axis direction).

Figure S3 (a, b) (103) plane synchrotron RSM of T’-BFO and O-BFOS thin films.

Figure S4 Large-scale cross-section HAADF-STEM of the O-BFOS thin film along the a-axis direction and FFT in a, b, and c regions.

Figure S5 (a) STEM-EDS elemental maps of the O-BFOS thin film. (b) The energy integral of the corresponding element mapping, with the inset representing the proportion of Bi, Fe, O, and S atoms obtained from the integration.

Figure S6 Optical second-harmonic generation (SHG) intensity of T’-BFO and O-BFOS thin films at room temperature.

SHG indicates diminished spatial-inversion symmetry breaking in O-BFOS films, which implies a reduction in ferroelectricity of the film. It is well known that the symmetry of O-phase is higher compared to monoclinic MC-phase, so the ferroelectricity of O-phase O-BFOS films is relatively weaker, which is an important reason for the weakening of SHG signals of O-BFOS films after sulfurization.

Figure S7 (a, b) Out-of-plane and in-plane magnetic hysteresis loops of T’-BFO films and O-BFOS films at 300 K.

Figure S8 Schematic of Fe 3d orbital in different crystal fields.

According to the crystal field theory, the Fe 3d orbital will split into a low-energy t2g and a high-energy eg orbital when the Fe ion is located at the centra of the FeO6 octahedron. The lattice is stretched along the c-axis when the film is subjected to clamping stresses from the LAO substrate, the splitting of the t2g and eg orbitals will be further increased when ideally the Fe ions are located at the FeO6 octahedron. For the T’-BFO film, the c/a can reach to ~1.23 causing Fe ions to offset from the centra of the FeO6 octahedron due to the LAO substrate clamping stress exceeding 4.5%, resulting in a greatly weakened hybridization of Fe ions with O ions at the bottom of FeO6 octahedron to form the pyramid-like of the FeO5 structure. For the O-BFOS film, the lattice distortion induced increases the hybridization of the Fe ions with the O ions by the S ions, the electron loss of Fe ions increases and tends to +3, thus the electron hybridization returns to the FeO6 octahedral