Translucent Color Organic Solar Cells: From Power Generating Windowpanes to Aesthetic Art

Baozhong Deng1#, Yi Li1#, Kaiwen Zheng1, Zhouyi Lu1, Tao Xu1*, Shenghao Wang2, Xiaoshu Luo3, Bruno Grandidier4, Jianhua Zhang1*, and Furong Zhu5*

1. School of Microelectronics, Shanghai University, 200444 Shanghai, China

2. Materials Genome Institute, Shanghai University, 200444 Shanghai, China

3. Shanghai Academy of Fine Arts, Shanghai University, 200444 Shanghai, China

4. Université de Lille, CNRS, Centrale Lille, Université Polytechnique Hauts-de-France, Junia-ISEN, UMR 8520 - IEMN, 59000 Lille, France

5. Department of Physics, Research Centre of Excellence for Organic Electronics and Institute of Advanced Materials, Hong Kong Baptist University, Kowloon Tong, Hong Kong, China,

# These authors contributed equally to this work.

E-mail: xtld@shu.edu.cn, jhzhang@oa.shu.edu.cn,  frzhu@hkbu.edu.hk

Figure S1. Absorption spectra of PM6 and L8-BO.

Figure S2. (a) J−V characteristics and (b) EQE spectra of 4.14 mm2-sized PM6:L8-BO opaque OSCs, fabricated using different BHJ active layer thicknesses, prepared at varying spin-coating speeds.

Figure S3. (a) Wavelength-dependent refractive indexes and (b) extinction coefficients of the function layers used in this work.

Figure S4. CIE chromaticity coordinates of the blue, green and red ST-OSCs.

Figure S5. Reflection spectra of the blue, green and red ST-OSCs.

Figure S6. (a) QUE spectra and (b) EQE+T+R spectra obtained for the blue, green, and red ST-OSCs. The transmission spectrum measured for the glass/ITO substrate is also shown for comparison.

Figure S7. (a) J−V characteristics, (b) EQE spectra and (c) photographs of the 1.0 cm2-sized opaque OSC, blue, green and red ST-OSCs.

Figure S8. The stability of the control opaque OSC, blue, green, and red ST-OSCs stored in a N2-purged glove box.

Figure S9. Profiles of the exciton generation in the active layers of the opaque device, blue, green, and red ST-OSCs.

Figure S10. (a) J−V characteristics and (b) EQE spectra measured for the 1.0 cm2-sized navy, sky blue, azure, yellow, vermilion, and brown ST-OSCs.

Figure S11. Reflection spectra measured for the navy, sky blue, azure, yellow, vermilion, and brown ST-OSCs.

Figure S12. (a) QUE spectra and (b) EQE+T+R spectra obtained for the navy, sky blue, azure, yellow, vermilion, and brown ST-OSCs.

Figure S13. Illustration of the slot-die coating process.

Figure S14. Schematic diagram illustrating the multi-step selective-area evaporation process for fabricating a 100 cm2-sized color ST-OSC module having different microcavity optical coupling layers.

Figure S15. An enabling translucent color BIPV technology: From power generating windowpanes to aesthetic art.

Table S1. Summary of photovoltaic parameters measured for the 4.14 mm2-sized PM6:L8-BO opaque devices, fabricated with BHJ active layer, which was prepared at varying spin-coating speeds. The results were averaged from the measurements of 15 cells.

| Rotation speed | VOC (V) | JSC (mA/cm2) | Jcal (mA/cm2) | FF (%) | PCE (%) |
| --- | --- | --- | --- | --- | --- |
| 2500 | 0.86±0.01 | 26.49±0.15 | 26.05 | 78.05±0.37 | 17.83±0.16 |
| 3000 | 0.86±0.01 | 26.42±0.13 | 25.90 | 78.74±0.23 | 17.97±0.14 |
| 3500 | 0.87±0.01 | 26.39±0.24 | 25.80 | 78.95±0.56 | 18.03±0.19 |
| 4000 | 0.86±0.01 | 26.00±0.27 | 25.65 | 79.01±0.43 | 17.74±0.23 |

Table S2. Summary of photovoltaic parameters measured for the large-area opaque device, opaque device, blue, green and red ST-OSCs. The results were averaged from the measurements of 15 cells, with an effective area of 1 cm2.

|  | VOC (V) | JSC (mA/cm2) | Jcal (mA/cm2) | FF (%) | PCE (%) |
| --- | --- | --- | --- | --- | --- |
| Opaque | 0.86±0.01 | 25.74±0.14 | 25.44 | 66.90±0.48 | 14.87±0.20 |
| Blue | 0.86±0.01 | 23.50±0.22 | 23.22 | 66.76±0.38 | 13.52±0.10 |
| Green | 0.86±0.01 | 23.25±0.16 | 23.02 | 65.48±0.57 | 13.06±0.14 |
| Red | 0.86±0.01 | 22.92±0.10 | 22.42 | 65.74±0.50 | 12.95±0.13 |

Table S3. Summary of microcavity configuration optimized for making navy, sky blue, azure, yellow, vermilion, and brown ST-OSCs.

| Color | Configuration of microcavity optical coupling layers |
| --- | --- |
| Navy | Ag(35 nm)/ZnS(40 nm)/Ag(35 nm) |
| Skyblue | Ag(20 nm)/ZnS(38 nm)/Ag(15 nm) |
| Azur | Ag(12 nm)/ZnS(35 nm)/Ag(10 nm) |
| Yellow | Ag(30 nm)/LaF3(130 nm)/Ag(30 nm) |
| Vermilion | Ag(35 nm)/MoO3(104 nm)/Ag(30 nm) |
| Brown | Ag(60 nm)/MoO3(106 nm)/Ag(60 nm) |

Table S4. Summary of photovoltaic parameters measured for the 1.0 cm2-sized navy, sky blue, azure, yellow, vermilion, and brown ST-OSCs. The results were averaged from the measurements of 15 cells.

| Device | VOC (V) | JSC (mA/cm2) | Jcal (mA/cm2) | FF (%) | PCE (%) | TMAX (%) | Peak (nm) | Color coordinates |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Navy | 0.859±0.001 | 24.54±0.21 | 24.42 | 66.01±0.22 | 13.91±0.11 | 20.54 | 436 | (0.1611, 0.0824) |
| Skyblue | 0.859±0.001 | 21.98±0.21 | 21.77 | 65.24±0.14 | 12.31±0.10 | 28.95 | 462 | (0.2195, 0.2627) |
| Azur | 0.858±0.002 | 19.31±0.15 | 19.04 | 63.66±0.55 | 10.55±0.12 | 37.50 | 404 | (0.2396, 0.2921) |
| Yellow | 0.860±0.002 | 22.27±0.16 | 22.18 | 66.22±0.40 | 12.69±0.11 | 25.13 | 583 | (0.3860, 0.4251) |
| Vermilion | 0.860±0.001 | 22.97±0.26 | 22.77 | 66.53±0.34 | 13.14±0.16 | 20.70 | 641 | (0.4775, 0.3301) |
| Brown | 0.863±0.001 | 25.01±0.19 | 24.65 | 66.99±0.44 | 14.46±0.15 | 3.60 | 628 | (0.5569, 0.2979) |

Table S5. A summary of the PCE and Tmax of the color ST-OSCs with small effective area reported by different groups and in this work.

| Reference | Blue ST-OSCs |  | Green ST-OSCs |  | Red ST-OSCs |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | PCE (%) | Tmax (%) | PCE (%) | Tmax (%) | PCE (%) | Tmax (%) |
| Adv. Optical Mater. 2018, 6, 1800051 | 4.54 | 27.7 | 4.46 | 32.1 | 4.31 | 25.7 |
| Adv. Funct. Mater. 2018, 28, 1703398 | 7.8 | 9.4 | 8.1 | 14.5 | 7.2 | 16.6 |
| ACS Appl. Mater. Interfaces. 2019, 11, 18887 | 5.68 | 43 | 5.58 | 36 | 5.48 | 14 |
| ACS Appl. Mater. Interfaces. 2019, 11, 47992 | 8.94 | 16.9 | 8.97 | 24.7 | 8.96 | 24.3 |
| ACS Energy Lett. 2020, 5, 3115 | 14.04 | 31 | 14.6 | 21.8 | 14.28 | 25.2 |
| J. Mater. Chem. C. 2021, 9, 11142 | 13.62 | 15.05 | 13.3 | 9.63 | 13.43 | 5.41 |
| Nano Energy 2021, 80, 105565 | 13.28 | 15.6 | 12.9 | 10.4 | 12.94 | 10.5 |
| Adv. Mater. 2023, 35, 2300360 | 13.3 | 24.9 | 13.3 | 22.2 | 13.4 | 16.6 |
| Adv. Energy Mater. 2023, 13, 2301361 | 15.6 | 13.8 | 15.75 | 21 | 15.7 | 12.9 |
| Adv. Optical Mater. 2024, 12, 2302285 | 13.8 | 37.8 | 13.31 | 28.4 | 13.2 | 27.7 |
| This work | 16.19 | 24.07 | 15.81 | 21.68 | 15.67 | 20.11 |