Supporting Information

Excellent energy storage properties with ultrahigh Wrec in lead-free ferroelectric ceramics via heterogeneous structure design

Qizhen Chaia, Zhaobo Liub, Zhongqi Dengc, Zhanhui Penga, Xiaolian Chaoa, Jiangbo Luc,*,  Houbing Huangb, *, Shujun Zhang,d, *Zupei Yanga, *

* Corresponding authors:

- mail addresses: S. Zhang (shujun@uow.edu.au), Z. Yang (yangzp@snnu.edu.cn)

This PDF file includes:

Fig. S1 to S9

Experimental

References

Fig. S1 a) Ambient-temperature P-E loops and b) Pmax and Pr of (1-x)KNN-xSNZ ceramics measured at 10 Hz under 200 kV cm-1. c) Calculated values of Wrec, Wtotal, and η.

Fig. S2 Ambient-temperature P-E loops of (1-x)KNN-xSNZ ceramics measured under various electric fields of a) x = 0.03, b) x = 0.06, c) x = 0.09, d) x = 0.12. Composition-dependent energy storage parameters (Wrec, Wtotal, and η) of e) x = 0.03, f) x = 0.06, g) x = 0.09, h) x = 0.12, all samples used in this study are 0.1 mm in thickness with electrode area of 0.785 mm2.

Fig. S3 Pmax, Pr, and ΔP under different electric fields of a) x = 0.14, b) x = 0.15, c) x = 0.16, d) x = 0.18.

Fig. S4 a) XRD patterns of (1-x)KNN-xSNZ ceramics measured at ambient temperature. b) Enlarged view of 2θ from 44° to 47°. Temperature-dependent XRD patterns of c) x = 0.03 and d) x = 0.15 ceramics.

Fig. S5 a) Raman spectra of the (1-x)KNN-xSNZ ceramics measured at ambient temperature. b) Composition-dependent wavenumber and FWHM of the v1 mode.

Fig. S6 FE-SEM images of (1-x)KNN-xSNZ ceramics of a) x = 0.03, b) x = 0.06, c) x = 0.09, d) x = 0.12, e) x = 0.14, f) x = 0.15, g) x = 0.16, h) x = 0.18.

Fig. S7 TEM images of (1-x)KNN-xSNZ ceramics of a) x = 0.15, b) x = 0. c) Atomic resolution HAADF-STEM image along [110]c of x = 0.15 ceramic.

Fig. S8 Simulation of the two-dimensional domain structure of (1-x)KNN-xSNZ ceramics of a) x = 0.12, b) x = 0.15, c) x = 0.18, exhibiting the O and T nanodomains in the C matrix.

Fig. S9 Optical transmittance spectra of (1-x)KNN-xSNZ ceramics. a) 3D plots, b) top view, c) left view, and d) front view. e) Visual photograph of (1-x)KNN-xSNZ samples with a thickness of ~0.3 mm.

Experimental

Phase-Field Simulations: To reveal the temporal evolution of the polarization field and the domain structure, we employed the time-dependent Ginzburg-Landau (TDGL) equation [1-4],

∂Pir,t∂t=-LδFδPir,t,      (i = 1,2,3)               (S1)

where Pi(r, t) is the polarization, r is the space position, t is time, L is the kinetic coefficient, and F is the total free energy of the system.

The total free energy of the system includes the bulk free energy, the gradient energy, the elastic energy, and the electrostatic energy:

(S2)

where V is the system volume, fbulk represents the Landau bulk free-energy density, fgrad is the gradient energy density, fela is the elastic energy density, and felec is the electrostatic energy density. The bulk free-energy density for a stress-free ferroelectric can be expressed as:

fbulk = a1Pi2 + a11Pi4 + a12Pi2Pj2 + a111Pi6 + a112Pi4Pj2 +a123Pi2Pj2Pk2     (S3)

where a1, a11, a12, a111, a112, a113 are Landau energy coefficients, whose values depend on concentration c and temperature T and determine the thermodynamic behaviors of bulk phases. The gradient energy density is related to the contribution of the domain wall to the total free energy,

fgrad = 12GijklPi,jPk,l                              (S4)

where Pi,j=∂Pi/∂xj, Gijkl is the gradient energy coefficient. The homologous elastic

energy density can be obtained as:

felas=12Cijklεij-εij0εkl-εkl0                      (S5)

where Cijkl is the elastic stiffness tensor, εijis the total strain, εij0 is the electrostrictive stress-free strain, For a given domain structure, the electrostatic energy density is calculated by

felec=fdep+fappel                             (S6)

fdep=-12ε0εrEiEj                              (S7)

fappl=-EiPi                                   (S8)

where ε0 is the vacuum conductivity, r is the dielectric constant, and Ei is the local electric field.

References

[1] L. Chen, J. Shen, J. Appl. Phys. 1998, 83, 5125-5136.

[2] M. Zhou, J. Wang, L. Chen, C. Nan, J. Appl. Phys. 2018, 123, 154106.

[3] H. Pohlmann, J. Wang, B. Wang, L. Chen, Appl. Phys. Lett. 2017, 110, 019901.

[4] J. J. Wang, P. P. Wu, X. Q. Ma, L. Q. Chen, J. Appl. Phys. 2010, 108, 114105.