# Title

Mesoporous SiO2-chitin/MoO3 Nanocomposite: Synthesis, Surface Investigation, Uptake Potential for Pb(II) and Cu(II), and Future Outlook

Authors:

Hany Fathy Heiba [1]*, Asia A. Taha [2], Alaa R. Mostafa [3], Abeer Elsaharty [1], Manal Gomaa [1], Laila A. Mohamed [1].

[1] National Institute of Oceanography and Fisheries, NIOF, Egypt.

[2] Alexandria University, Faculty of science, Department of Chemistry, Alexandria, Egypt.

[3] Alexandria University, Faculty of science, Department of Environmental Sciences, Alexandria, Egypt.

* Corresponding author:

Hany Fathy Heiba: hanyheiba@gmail.com;hf.heiba@niof.sci.eg (https://orcid.org/0000-0001-5253-5670)

# SUPPLEMENTARY MATERIAL

Table S1 Experimental conditions during studying different adsorption parameters.

| Parameter | pH | Time (min) | C0 (mg/L) | Adsorbent mass (g) | Temperature (K) | Agitation speed (rpm) |
| --- | --- | --- | --- | --- | --- | --- |
| pH | 2-7 | 60 | 40 | 0.25 | RT*** | 100 |
| Time (min) | 5*, 6** | 1-60 | 40 | 0.25 | RT | 100 |
| Concentration, C0 (mg/L) | 5*, 6** | 60 | 10 - 60 | 0.25 | RT | 100 |
| Adsorbent mass (g) | 5*, 6** | 60 | 40 | 0.05 - 0.5 | RT | 100 |
| Temperature (K) | 5*, 6** | 60 | 40 | 0.25 | 293 - 318 | 100 |

* in Cu(II) adsorption, ** in Pb(II) adsorption, *** RT = Room Temperature

Table S2. List of chemicals used during the study

| Chemical | Company Name | Purity (Assay) |
| --- | --- | --- |
| Hydrochloric Acid | SIGMA ALDRICH | 36.5 % - 38.0 % |
| Sodium Hydroxide | SIGMA ALDRICH | ≥98.0 % |
| Acetone | SIGMA ALDRICH | ≥99.5 % |
| Acetic Acid | LOBA CHEMIE | >99 % |
| Ammonium heptamolybdate tetrahydrate | SIGMA ALDRICH | > 99.3 % |
| SiO2 | SIGMA ALDRICH | 99.5% trace metals basis |
| Cu(NO3)2 | Merk | 1000 mg/l (>99.9%) |
| Pb(NO3)2 | Merk | 1000 mg/l (>99.9%) |

Fig. S1 FTIR showing SiO2-Chitin supported MoO3 before and after the Cu(II) and Pb(II) loading

Fig. S2 SEM images of A- SiO2-Chitin supported MoO3, B- SiO2-Chitin supported MoO3 + Cu(II), C- SiO2-Chitin supported MoO3 + Pb(II).

Fig. S3 XRD patterns of SiO2-chitin supported MoO3.

Fig. S4 Van't Hoff plot for Cu(II) and Pb(II) adsorption onto SiO2-Chitin supported MoO3.

Fig. S5 Arrhenius plot for Cu(II) and Pb(II) adsorption onto SiO2-Chitin supported MoO3 .