Supporting Information for

ZnO/NiCo2O4@NF self-supporting anode with a mechanical anchoring strategy to enhance the electrochemical performance for lithium-ion batteries

Experimental methods:

The Brunauer–Emmett–Teller (BET, Micromeritics, ASAP 2460) method was used to determine the specific surface area of the sample. And thermal stability of the ZnO/NiCo2O4@NF was tested by a thermogravimetric analyzer (Pyris 1 TGA, Perkin–Elmer), the temperature range was 25–700 °C with heating increment of 20 °C/min under a continuing stream of argon.

Figures：

Fig. S1. TGA curves of the ZnO/NiCo2O4@NF.

Fig. S2. Nitrogen adsorption-desorption isotherms of NF, NiCo2O4@NF, ZnO/NiCo2O4@NF.