Supplementary information

Level Scaling and Pulse Regulating Methods to Mitigate Cycle-to-cycle Variation in Memristor Based Learning System

Zhiheng Liao1, Jingyan Fu1, Jinhui Wang2

___________________________________________________________________

- Department of Electrical and Computer Engineering, North Dakota State University, Fargo, ND, USA.

- Department of Electrical and Computer Engineering, University of South Alabama, Mobile, AL, USA.

This PDF file includes:

Supplementary Figures 1 to 8;

Supplementary Table 1;

Supplementary Note 1;

Supplementary References

Supplementary Figures:

Supplementary Figure S1. exponential formula1 fitting for the LTP/LTD with different width of pulses. The width of pulses is 520 μs, 540 μs, 600 μs, 800 μs, 1000 μs, 1200 μs, 1400 μs, 1600 μs, 1800 μs, and 2000 μs, respectively. The squire dots are experimental data and solid lines are fitting curves.

Supplementary Figure S2. Residual data after exponential formula fitting. We normalized the residual data by dividing the difference of maximum conductance and minimum conductance corresponding width of pulses. Every single point of residual was plotted with order of number of points as X-axis. The squire points are residual value of the LTP and the triangle points are residual value of the LTD with different width of pulses.

Supplementary Figure S3. Gaussian distribution analysis for the residual data after exponential formula fitting. The red and blue lines are Gaussian distribution fitting curves that are LTP and LTD, respectively.  According to Gaussian distribution, the coefficient, α, can be obtained and shown in the supplementary Table 1.

Supplementary Figure S4. The difference of accuracy between ideal case (α=0) and that with c2c variation (α=0.03577). Both cases are under truncation function for an integer number of pulses involved condition. The black squires represent the negative values that means the prediction accuracy with cycle-to-cycle variation is higher than that without the cycle-to-cycle variation. The truncation function for an integer number of pulses is employed for hardware implementation. The updated weight gets the deviation by an integer number of pulses. But when cycle-to-cycle variation is involved in every weight update, sometimes they make the updated weight achieve closer to the accurate number of pulses that algorithm requires and then the system gets even higher prediction accuracy.

Supplementary Figure S5. Prediction accuracy without cycle-to-cycle variation (α = 0) with different LTP and LTD number of levels values (from 10 to 200, step is 10) in 5 algorithms. The truncation function for converting ∆weight to integer number of pulses is disable, which means the number of pulses can be decimal number. Therefore, the number of the levels doesn’t limit the accuracy of weight that system desires to reach. Thus, all of predictions are higher than 93% and there is no difference between low number of the levels and high number of the levels.

Supplementary Figure S6. Prediction accuracy with different number of the levels (from 10 to 200, step is 10) in 5 algorithms under measured cycle-to-cycle variation (α = 0.03577). The truncation function for converting ∆weight to integer number of pulses is disable. When cycle-to-cycle variation is involved, although the number of update pulses can be decimal and the desired value of weight still can be reached, according to equation (2), higher number of the levels introduces more cycle-to-cycle variation even when the system has same ∆weight that need to be updated. Therefore, the prediction of accuracy is higher when the system has lower number of the levels than that with higher number of the levels.

Supplementary Figure S7. The difference of accuracy between ideal case (α=0) and that with c2c variation (α=0.03577). The black squires represent the negative values. The truncation function for converting ∆weight to integer number of pulses is disable for both cases. Note that, all of difference of prediction accuracies are positive, which means the accuracy in ideal case is higher than that with cycle-to-cycle variations. Therefore, the truncation function for an integer number of pulses, sometimes, makes the system with cycle-to-cycle variations achieves closer accurate weight that algorithm requires and then the system gets even higher prediction accuracy than without cycle-to-cycle variation.

Supplementary Figure S8. Testing platform. Kaysight B1500a semiconductor parameter analyzer is used to test memristor crossbar array. The wafer was set on the Micromanipulator probe station and the pads were contacted by gold probe tips.

Supplementary Tables:

Supplementary Table 1. The coefficient values (α) with different width of pulses.

| Width of pulse (μs) | 520 | 540 | 600 | 800 | 1000 | 1200 | 1400 | 1600 | 1800 | 2000 | Average |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| α (LTP) | 0.04354 | 0.05060 | 0.03846 | 0.03714 | 0.04077 | 0.03191 | 0.03278 | 0.03277 | 0.03280 | 0.05307 | 0.03577 |
| α (LTD) | 0.03712 | 0.06754 | 0.03279 | 0.03109 | 0.02746 | 0.02173 | 0.02064 | 0.02444 | 0.03045 | 0.02825 |  |

We can fit these LTP and LTD experimental data with exponential formulas and the residual analysis is done by Gaussian distribution fitting after normalization. After Gaussian distribution fitting, we get a distribution of α values with different pulse widths. It can be concluded that increasing the pulse width does not increase the cycle-to-cycle variation when using the same number of pulses to tune conductance. The average of the α is 0.03577.

Supplementary Notes:

Supplementary note 1

Because stochastic behavior of the cycle-to-cycle variation can be approximated as Gaussian distribution2,3, the value of cycle-to-cycle variation corresponding to one pulse can be defined as

ψ=N0,  δ                                                                                   (1)

where ψ is cycle-to-cycle variation that is generated for one pulse update process, N0,  δ is Gaussian noise, and δ is standard deviation. The value of cycle-to-cycle variation corresponding to two pulses can be calculated as

ψ1+2=N10,  δ1+ N20,  δ2                                                                      (2)

Because different cycle-to-cycle variation obey Gaussian distributions and that are independent and identically distributed corresponding to different one pulse, δ1=δ2=δ, the equation (2) can be converted as4

ψ1+2=N0,  δ1+ δ2=N0,  2δ=N0,  δ*2                                              (3)

Therefore, the total cycle-to-cycle variation that is generated for one memristor at one update process with n pulses can be calculated as

ψtotal=N0,  δ* n                                                                       (4)

Supplementary References

1	Chen, P.-Y. et al. in Proceedings of the IEEE/ACM International Conference on Computer-Aided Design.  194-199 (IEEE Press).

2	Tuma, T., Pantazi, A., Le Gallo, M., Sebastian, A. & Eleftheriou, E. Stochastic phase-change neurons. Nature nanotechnology 11, 693 (2016).

3	Jiang, H. et al. A novel true random number generator based on a stochastic diffusive memristor. Nat Commun 8, 882, doi:10.1038/s41467-017-00869-x (2017).

4	Lemons, D. S. & Langevin, P. An introduction to stochastic processes in physics.  (JHU Press, 2002).