Supporting Information

Balancing vacancy and carrier concentration in halide solid electrolytes for all-solid-state sodium batteries

Meng Wu, Xinyu Liu, Hong Liu, Dabing Li, Xiang Qi, Lei Gao, Ce-Wen Nan, Li-Zhen Fan*

M. Wu, X. Liu, D. Li, X. Qi, Prof. L. Gao, Prof. L.-Z. Fan*

Beijing Advanced Innovation Center for Materials Genome Engineering,

Beijing Key Laboratory for Advanced Energy Materials and Technologies,

University of Science and Technology Beijing, Beijing 100083, China

E-mail: fanlizhen@ustb.edu.cn

Prof. C.-W. Nan, Dr. H. Liu, State Key Laboratory of New Ceramics and Fine Processing, School of Materials Science and Engineering, Tsinghua University, Beijing, China

Supplementary Figures and Tables

Figure S1. Schematic illustration the crystal structure of Na0.5ZrCl4.5 along [001] views.

Figure S2. (a) XRD structure Rietveld refinement of Na2ZrCl6. (b-c) The crystal structures of Na2ZrCl6.

Figure S3. Raman spectra of Na2ZrCl6, Na0.5ZrCl4.5, and ZrCl4.

Figure S4. The micro-morphology and compressibility (under 300 MPa) comparations of various SEs systems. (a-b) Na3PS4 (NPS), (c-d) Na2ZrCl6, and (e-f) Na0.5ZrCl4.5.

Figure S5. Typical EIS Nyquist plots of NaxZrCl4+x SE samples at 25 ℃.

Figure S6. DC polarization measurements of NaxZrCl4+x with a voltage step of 1 V. Corresponding electronic conductivities were ~ 10-9 S cm-1.

Figure S7. The vacancies (including Na and Cl vacant sites) and charge carriers (Na-ion) content within NaxZrCl4+x structures.

Figure S8. The phase structure and ionic transport property of NaxEr0.4Zr0.6Cl3.6+x (0.2 ≤ x ≤ 2.4) SE samples. (a) XRD patterns. (b) Arrhenius plots. (c) Typical EIS Nyquist plots at 25 ℃. (d) The σ and corresponding activation energy (Ea) at 25 ℃.

Figure S9. The phase structure and ionic transport property of NaxYb0.25Zr0.75Cl3.75+x (0.2 ≤ x ≤ 2.25) SE samples. (a) XRD patterns. (b) Arrhenius plot. (c) Typical EIS Nyquist plots 25 ℃. (d) The σ and corresponding Ea at 25 ℃.

Figure S10. (a) Cold-press pellets (under 300 MPa) of Na0.5ZrCl4F0.5, and (b-d) corresponding EDS element mappings.

Figure S11. (a) Arrhenius plots of various Na0.5ZrCl4.5-yFy SE systems. (b) Typical EIS Nyquist plots of Na0.5ZrCl4.5-yFy series at 25 ℃. (c) DC polarization measurements of Na0.5ZrCl4F0.5 with a voltage step of 1 V.

Figure S12. The XRD pattern of Na0.5ZrCl4F0.5 after being exposed to relative humidity (RH) of 35 ± 5% for 10 min.

Figure S13. (a) The XRD patterns and, (b) EIS Nyquist plots comparisons of Na0.5ZrCl4.5 before and after exposed in ambient humidity (35 ± 5% RH) for 10 min.

Figure S14. The XPS results of different halide SEs before and after oxidize to 5 V. (a) Na2ZrCl6, (b) Na0.5ZrCl4.5, and (c) Na0.5ZrCl4F0.5.

Figure S15. CV curves for the asymmetric Na15Sn4|NPS/HNISEs|HNISEs-VGCF cells at a scan rate of 0.1 mV s-1.

Figure S16. The long cycling performance comparisons of Na15Sn4/Na15Sn4 symmetrical cells based on various HNISEs systems.

Figure S17. The XPS spectra of F 1s at the Na15Sn4/Na0.5ZrCl4F0.5 interface after symmetrical cell cycling.

Figure S18. The long cycling performance comparisons of Na15Sn4|NPS/HNISEs/NPS|Na15Sn4 symmetrical cells.

Figure S19. Phase structure and micro-morphology of Na3V2(PO4)3 positive materials.

Figure S20. Phase structure and electrochemical properties of NPS SEs. (a) XRD pattern. (b) Arrhenius plots. (c) DC polarization measurements. (d) CV curves for the asymmetric Na15Sn4|NPS|VGCF-NPS cells at a scan rate of 0.1 mV s-1.

Figure S21. (a) Schematic illustration of NPS-based ASSIBs. (b) The charge-discharge curves at 0.1 C. (c) The EIS Nyquist plots comparisons before and after cycles.

Figure S22. The charge-discharge voltage profile comparisons of different HNISEs-based cells at 0.1 C under RT during different cycles.

Figure S23. The dQ/dV integral curve comparisons of different HNISEs-based cells under different cycles.

Figure S24. The EIS Nyquist plot comparisons of different HNISEs-based cells before and after cycles.

Figure S25. Impedance evolution during the initial charge cycle of different HNISEs-based cells. (a-c) In-situ EIS tests, and (d-f) corresponding detailed electrochemical evolution process evaluated by the distribution of relaxation time (DRT) method.

Figure S26. GITT potential response curve with time of three cells (a-c). The experiment is conducted at 0.1 C for 10 min followed by a relaxation period of 60 min. (d) The GITT curves and ion diffusion coefficients (DNa+) of Na2ZrCl6 cell.

Table S1. Rietveld refinement results from the XRD pattern of Na0.5ZrCl4.5. The space group is P—3m1; the refined lattice parameters are a = 11.24 (2) Å and c = 6.117 (7) Å.

| Atom | x | y | z | Occupancy | Site | Uiso(Å2) |
| --- | --- | --- | --- | --- | --- | --- |
| Na1 | 0.33333 | 0 | 0 | 0.31 | 6g | 0.005 |
| Na2 | 0.3384 | 0 | 0.5 | 0.19 | 6h | 0.005 |
| Zr1 | 0 | 0 | 0 | 0.65 | 1a | 0.013 |
| Zr2 | 0.33333 | 0.66667 | 0.52875 | 0.57 | 2d | 0.013 |
| Zr3 | 0 | 0 | 0.5 | 0.71 | 1b | 0.013 |
| Zr4 | 0.33333 | 0.66667 | 0.89231 | 0.25 | 2d | 0.013 |
| Cl1 | 0.10487 | -0.10487 | 0.70568 | 0.897 | 6i | 0.01 |
| Cl2 | 0.22447 | -0.22447 | 0.26257 | 0.723 | 6i | 0.01 |
| Cl3 | 0.45021 | -0.45021 | 0.7335 | 0.63 | 6i | 0.01 |

Table S2. Rietveld refinement results from the XRD pattern of Na2ZrCl6. The space group is P—3m1; the refined lattice parameters are a = 11.483 (2) Å and c = 6.253 (5) Å.

| Atom | x | y | z | Occupancy | Site | Uiso(Å2) |
| --- | --- | --- | --- | --- | --- | --- |
| Na1 | 0.33566 | 0 | 0 | 0.564 | 6g | 0.012 |
| Na2 | 0.31961 | 0 | 0.5 | 0.436 | 6h | 0.012 |
| Zr1 | 0 | 0 | 0 | 0.561 | 1a | 0.004 |
| Zr2 | 0.33333 | 0.66667 | 0.53315 | 0.623 | 2d | 0.004 |
| Zr3 | 0 | 0 | 0.5 | 0.719 | 1b | 0.004 |
| Zr4 | 0.33333 | 0.66667 | 0.99879 | 0.236 | 2d | 0.004 |
| Cl1 | 0.0997 | -0.0997 | 0.72944 | 1 | 6i | 0.015 |
| Cl2 | 0.23458 | -0.23458 | 0.29535 | 1 | 6i | 0.015 |
| Cl3 | 0.44631 | -0.44631 | 0.77469 | 1 | 6i | 0.015 |

Table S3. Summary of the ionic conductivities and corresponding activation energy values of NaxZrCl4+x SEs obtained by impedance spectra of the cold-pressed NaxZrCl4+x pellets.

| Samples | Ionic conductivity at 25 ℃ (S cm-1) | Activation energy (eV) |
| --- | --- | --- |
| Na0.2ZrCl4.2 | 1.90 × 10-5 | 0.40 |
| Na0.4ZrCl4.4 | 4.72 × 10-5 | 0.37 |
| Na0.5ZrCl4.5 | 8.10 × 10-5 | 0.35 |
| Na0.6ZrCl4.6 | 6.02 × 10-5 | 0.36 |
| Na0.8ZrCl4.8 | 4.53 × 10-5 | 0.37 |
| Na1.2ZrCl5.2 | 3.72 × 10-5 | 0.39 |
| Na2ZrCl6 | 1.31 × 10-5 | 0.44 |

Table S4. Summary of the ionic conductivities and corresponding activation energy values of NaxEr0.4Zr0.6Cl3.6+x SEs obtained by impedance spectra of the cold-pressed NaxEr0.4Zr0.6Cl3.6+x pellets.

| Samples | Ionic conductivity at 25 ℃ (S cm-1) | Activation energy (eV) |
| --- | --- | --- |
| Na0.2Er0.4Zr0.6Cl3.8 | 1.02 × 10-5 | 0.48 |
| Na0.4Er0.4Zr0.6Cl4 | 5.25 × 10-5 | 0.39 |
| Na0.6Er0.4Zr0.6Cl4.2 | 5.72 × 10-5 | 0.38 |
| Na0.8Er0.4Zr0.6Cl4.4 | 3.43 × 10-5 | 0.42 |
| Na2.4Er0.4Zr0.6Cl6 | 1.93 × 10-5 | 0.44 |

Table S5. Summary of the ionic conductivities and corresponding activation energies values of NaxYb0.25Zr0.75Cl3.75+x SEs obtained by impedance spectra of the cold-pressed NaxYb0.25Zr0.75Cl3.75+x pellets.

| Samples | Ionic conductivity at 25 ℃ (S cm-1) | Activation energy (eV) |
| --- | --- | --- |
| Na0.2Yb0.25Zr0.75Cl3.95 | 2.23 × 10-5 | 0.45 |
| Na0.4Yb0.25Zr0.75Cl4.15 | 2 × 10-4 | 0.33 |
| Na0.6Yb0.25Zr0.75Cl4.35 | 1.22 × 10-4 | 0.37 |
| Na0.8Yb0.25Zr0.75Cl4.55 | 7.67 × 10-5 | 0.39 |
| Na2.25Yb0.25Zr0.75Cl6 | 2.94 × 10-5 | 0.43 |

Table S6. Summary of the ionic conductivities and corresponding activation energy values of Na0.5ZrCl4.5-yFy SEs obtained by impedance spectra of the cold-pressed Na0.5ZrCl4.5-yFy pellets.

| Samples | Ionic conductivity at 25 ℃ (S cm-1) | Activation energy (eV) |
| --- | --- | --- |
| Na0.5ZrCl4.25F0.25 | 8.67 × 10-5 | 0.36 |
| Na0.5ZrCl4F0.5 | 1.12 × 10-4 | 0.37 |
| Na0.5ZrCl3.75F0.75 | 3.35 × 10-5 | 0.44 |
| Na0.5ZrCl3.5F | 1.76× 10-5 | 0.49 |

Table S7. Summary of the electronic conductivities of different SEs systems obtained by DC polarization measurements.

| Samples | Electronic conductivity at 25 ℃ (S cm-1) |
| --- | --- |
| Na0.2ZrCl4.2 | 1.54 × 10-9 |
| Na0.4ZrCl4.4 | 1.75 × 10-9 |
| Na0.5ZrCl4.5 | 3.64 × 10-9 |
| Na0.6ZrCl4.6 | 5.19 × 10-9 |
| Na0.8ZrCl4.8 | 1.31 × 10-9 |
| Na1.2ZrCl5.2 | 3.43 × 10-9 |
| Na2ZrCl6 | 1.92 × 10-9 |
| Na0.5ZrCl4F0.5 | 9.83 × 10-10 |
| Na3PS4 | 1.20 × 10-8 |

Table S8. Summary of the relative densities of different SE systems estimated by SEM images.

| Samples | Relative densities (%) |
| --- | --- |
| Na0.5ZrCl4.5 | 95.8 |
| Na2ZrCl6 | 91.3 |
| Na0.5ZrCl4F0.5 | 98.2 |
| Na3PS4 | 97.5 |

Table S9. Phase equilibria at the interfaces between NVP, Na, Na15Sn4, and the SEs with the minimum decomposition energies.

| SEs | Electrodes | Mole fraction of SEs (x) | Phase equilibria at Xm | Minimum mutual reaction energy (meV/atom) |
| --- | --- | --- | --- | --- |
| Na0.5ZrCl4.5 | NVP | 0.38 | NaZr2(PO4)3, VCl3, NaCl | -87.96 |
|  | Na | 0.6 | Zr, NaCl | -553.84 |
|  | Na15Sn4 | 0.54 | ZrSn2, Zr5Sn4, NaCl, | -530.09 |
| Na0.5ZrCl4F0.5 | NVP | 0.4 | NaZr2(PO4)3, Na2ZrF6, VCl3, NaCl | -84.53 |
|  | Na | 0.6 | Zr, NaCl, NaF | -528.30 |
|  | Na15Sn4 | 0.54 | ZrSn2, Zr5Sn4, NaCl, NaF | -507.02 |
| Na2ZrF6 | NVP | 0.23 | NaF, NaZr2(PO4)3, Na3V2P2O8F3 | -15.50 |
|  | Na | / | Na, NaF | 0 |
| NaF | Na15Sn4 | / | Na15Sn4, NaF | 0 |
|  | NVP | / | NVP, NaF | 0 |