A cotton swab platform for fluorescent detection of aluminum ion in food samples based on aggregation-induced emission of carbon dots

Tong Shao, Dou Yang, Xiaoshuang Wang, Ruirui Wang, Qiaoli Yue*

School of Chemistry and Chemical Engineering, Liaocheng University, Liaocheng 252059, China

Corresponding author:

Dr. Qiaoli Yue

Email, yueqiaoli@lcu.edu.cn

Fig. S1 The stability of NCDs at room temperature (A) and illumination with a LED lamp (B)

Fig. S2 Photo of cotton swab sensor under natural light and UV lamp

Fig. S3 DLS measurements for the size distribution of NCDs and NCDs+Al3+

Fig. S4 Fluorescence decay of NCDs and NCDs+Al3+

|  | Table S1 Results for Al3+ detection in real samples |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Samples | Present method |  |  |  | AAS (μM) |
|  | Added (μM) | Found (μM) | Recovery (%) | RSD (%) |  |
| Spicy strip | 0 | / | / | / | / |
|  | 20 | 19.35 | 96.75 | 0.2112 | 20.35 |
|  | 40 | 40.21 | 100.53 | 0.3149 | 39.87 |
| Fried cake | 0 | / | / | / | / |
|  | 20 | 20.11 | 100.55 | 0.3181 | 19.76 |
|  | 40 | 39.42 | 98.55 | 0.2691 | 39.95 |
| Bread | 0 | / | / | / | / |
|  | 20 | 18.96 | 94.80 | 0.2635 | 19.86 |
|  | 40 | 39.69 | 99.23 | 0.5812 | 39.25 |

|  | Table S2 Results for the fluorescence detection of Al3+ with different CDs |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Materials |  | Linear range (μM) | LOD (μM) | portable | Reference |
| CDs |  | 150-1200 | 7.998 | Yes | [1] |
| Y-CDs |  | 0-10 | 0.095 | No | [2] |
| G- NSCDs |  | 0.1-2 | 0.0458 | No | [3] |
| # B,N-CQDs |  | 0-20 | 0.187 | No | [4] |
| # NCDs |  | 2.5-300 | 0.16 | Yes | This work |

Reference

- Yan, L. et al. . (2023) Artificial intelligence-integrated smartphone-based handheld detection of fluoride ion by Al3+-triggered aggregation-induced red-emssion enhanced carbon dots. Journal of Colloid and Interface Science, 651, 59-67.

- Gao, X. et al. . (2023) Hydrothermal synthesis of dual emission carbon dots with yellow fluorescence for ratio detection of Al3+. Optical Materials, 143, 114132.

- Tang, X. et al. . (2023) Concentration-regulated multi-color fluorescent carbon dots for the detection of rifampicin, morin and Al3+. Materials Today Advances, 18, 100383.

- Wang, C. et al. . (2022) Biocompatible double emission boron nitrogen co-doped carbon quantum dots for selective and sensitive detection of Al3+ and Fe2+. Materials Research Bulletin, 155, 111970.