Supporting Information

Synthesis of MnO2@TiO2 composite electrodes via hydrolysis and calcination for high stability zinc ions batteries

Jun Zhu , Hongwei Shi, Chengcheng Liu, Wenzhu Ouyang, Yuling Liu, Xiaoling Li

Key Laboratory of Spin Electron and Nanomaterials of Anhui Higher Education Institutes, Suzhou University, Educational Park No. 1769 Xuefu Avenue, Suzhou 234000, P. R. China

Figure S1. SEM images of (a, b) MnO2@TiO2-1 and (c, d) MnO2@TiO2-3.

Table S1. Comparison of electrochemical performance of MnO2@TiO2-2 anode with different manganese oxide anodes in recent years

| Cathode | electric current (A g-1) | Capacity (mAh g-1) | Retention/Cycles | Ref. |
| --- | --- | --- | --- | --- |
| MnO2@TiO2-2 | 3 | 93.35 | 97.47 % /1500 | This work |
| MnO2@V2O5 | 2 | 77.45 | 73 %/3000 | 1 |
| ε-MnO2@C | 1 | 172 | 91 %/1700 | 2 |
| α-MnO2@LMO | 1 | 115 | 90 %/1500 | 3 |
| KMO | 1 | 99.6 | 50.74 % /1400 | 4 |
| Ag0.4Mn8O16 | 1 | 110 | 50 %/800 | 5 |
| α-MnO2/super-P | 1 | 84.6 | 47 %/1000 | 6 |
| α-MnO2@DCDA | 3 | 102.6 | 62 %/1500 | 7 |

Figure S2. (a) Coin cell battery successfully lights up the electronic watch, (b) CV curves of MnO2 at different scan rates, (c) Linear logarithmic plot between scan rate and peak current response value for MnO2, (c) Contributions of capacitance control and diffusion control at different scan rates for MnO2.

REFERENCES

(1)	Shang, H.;  Zhang, Z.;  Liu, C.;  Zhang, X.;  Li, S.;  Wen, Z.;  Ji, S.; Sun, J., MnO2@ V2O5 microspheres as cathode materials for high performance aqueous rechargeable Zn-ion battery. Journal of Electroanalytical Chemistry 2021, 890, 115253.

(2)	Zhao, W.;  Kong, Q.;  Wu, X.;  An, X.;  Zhang, J.;  Liu, X.; Yao, W., ε-MnO2@ C cathode with high stability for aqueous zinc-ion batteries. Applied Surface Science 2022, 605, 154685.

(3)	Li, H.;  Zhou, X.;  Liu, L.;  Huang, D.;  Zhang, W.; Zhang, S., Hierarchical α-MnO2@ LaxMn1-xO2-δ core–shell nanostructure cathode for high-performance aqueous Zn-ion batteries. Ionics 2024, 1-11.

(4)	Yang, Q.;  Chen, Y.;  Yang, Y.;  Xu, T.;  Lin, Y.;  Zhang, X.;  Wang, J.;  Liu, Y.-N.; Li, Y., Batch Synthesis of K-Doped α-MnO2 Nanorods as Cathode Materials for Aqueous Zinc-Ion Battery. Industrial & Engineering Chemistry Research 2023, 62 (41), 16757-16765.

(5)	Fenta, F. W.;  Olbasa, B. W.;  Tsai, M.-C.;  Temesgen, N. T.;  Huang, W.-H.;  Tekaligne, T. M.;  Nikodimos, Y.;  Wu, S.-h.;  Su, W.-N.; Dai, H., Structural engineering of α-MnO2 cathode by Ag+ incorporation for high capacity aqueous zinc-ion batteries. Journal of Power Sources 2022, 548, 232010.

(6)	Yang, C.;  Wu, Q.;  Cao, Y.;  Gao, Y.;  Li, A.;  Liu, X.;  Zhang, X.;  Tian, Z.; Liu, R., α-MnO2/super-P with conductive carbon network for rechargeable aqueous Zinc ion batteries. Materials Letters 2021, 302, 130419.

(7)	Lu, C.-h.; Du, D., Construction of dicyandiamide-coated manganese dioxide composite and its mechanism for improving zinc storage performance. Journal of Central South University 2024, 31 (5), 1443-1460.

Corresponding author: szxyhsxyzj@163.com