Ultra-tough and high-resilient mechanochromic fibres for real-world stress detection

Yu Jin Jeong1, Youngeun Lee1, Taekyung Won2, Jiwon Lee1, Youngho Eom2,*, Dae Seok Kim1,*

1Department of Polymer Engineering Pukyong National University Busan 48513, Republic of Korea

E-mail:daeseok@pknu.ac.kr

2 Department of Organic and Nano Engineering, Hanyang University, Seoul, Republic of Korea

E-mail:eomyh@hanyang.ac.kr

Supplementary Note 1-3

Supplementary Figure 1-10

Table S1

Supplementary Movie captions (S1 – S3)

Supplementary Note 1.

Preparation of CLCE precursors

A thiol-terminated liquid crystal (LC) oligomer was synthesised via the thiol-acrylate Michael addition1 of 2-methyl-1,4-phenylene bis(4-((6-(acryloyloxy)hexyl)oxy)benzoate) (RM82) and 1,5-pentanedithiol (1,5-PDT).42 The LC oligomer was vigorously mixed with a mixture of LC reactive monomers (RM82 and RM257), a chiral dopant ((3R,3aR,6S,6aR)-hexahydrofuro[3,2-b] furan-3,6-diyl bis(4-((4-(((4-(acryloyloxy)butoxy) carbonyl)oxy) benzoyl)oxy)benzoate, LC756), and a photoinitiator (2,2-dimethoxy-2-phenylacetophenone, DMPA) (Fig. S1) at 100 °C for 30 min. Then, the resultant CLCE precursor was coated on TPE core fibres. TPE fibres of 0.8 mm diameter were prepared via melt-spinning with varying contents of CB to control the elastic modulus of the core.

Supplementary Note 2.

Rheological behavior of CLCE precursors

According to the temperature sweeping test (Fig. S4a, Supplementary information), dynamic viscosity (η') and storage modulus (G'), rheological indicators of flow resistance and elasticity, experience an abrupt change in the vicinity of TNI. Particularly at the nematic state, the G' prevails over the η' over the with almost temperature-independent trend. Such high elasticity is in line with the high elasticity of CLCE precursor, which is eventually responsible for the poor wettability. After the TNI, however, the sudden drop of the G' reveals the dissociation of the liquid crystalline ordering. According to the yield stress (τy) calculated by Casson plot (Fig S4b, c, and d, Supplementary information), the sharp reduction of the τy from 0.8 (50 C) to 0 Pa (60 C) quantitatively confirms the collapse of the 3D nematic network. As a result, the τy can be designated as a direct indicator of determining the morphology quality of coating surfaces. Nonetheless, the colour appearance of the coating layer is determined by the formation of shear-induced ordering. In the stress sweeping test (Fig. S4e, Supplementary information), the CLCE precursor exhibits sharp drop and subsequent jump at 80 C, namely the slip-and-stick phenomenon. In this situation, the shearing brings about the rapid switching of ordering-disordering of the highly flowable molecules. As a result, the shear-induced orientation is hardly developed at the isotropic phase. On the other hand, the CLCE precursor follow the gradual reduction of the G' at 40 and 60 ℃, resulting from the continuous alignment of helixes along the shear direction. Particularly at 60 ℃, the CLCE precursor exhibits the stable stress thinning behavior as well as the high fluidity with negligible τy, typical trend of the biphase. Consequently, the use of the biphasic precursor in the vicinity of TNI, is the key for simultaneously obtaining the desired coating quality and the vivid reflective colours.

Supplementary Note 3.

Poisson’s ratio of CLCE-SC fibres

As the CLCE-SC fibres were stretched along the x-axis, deformation occurred from the transverse axis to the x-axis because of Poisson’s effect, resulting in a blue shift owing to the decrease in pitch length. The Poisson’s ratio (ν) of the CLCE-SC fibres is expressed as follows:

ν= -εtεx

where εx is the strain along the x-axis, and εt is the strain in the direction transverse to the x-axis. The εx and εt of the CLCE-SC fibres upon elongation were positive and negative, respectively, resulting in the changes in the helical pitch (p) and reflective wavelength (λ) of the CLCE sheath. When the thickness of the CLCE sheath is significantly higher than p, εt can be expressed as ∆λ/λo, where λo is an initial CLCE reflection wavelength (when θ = 0).2 The Poisson’s ratios for the LM-, MM-, and HM-CLCE-SC fibres were 0.13, 0.12, and 0.13, respectively (Fig. S8). This indicates that the CLCE sheath adhered to the surface of the TPE fibres in the same manner, regardless of its CB content.

Supplementary Figure 1. Chemical structures of the CLCE precursor.

Supplementary Figure 2. Differential Scanning Calorimetry (DSC) measurement of CLCE precursor.

Supplementary Figure 3. CLCE sheath coating quality at different temperatures. (a, b, and c) Optical microscope (OM) images showing the thickness of the CLCE sheath at the 26 different sites under nematic (30 °C), TNI (54 °C), and isotropic (80 °C) conditions, respectively. The mentioned thickness refers to the average. (d) The deviation of thickness with coating temperatures.

Supplementary Figure 4. Rheological analysis of CLCE precursors at different temperatures. (a) Temperature sweeping test of dynamic viscosity (η') and storage modulus (G'). (b) Time sweeping test of storage modulus (G'). (c) Casson plot measured at temperatures ranging from 30 to 80 °C. (d) Yield stress (τy) calculated by Casson plot. (e) Stress sweeping test of storage modulus.

Supplementary Figure 5. Stress-strain curve of CLCE-SC and neat CLCE fibres.

Supplementary Figure 6. Strain - relaxation test. (a) Strain-relaxation curve of the neat CLCE fibre. (b) Fitting curves of the CLCE-SC and neat CLCE fibres according to a Kelvin-Voigt creep test equation, εt=ε0exp-tτ.

Supplementary Figure 7. Spectrometer of thermal stability test of CLCE-SC fibre. The reflective wavelength of the CLCE sheath was observed while increasing the temperature from 20 to 140 °C.

Supplementary Figure 8. Strain-stress curve of the LM-, MM-, and HM-TPE fibres.

Supplementary Figure 9. Poisson’s ratio of the LM-, MM-, and HM-CLCE-SC fibres. (a, b, and c) The CLCE-SC fibre’s reflective wavelength was measured in 10 % increments from 10 to 170 % strain. The Poisson’s ratio (ν) was determined from the slope of the linear fit curves.

Supplementary Figure 10. Spectrometer of LM-, MM-, and HM-CLCE-SC fibres. (a, c, and e) The reflective wavelength across strain levels ranging from 0 to 170 % strain of LM-, MM-, and HM-CLCE-SC fibres, respectively. (b, d, and f) The reflective wavelength across load levels ranging from 0 to 6 N load of LM-, MM-, and HM-CLCE-SC fibres, respectively.

Table S1. The reflective wavelength at 0 % (λ0) and 100 % (λε=100%)  strain as a function of dopant concentration.

| Dopant (wt %) | λ0 (nm) | λε=100% (nm) |
| --- | --- | --- |
| 3.5 | 673 | 582 |
| 3.75 | 599 | 521 |
| 4 | 560 | 500 |
| 4.25 | 540 | 494 |
| 4.5 | 532 | UV region |

Supplementary Movie captions

Movie S1: Ultra-fast loading-unloading cycles of CLCE-SC fibre showing up to 160% strain with an increase in frequency from 3.03 Hz (= 23.33 cm s-1) to 8.33 Hz (= 128.28 cm s-1).

Movie S2: Ultra-fast loading-unloading cycles of neat CLCE fibre showing up to 60 % stain with an increase in the frequency from 3.03 Hz (= 18.18 cm s-1) to 8.33 Hz (= 49.98 cm s-1).

Movie S3: Mechanochromic response of the dynamic sensory net depending on the height of the steel ball drop.

Supplementary references

1. Xia, Y., Zhang, X. & Yang, S. Instant Locking of Molecular Ordering in Liquid Crystal Elastomers by Oxygen-Mediated Thiol–Acrylate Click Reactions. Angewandte Chemie 130, 5767–5770 (2018).

2. Serra, F., Matranga, M. A., Ji, Y. & Terentjev, E. M. Single-mode laser tuning from cholesteric elastomers using a “notch” band-gap configuration. Opt. Express 18, 575 (2010).