Supporting Information

Bismuth Atom Tailoring of Indium Oxide Surface Frustrated Lewis Pairs Boosts Heterogeneous CO2 Photocatalytic Hydrogenation

Tingjiang Yan,a,b* Na Li,c* Linlin Wang,a Weiguang Ran,a Paul N. Duchesne,b Lili Wan,b Nhat Truong Nguyen,b Lu Wang,b Meikun Xia,b Geoffrey A. Ozinb*

a The Key Laboratory of Life-Organic Analysis, College of Chemistry and Chemical Engineering, Qufu Normal University, Qufu, Shandong 273165, P. R. China.

b Materials Chemistry and Nanochemistry Research Group, Solar Fuels Cluster, Department of Chemistry, University of Toronto, 80 St. George Street, Toronto, Ontario M5S 3H6, Canada.

c Qufu Normal University Library, Qufu Normal University, Qufu, Shandong 273165, P. R. China.

Corresponding Authors

*Email: tingjiangn@163.com, chessmantj@163.com, gozin@chem.utoronto.ca

Table S1. The molar contents of Bi in the series of BixIn2-xO3 nanocrystals determined by ICP-MS.

| Catalyst | Molar content of Bi (%) |
| --- | --- |
| 0.5% BixIn2-xO3 | 0.43 |
| 1.0% BixIn2-xO3 | 0.89 |
| 3.0% BixIn2-xO3 | 2.35 |
| 5.0% BixIn2-xO3 | 4.84 |

Table S2. Fitting results of Bi L3-edge and In K-edge FT-EXAFS data.

| Sample | Path | CN | R (Å2) | 2 (Å2) | E0 (eV) |
| --- | --- | --- | --- | --- | --- |
| Bi2O3 | Bi-O Bi-O Bi-Bi | 2.8(4) 2.7(4) 3.8(9) | 2.169(9) 2.52(3) 3.590(8) | 0.005(1) 0.022(9) 0.006(1) | 1.5(7) |
| 1.0% BixIn2-xO3 | Bi-O Bi-In | 5(1) 4(1) | 2.21(1) 3.42(1) | 0.016(4) 0.007(1) | -7(1) |
| 5.0% BixIn2-xO3 | Bi-O Bi-In | 4.4(6) 2.9(7) | 2.18(1) 3.42(1) | 0.014(3) 0.009(1) | -8.6(8) |
| In2O3 | In-O In-In In-In | 6.1(3) 4.9(6) 3.6(9) | 2.170(3) 3.359(3) 3.843(4) | 0.0061(9) 0.0031(6) 0.003(1) | -0.4(4) |

CN = coordination numbers of Bi and In atoms; R = bond length; 2 = the Debye−Waller factor coefficient.

Table S3. The compared CO production rate of different catalysts for photocatalytic CO2 hydrogenation.

| Catalyst | Feeds (CO2+H2) | Light Source | T (C) | CO rate (molg-1h-1) | Ref. |
| --- | --- | --- | --- | --- | --- |
| In2O3-x(OH)y superstructures | 1:1 | 1000 W Hortilux Blue metal halide bulb | - | 1.2 | 1 |
| BizIn2−zO3−x(OH)y | 1:1 | 1000 W Hortilux Blue metal halide bulb | 150 | 1.32 | 2 |
| Pd/Nb2O5 | 1:1 | 300 W Xe lamp | - | 1800 | 3 |
| Pd@HyWO3−x | 1:1 | 300 W Xe lamp | 250 | 3000 | 4 |
| Pt/NaTaO3 | 1:1 | 300 W UV-enhanced Xe lamp | - | 139.1 | 5 |
| Pd@SiNS | 1:1 | 300 W Xe lamp | 170 | 10 | 6 |
| In2O3-x(OH)y/Nb2O5 | 1:1 | 300 W Xe lamp | - | 1400 | 7 |
| BixIn2-xO3 | 1:1 | 300 W Xe lamp | - | 8000 | This work |

Table S4. Specific surface area of pristine In2O3 and BixIn2-xO3 nanocrystals.

| Catalyst | Surface area (m2 g-1) |
| --- | --- |
| Pristine In2O3 | 33.5 |
| 0.5% BixIn2-xO3 | 33.8 |
| 1.0% BixIn2-xO3 | 34.2 |
| 3.0% BixIn2-xO3 | 34.0 |
| 5.0% BixIn2-xO3 | 32.5 |

Fig. S1 (a) TEM, (b) HRTEM, (c) size distribution, and (d) SAED of pristine In2O3. The highlighted yellow ring in (a) shows one flower-like agglomerate. The red arrows in (b) represent the single nanocrystals, and the inset in (b) shows the lattice fringe with a spacing of 2.92 Å.

Fig. S2 (a) TEM, (b) HRTEM, (c) size distribution, and (d) SAED of 1.0% BixIn2-xO3 sample. (e) TEM and HRTEM of 3.0% BixIn2-xO3 sample. (f) TEM and HRTEM of 5.0% BixIn2-xO3 sample.

Fig. S3 Elemental mapping profiles of 1.0% BixIn2-xO3.

Fig. S4 (a) In 3d and (b) Bi 4f XPS spectra of pure In2O3 and BixIn2-xO3 nanocrystals.

Fig. S5 EPR spectra of 1.0% BixIn2-xO3 nanocrystals recorded at room temperature and 77 K.

Fig. S6 Fitted Bi L3-edge and In K-edge FT-EXAFS spectra from (a) Bi2O3 and (b) In2O3 reference materials, as well as (c) 1.0% and (d) 5.0% BixIn2-xO3 samples.

Fig. S7 The actual reaction temperature tested by IR camera on (a) pristine In2O3 and (b) 1.0% BixIn2-xO3 nanocrystals.

Fig. S8 CO production rate as a function of absorption cut-off filter wavelength for pure In2O3 sample.

Fig. S9 (a) CH3OH production and (b) CO production as function of reaction time on pristine In2O3 and BixIn2-xO3 nanocrystals in the flow reactor at 230 C, with and without light irradiation.

Fig. S10 (a) Plotted reaction rates demonstrating the long-term (50 h) catalytic stability of 1.0% BixIn2-xO3 nanocrystals during photocatalytic CO2 hydrogenation. (b) XRD patterns, (c) TEM image, and (d) Bi 4f XPS spectra of fresh and spent (i.e., after 50 h stability testing) 1.0% BixIn2-xO3 nanocrystals.

Fig. S11 (a) CH3OH production rates and (b) CO production rates of the top-performing catalyst 1.0% BixIn2-xO3 as a function of reaction temperatures.

Fig. S12 The color of pure In2O3 and substituted BixIn2-xO3 nanocrystals.

Fig. S13 Inferred band gaps of pristine In2O3 and various BixIn2-xO3 nanocrystals.

Fig. S14 Calculated DOS plots for (a) pristine In2O3 and (b) BixIn2-xO3 nanocrystals.

Fig. S15 High-resolution O 1s core-level XPS spectra of 1.0% BixIn2-xO3 nanocrystals. The O 1s core level XPS spectra could be fitted into three peaks at 529.3 eV, 530.9 eV, and 532.8 eV, which are assigned to oxides (OI), oxygen vacancies (OII), and hydroxyl groups (OIII), respectively.

Fig. S16 High-resolution O 1s core-level XPS spectra of pure In2O3 and BixIn2-xO3 nanocrystals.

Fig. S17 Time-resolved PL spectra of pristine In2O3 and 1.0% BixIn2-xO3 nanocrystals.

Fig. S18 Schematic of surface species contributing to the adsorption of CO2 on BixIn2-xO3 nanocrystals, as exemplified by monodentate carbonate-like species (m-CO32-), bidentate carbonate-like species (b-CO32-), bent adsorbed species (CO2-), and bicarbonate-like species (HCO3-).

Fig. S19 In-situ DRIFTS spectra for CO2 hydrogenation under (a) dark and (b) light conditions on 1.0% BixIn2-xO3.

Fig. S20 In-situ DRIFTS spectra for CO2 hydrogenation under (a) dark and (b) light conditions on pristine In2O3.

Note 1.

Calculation of turnover frequency (TOF)

TOF = number of produced molecues / (number of active sites * total reaction time)

NA = 6.022 x 1017 mol-1

Number of produced molecules per hour = CO rate (mol h-1m-2) x NA / total reaction time

Total reaction time = 1 h

Number of surface O atoms at exposed facet = 9.23 x 1018 m-2

- Pristine In2O3 rate: 35.6 mol h-1g-1      1.06 mol h-1m-2 (accoring to the surface area: 33.5 m2g-1)

The number of produced molecules per hour for pristine In2O3 is 6.38 x 1017 m-2h-1

- 1.0% BixIn2-xO3 rate: 7959 mol h-1g-1      232.72 mol h-1m-2 (accoring to the surface area: 34.2 m2g-1)

The number of produced molecules per hour for 1.0% BixIn2-xO3 is 1.4 x 1020 m-2h-1

Model 1: Assume all [O] will be used for reaction

Number of active sites = number of [O] = 9.23 x 1018 m-2 x [O] value obtained from XPS (41.34%) = 3.82 x 1018 m-2

TOFIn2O3 = 6.38 x 1017 m-2h-1 / 3.82 x 1018 m-2 = 0.167 h-1

Similarly, TOF1.0% BixIn2-xO3 = 36.8 h-1.

Model 2: Assume only extrinsic [O] will be used for reaction

Number of active sites = number of extrinsic [O] = 9.23 x 1018 m-2 x ([O] value obtained from XPS (41.34%) – intrinsic [O] of In2O3 (25%) ) = 1.51 x 1018 m-2

TOFIn2O3 = 6.38 x 1017 m-2h-1 / 1.51 x 1018 m-2 = 0.42 h-1

As a result, TOF1.0% BixIn2-xO3 = 93.6 h-1.

References

- L. He, T. E. Wood, B. Wu, Y. C. Dong, L. B. Hoch, L. M. Reyes, D. Wang, C. Kubel, C. X. Qian, J. Jia, K. Liao, P. G. O'Brien, A. Sandhel, J. Y. Y. Loh, P. Szymanski, N. P. Kherani, T. C. Sum, C. A. Mims, G. A. Ozin, ACS Nano 2016, 10, 5578.

- Y. C. Dong, K. K.Ghuman, R. Popescu, P. N. Duchesne, W. J. Zhou, J. Y. Y. Loh, A. A. Jelle, J. Jia, D. Wang, X. K. Mu, G. A. Ozin, Adv. Sci. 2018, 5. 1700732.

- J. Jia, P. G. O’Brien, L. He, Q. Qiao, T. Fei, L. M. Reyes, T. E. Burrow, Y. C. Dong, K. Liao,  M. Varela, S. J. Pennycook, M. Hmadeh, A. S. Helmy, N. P. Kherani, D. D. Perovic, G. A. Ozin, Adv. Sci. 2016, 3, 1600189.

- Y. F. Li, N. Soheilnia, M. Geriner, U. Ulmer, T. Wood, A. A. Jelle, Y. C. Dong, A. P. Y. Wong, J. Jia,  G. A. Ozin, ACS Appl. Mater. Interfaces 2019, 11, 5610.

- M. Li, P. Li, K. Chang, T. Wang, L. Q. Liu, Q. Kang, S. X. Ouyang, J. H. Ye, Chem. Commun. 2015, 51, 7645.

- C. X. Qian, W. Sun, D. L. H. Hung, C. Y. Qiu, M. Makaremi, S. G. H. Kumar, L. L. Wan,  M. Ghoussoub, T. E. Wood, M. K. Xia, A. A. Tountas, Y. F. Li, L. Wang, Y. C. Dong, I. Gourevich,  C. V. Singh, G. A. Ozin, Nat. Catal. 2019, 2, 46-54.

- H. Wang, J. Jia, K. Butler, R. Song, G. Casillas, L. He, N. P. Kherani,  D. D. Perovic, L. Q. Jing, A.  Walsh, R. Dittmeyer, G. A. Ozin, Adv. Sci. 2019, 6, 1902170.