Supplementary Information

Experimental Study of Carbon Dioxide Absorption by Fe2O3@glutamine/NMP Nanofluid

Abbas Elhambakhsh a, Samira Heidari a, Peyman Keshavarz a,1

a School of Chemical and Petroleum Engineering, Shiraz University, Shiraz, Iran

1- Corresponding author. Tel.: þ98 7116133713; Fax: +98 7116473180.

E-mail address: pkeshavarz@shirazu.ac.ir (P. Keshavarz).

The results of CO2 absorption experiment for NMP, Fe2O3-NMP nanofluid, and Fe2O3@glutamine-NMP nanofluid are listed  in Tables S1 to S9.

Table S1. CO2 absorption in NMP solution at Time t, Pressure P and Temperature T= 308 K.

| t/min | α/mol.kg-1 | t/min | α/mol.kg-1 | t/min | α/mol.kg-1 |
| --- | --- | --- | --- | --- | --- |
| NMP solution/P= 20bar |  | NMP solution/P= 30bar |  | NMP solution/P= 40bar |  |
| 0 | 0 | 0 | 0 | 0 | 0 |
| 5 | 0.3294 | 5 | 0.5162 | 5 | 0.6274 |
| 10 | 0.3723 | 10 | 0.5658 | 10 | 0.6775 |
| 15 | 0.3937 | 15 | 0.6154 | 15 | 0.7276 |
| 20 | 0.4151 | 20 | 0.6401 | 20 | 0.7676 |
| 40 | 0.4792 | 40 | 0.7142 | 40 | 0.8874 |
| 60 | 0.5218 | 60 | 0.7634 | 60 | 0.9767 |
| 80 | 0.5644 | 80 | 0.8126 | 80 | 1.0361 |
| 100 | 0.6019 | 100 | 0.8617 | 100 | 1.0954 |
| 120 | 0.6281 | 120 | 0.8862 | 120 | 1.125 |
| 140 | 0.6493 | 140 | 0.9107 | 140 | 1.1545 |
| 160 | 0.6607 | 160 | 0.9351 | 160 | 1.184 |
| 180 | 0.6705 | 180 | 0.9596 | 180 | 1.2034 |
| 200 | 0.6705 | 200 | 0.9596 | 200 | 1.2134 |
| 220 | 0.6705 | 220 | 0.9596 | 220 | 1.2134 |
| 240 | 0.6705 | 240 | 0.9596 | 240 | 1.2134 |
| 260 | 0.6705 | 260 | 0.9596 | 260 | 1.2134 |
| 280 | 0.6705 | 280 | 0.9596 | 280 | 1.2134 |
| 300 | 0.6705 | 300 | 0.9596 | 300 | 1.2134 |

Table S2. CO2 absorption in Fe2O3-NMP nanosolution in NPs concentration of 0.01wt.% and  at Time t, Pressure P and Temperature T= 308 K.

| t/min | α/mol.kg-1 | t/min | α/mol.kg-1 | t/min | α/mol.kg-1 |
| --- | --- | --- | --- | --- | --- |
| Fe2O3-NMP nanosolution/P= 20bar |  | Fe2O3-NMP nanosolution/P= 30bar |  | Fe2O3-NMP nanosolution/P= 40bar |  |
| 0 | 0 | 0 | 0 | 0 | 0 |
| 5 | 0.3845 | 5 | 0.6315 | 5 | 0.662 |
| 10 | 0.4315 | 10 | 0.731 | 10 | 0.7174 |
| 15 | 0.4765 | 15 | 0.7561 | 15 | 0.7776 |
| 20 | 0.5034 | 20 | 0.7816 | 20 | 0.8286 |
| 40 | 0.5773 | 40 | 0.8376 | 40 | 0.9559 |
| 60 | 0.62 | 60 | 0.8753 | 60 | 1.0506 |
| 80 | 0.645 | 80 | 0.9003 | 80 | 1.1356 |
| 100 | 0.6667 | 100 | 0.9254 | 100 | 1.1954 |
| 120 | 0.6834 | 120 | 0.949 | 120 | 1.2324 |
| 140 | 0.6943 | 140 | 0.9705 | 140 | 1.2554 |
| 160 | 0.702 | 160 | 0.9859 | 160 | 1.2685 |
| 180 | 0.702 | 180 | 0.9991 | 180 | 1.2807 |
| 200 | 0.702 | 200 | 0.9991 | 200 | 1.2807 |
| 220 | 0.702 | 220 | 0.9991 | 220 | 1.2807 |
| 240 | 0.702 | 240 | 0.9991 | 240 | 1.2807 |
| 260 | 0.702 | 260 | 0.9991 | 260 | 1.2807 |
| 280 | 0.702 | 280 | 0.9991 | 280 | 1.2807 |
| 300 | 0.702 | 300 | 0.9991 | 300 | 1.2807 |

Table S3. CO2 absorption in Fe2O3-NMP nanosolution in NPs concentration of 0.025wt.% and  at Time t, Pressure P and Temperature T= 308 K.

| t/min | α/mol.kg-1 | t/min | α/mol.kg-1 | t/min | α/mol.kg-1 |
| --- | --- | --- | --- | --- | --- |
| Fe2O3-NMP nanosolution/P= 20bar |  | Fe2O3-NMP nanosolution/P= 30bar |  | Fe2O3-NMP nanosolution/P= 40bar |  |
| 0 | 0 | 0 | 0 | 0 | 0 |
| 5 | 0.4812 | 5 | 0.718 | 5 | 0.7324 |
| 10 | 0.5356 | 10 | 0.8015 | 10 | 0.8161 |
| 15 | 0.5695 | 15 | 0.8257 | 15 | 0.865 |
| 20 | 0.5886 | 20 | 0.8516 | 20 | 0.9156 |
| 40 | 0.6384 | 40 | 0.9076 | 40 | 1.0345 |
| 60 | 0.6803 | 60 | 0.9436 | 60 | 1.123 |
| 80 | 0.7034 | 80 | 0.9703 | 80 | 1.2035 |
| 100 | 0.7149 | 100 | 0.9945 | 100 | 1.2601 |
| 120 | 0.7278 | 120 | 1.0195 | 120 | 1.2906 |
| 140 | 0.739 | 140 | 1.0405 | 140 | 1.3134 |
| 160 | 0.7445 | 160 | 1.0549 | 160 | 1.3244 |
| 180 | 0.7445 | 180 | 1.0635 | 180 | 1.3244 |
| 200 | 0.7445 | 200 | 1.0751 | 200 | 1.3244 |
| 220 | 0.7445 | 220 | 1.0751 | 220 | 1.3244 |
| 240 | 0.7445 | 240 | 1.0751 | 240 | 1.3244 |
| 260 | 0.7445 | 260 | 1.0751 | 260 | 1.3244 |
| 280 | 0.7445 | 280 | 1.0751 | 280 | 1.3244 |
| 300 | 0.7445 | 300 | 1.0751 | 300 | 1.3244 |

Table S4. CO2 absorption in Fe2O3-NMP nanosolution in NPs concentration of 0.05wt.% and  at Time t, Pressure P and Temperature T= 308 K.

| t/min | α/mol.kg-1 | t/min | α/mol.kg-1 | t/min | α/mol.kg-1 |  |
| --- | --- | --- | --- | --- | --- | --- |
| Fe2O3-NMP nanosolution/P= 20bar |  | Fe2O3-NMP nanosolution/P= 30bar |  | Fe2O3-NMP nanosolution/P= 40bar |  |
| 0 | 0 | 0 | 0 | 0 | 0 |
| 5 | 0.4153 | 5 | 0.6904 | 5 | 0.6976 |
| 10 | 0.4756 | 10 | 0.7664 | 10 | 0.7446 |
| 15 | 0.5164 | 15 | 0.7921 | 15 | 0.8053 |
| 20 | 0.5435 | 20 | 0.8064 | 20 | 0.8564 |
| 40 | 0.6057 | 40 | 0.8515 | 40 | 0.9934 |
| 60 | 0.6451 | 60 | 0.8963 | 60 | 1.0775 |
| 80 | 0.6683 | 80 | 0.9315 | 80 | 1.163 |
| 100 | 0.6873 | 100 | 0.9651 | 100 | 1.224 |
| 120 | 0.7063 | 120 | 0.9852 | 120 | 1.2525 |
| 140 | 0.717 | 140 | 1.005 | 140 | 1.2836 |
| 160 | 0.7269 | 160 | 1.0242 | 160 | 1.2979 |
| 180 | 0.7269 | 180 | 1.0335 | 180 | 1.2979 |
| 200 | 0.7269 | 200 | 1.0392 | 200 | 1.2979 |
| 220 | 0.7269 | 220 | 1.0392 | 220 | 1.2979 |
| 240 | 0.7269 | 240 | 1.0392 | 240 | 1.2979 |
| 260 | 0.7269 | 260 | 1.0392 | 260 | 1.2979 |
| 280 | 0.7269 | 280 | 1.0392 | 280 | 1.2979 |
| 300 | 0.7269 | 300 | 1.0392 | 300 | 1.2979 |

Table S5. CO2 absorption in Fe2O3-NMP nanosolution in NPs concentration of 0.075wt.% and  at Time t, Pressure P and Temperature T= 308 K.

| t/min | α/mol.kg-1 | t/min | α/mol.kg-1 | t/min | α/mol.kg-1 |
| --- | --- | --- | --- | --- | --- |
| Fe2O3-NMP nanosolution/P= 20bar |  | Fe2O3-NMP nanosolution/P= 30bar |  | Fe2O3-NMP nanosolution/P= 40bar |  |
| 0 | 0 | 0 | 0 | 0 | 0 |
| 5 | 0.36 | 5 | 0.6015 | 5 | 0.6213 |
| 10 | 0.4105 | 10 | 0.6653 | 10 | 0.6934 |
| 15 | 0.4416 | 15 | 0.7073 | 15 | 0.7429 |
| 20 | 0.4712 | 20 | 0.7314 | 20 | 0.8053 |
| 40 | 0.5483 | 40 | 0.7986 | 40 | 0.9176 |
| 60 | 0.5916 | 60 | 0.8358 | 60 | 1.022 |
| 80 | 0.6245 | 80 | 0.8718 | 80 | 1.0953 |
| 100 | 0.6479 | 100 | 0.9096 | 100 | 1.1715 |
| 120 | 0.6675 | 120 | 0.925 | 120 | 1.2088 |
| 140 | 0.6766 | 140 | 0.9445 | 140 | 1.2257 |
| 160 | 0.6875 | 160 | 0.9633 | 160 | 1.2453 |
| 180 | 0.6875 | 180 | 0.9731 | 180 | 1.2453 |
| 200 | 0.6875 | 200 | 0.9779 | 200 | 1.2453 |
| 220 | 0.6875 | 220 | 0.9779 | 220 | 1.2453 |
| 240 | 0.6875 | 240 | 0.9779 | 240 | 1.2453 |
| 260 | 0.6875 | 260 | 0.9779 | 260 | 1.2453 |
| 280 | 0.6875 | 280 | 0.9779 | 280 | 1.2453 |
| 300 | 0.6875 | 300 | 0.9779 | 300 | 1.2453 |

Table S6. CO2 absorption in Fe2O3@glutamine-NMP nanosolution in NPs concentration of 0.01wt.% and  at Time t, Pressure P and Temperature T= 308 K.

| t/min | α/mol.kg-1 | t/min | α/mol.kg-1 | t/min | α/mol.kg-1 |
| --- | --- | --- | --- | --- | --- |
| Fe2O3@glutamine-NMP nanosolution/P= 20bar |  | Fe2O3@glutamine-NMP nanosolution/P= 30bar |  | Fe2O3@glutamine-NMP nanosolution/P= 40bar |  |
| 0 | 0 | 0 | 0 | 0 | 0 |
| 5 | 0.43 | 5 | 0.6395 | 5 | 0.6413 |
| 10 | 0.4734 | 10 | 0.7356 | 10 | 0.7346 |
| 15 | 0.5016 | 15 | 0.7893 | 15 | 0.8369 |
| 20 | 0.5246 | 20 | 0.8315 | 20 | 0.9051 |
| 40 | 0.5981 | 40 | 0.9236 | 40 | 1.064 |
| 60 | 0.643 | 60 | 0.9635 | 60 | 1.146 |
| 80 | 0.6674 | 80 | 1.0033 | 80 | 1.2109 |
| 100 | 0.6895 | 100 | 1.0232 | 100 | 1.2564 |
| 120 | 0.7085 | 120 | 1.0436 | 120 | 1.291 |
| 140 | 0.7215 | 140 | 1.0549 | 140 | 1.3131 |
| 160 | 0.7294 | 160 | 1.0549 | 160 | 1.3131 |
| 180 | 0.7412 | 180 | 1.0549 | 180 | 1.3131 |
| 200 | 0.7412 | 200 | 1.0549 | 200 | 1.3131 |
| 220 | 0.7412 | 220 | 1.0549 | 220 | 1.3131 |
| 240 | 0.7412 | 240 | 1.0549 | 240 | 1.3131 |
| 260 | 0.7412 | 260 | 1.0549 | 260 | 1.3131 |
| 280 | 0.7412 | 280 | 1.0549 | 280 | 1.3131 |
| 300 | 0.7412 | 300 | 1.0549 | 300 | 1.3131 |

Table S7. CO2 absorption in Fe2O3@glutamine-NMP nanosolution in NPs concentration of 0.025wt.% and  at Time t, Pressure P and Temperature T= 308 K.

| t/min | α/mol.kg-1 | t/min | α/mol.kg-1 | t/min | α/mol.kg-1 |
| --- | --- | --- | --- | --- | --- |
| Fe2O3@glutamine-NMP nanosolution/P= 20bar |  | Fe2O3@glutamine-NMP nanosolution/P= 30bar |  | Fe2O3@glutamine-NMP nanosolution/P= 40bar |  |
| 0 | 0 | 0 | 0 | 0 | 0 |
| 5 | 0.4812 | 5 | 0.6972 | 5 | 0.6554 |
| 10 | 0.5201 | 10 | 0.7953 | 10 | 0.7659 |
| 15 | 0.5519 | 15 | 0.8564 | 15 | 0.8649 |
| 20 | 0.5745 | 20 | 0.8856 | 20 | 0.9567 |
| 40 | 0.6512 | 40 | 0.9712 | 40 | 1.116 |
| 60 | 0.6908 | 60 | 1.014 | 60 | 1.2136 |
| 80 | 0.7232 | 80 | 1.054 | 80 | 1.2738 |
| 100 | 0.7452 | 100 | 1.078 | 100 | 1.3075 |
| 120 | 0.7545 | 120 | 1.087 | 120 | 1.3326 |
| 140 | 0.7663 | 140 | 1.105 | 140 | 1.3556 |
| 160 | 0.7768 | 160 | 1.1154 | 160 | 1.3556 |
| 180 | 0.7768 | 180 | 1.1154 | 180 | 1.3556 |
| 200 | 0.7768 | 200 | 1.1154 | 200 | 1.3556 |
| 220 | 0.7768 | 220 | 1.1154 | 220 | 1.3556 |
| 240 | 0.7768 | 240 | 1.1154 | 240 | 1.3556 |
| 260 | 0.7768 | 260 | 1.1154 | 260 | 1.3556 |
| 280 | 0.7768 | 280 | 1.1154 | 280 | 1.3556 |
| 300 | 0.7768 | 300 | 1.1154 | 300 | 1.3556 |

Table S8. CO2 absorption in Fe2O3@glutamine-NMP nanosolution in NPs concentration of 0.05wt.% and  at Time t, Pressure P and Temperature T= 308 K.

| t/min | α/mol.kg-1 | t/min | α/mol.kg-1 | t/min | α/mol.kg-1 |
| --- | --- | --- | --- | --- | --- |
| Fe2O3@glutamine-NMP nanosolution/P= 20bar |  | Fe2O3@glutamine-NMP nanosolution/P= 30bar |  | Fe2O3@glutamine-NMP nanosolution/P= 40bar |  |
| 0 | 0 | 0 | 0 | 0 | 0 |
| 5 | 0.5693 | 5 | 0.8532 | 5 | 0.7166 |
| 10 | 0.6034 | 10 | 0.9024 | 10 | 0.8443 |
| 15 | 0.6253 | 15 | 0.9462 | 15 | 0.9468 |
| 20 | 0.6474 | 20 | 0.9706 | 20 | 1.0224 |
| 40 | 0.7085 | 40 | 1.0443 | 40 | 1.1805 |
| 60 | 0.7471 | 60 | 1.0827 | 60 | 1.2799 |
| 80 | 0.779 | 80 | 1.1047 | 80 | 1.3345 |
| 100 | 0.8021 | 100 | 1.13 | 100 | 1.3745 |
| 120 | 0.8126 | 120 | 1.141 | 120 | 1.3993 |
| 140 | 0.8211 | 140 | 1.1604 | 140 | 1.4149 |
| 160 | 0.8211 | 160 | 1.163 | 160 | 1.4296 |
| 180 | 0.8211 | 180 | 1.1694 | 180 | 1.4385 |
| 200 | 0.8211 | 200 | 1.1694 | 200 | 1.449 |
| 220 | 0.8211 | 220 | 1.1694 | 220 | 1.449 |
| 240 | 0.8211 | 240 | 1.1694 | 240 | 1.449 |
| 260 | 0.8211 | 260 | 1.1694 | 260 | 1.449 |
| 280 | 0.8211 | 280 | 1.1694 | 280 | 1.449 |
| 300 | 0.8211 | 300 | 1.1694 | 300 | 1.449 |

Table S9. CO2 absorption in Fe2O3@glutamine-NMP nanosolution in NPs concentration of 0.075wt.% and  at Time t, Pressure P and Temperature T= 308 K.

| t/min | α/mol.kg-1 | t/min | α/mol.kg-1 | t/min | α/mol.kg-1 |
| --- | --- | --- | --- | --- | --- |
| Fe2O3@glutamine-NMP nanosolution/P= 20bar |  | Fe2O3@glutamine-NMP nanosolution/P= 30bar |  | Fe2O3@glutamine-NMP nanosolution/P= 40bar |  |
| 0 | 0 | 0 | 0 | 0 | 0 |
| 5 | 0.5218 | 5 | 0.8079 | 5 | 0.6779 |
| 10 | 0.5664 | 10 | 0.8573 | 10 | 0.8065 |
| 15 | 0.5884 | 15 | 0.9021 | 15 | 0.9167 |
| 20 | 0.6104 | 20 | 0.9268 | 20 | 0.9835 |
| 40 | 0.6759 | 40 | 1.003 | 40 | 1.1563 |
| 60 | 0.7206 | 60 | 1.049 | 60 | 1.2394 |
| 80 | 0.7462 | 80 | 1.0735 | 80 | 1.2976 |
| 100 | 0.7651 | 100 | 1.0958 | 100 | 1.3376 |
| 120 | 0.7771 | 120 | 1.1065 | 120 | 1.3605 |
| 140 | 0.7869 | 140 | 1.1156 | 140 | 1.3851 |
| 160 | 0.7978 | 160 | 1.1256 | 160 | 1.4043 |
| 180 | 0.7978 | 180 | 1.1336 | 180 | 1.4043 |
| 200 | 0.7978 | 200 | 1.1336 | 200 | 1.4043 |
| 220 | 0.7978 | 220 | 1.1336 | 220 | 1.4043 |
| 240 | 0.7978 | 240 | 1.1336 | 240 | 1.4043 |
| 260 | 0.7978 | 260 | 1.1336 | 260 | 1.4043 |
| 280 | 0.7978 | 280 | 1.1336 | 280 | 1.4043 |
| 300 | 0.7978 | 300 | 1.1336 | 300 | 1.4043 |