Supplementary Information for:

Entanglement of Spin Transition and Elastic Interactions: Manipulating the Slow Spin Equilibrium by Guest-Mediated Fine-Tuning Elastic Frustration

Yuqiao Chai,1 Yu-Ting Yang,1,2 Xing Li,2 Bao Li,3* and Jin-Peng Xue2*

1School of Material and Chemical Engineering, Ningbo University of Technology, Ningbo, Zhejiang, 315211, China.

2School of Materials Science and Chemical Engineering, Ningbo University, Ningbo, 315211, China

3Key Laboratory of Material Chemistry for Energy Conversion and Storage, School of Chemistry and Chemical Engineering, Huazhong University of Science and Technology, Wuhan, Hubei 430074, China

*Correspondence to: xuejinpeng@nbu.edu.cn (J.-P. Xue.); libao@hust.edu.cn (B. Li).

Table of Contents

General Experimental Section 	S4

Synthesis of ligand (1E,2E)-3-phenyl-N-(4H-1,2,4-triazol-4-yl)prop-2-en-1-imine 	S4

Assignation of the guest molecules types in 1·3H2O·3/2CH3OH	S4

Figure S1 | The asymmetric unit of 1·3H2O·3/2CH3OH.	S5

Figure S2 | The asymmetric unit with Q peaks in the pore of framework	S5

Figure S3 | Building units of the title 2D coordination polymer	S6

Figure S4 | Pore structure and supramolecular packing	S6

Figure S5 | Distribution of H2O and CH3OH at different temperatures	S7

Figure S6 | The inferred instability of the framework in pure CH3OH	S7

Figure S7 | The full PXRD patterns during guest exchange	S8

Figure S8 | T-dependent χMT values with various H2O-CH3OH ratios.	S8

Figure S9 | T-dependent χMT values with 5:5 H2O-CH3OH ratio	S9

Figure S10 | T-dependent χMT values with 10:0 H2O-CH3OH ratio	S9

Figure S11 | The enlarged view of the χMT with various H2O-CH3OH ratios	S10

Figure S12 | T-dependent unit-cell volume	S10

Figure S13 | T vs χMT of 10:0 D2O-CH3OH ratio and local enlarged view	S11

Figure S14 | T vs χMT of 5:5 H2O-D2O ratio and local enlarged view	S11

Figure S15 | T vs χMT of D2O, H2O, 5:5 H2O-D2O, 8:2 H2O(D2O)-CH3OH ratios.	S12

Figure S16 | T vs χMT of 8:2 D2O-CH3OH ratio and local enlarged view	S12

Figure S17 | Plot of the guest dependence of γHS	S13

Figure S18 | T vs χMT values of 8:2 H2O-CH3OH ratio starting at 250 K	S13

Figure S19 | The enlarged view of the interval of 140−220 (a) and 60−115 K (b)	S14

Figure S20 | T vs χMT values of 8:2 H2O-CH3OH ratio starting at 300 K	S14

Figure S21 | The enlarged view of the interval of 140−220 (a) and 60−115 K (b)	S15

Figure S22 | T vs χMT values of 10:0 H2O-CH3OH ratio starting at 250 K	S15

Figure S23 | The enlarged view of the interval of 140−220 (a) and 60−115 K (b)	S16

Figure S24 | T vs χMT values of 10:0 H2O-CH3OH ratio starting at 300 K	S16

Figure S25 | The enlarged view of the interval of 140−220 (a) and 60−115 K (b)	S17

Figure S26 | T vs χMT values of 2:8 H2O-CH3OH ratio starting at 250 and 300 K 	S17

Figure S27 | T vs χMT values of 2:8 H2O-CH3OH ratio starting at 395 K	S18

Figure S28 | T vs χMT values of rehydrated sample starting at 250 K	S18

Figure S29 | The temperature-scan rate vs γHS for rehydrated sample	S19

Table S1 | Crystal data and structural refinements	S20

Table S2 | Selected bond lengths and angles at different temperatures	S21

Table S3 | Selected structural parameters at different temperatures	S22

References	S22

General Experimental Section:

Synthesis of ligand (1E,2E)-3-phenyl-N-(4H-1,2,4-triazol-4-yl)prop-2-en-1-imine (prentrz). The ligand prentrz was synthesized by a modified literature procedure1,2.

Assignation of the guest molecules types in the guest-saturated state. Single-crystal X-ray diffraction (SC-XRD) data are utilized to determine the number and type of solvent molecules within the channel-type pore. To eliminate this potential interference, SC-XRD data of the guest-saturated state (1·3H2O·3/2CH3OH) at 150 K is compared with previously published SC-XRD data of the stable state in air (1·9/2H2O) at 150 K (Figure S2). The Q peak in close proximity to the uncoordinated nitrogen atoms of the prentrz ligand is unambiguously assigned as a water molecule (O1).

The residual four Q peaks with heights of 2.5, 5.61, 6.14, and 7.7 were observed in the pore of the framework structure in 1·9/2H2O. These Q peaks, being relatively far from each other, can more reasonably be assigned as water molecules. The relatively high heights of Q peaks may be attributed to a network of hydrogen bonding interactions formed between water guest molecules.

For 1·3H2O·3/2CH3OH, excluding the Q peak identified as O1, the pore is dominated by residual six Q peaks with heights of 2.36, 2.38, 2.87, 3.72, 5.16, and 5.94. The Q peaks located in the middle region of the pore are relatively close to each other, which can be recognized as methanol molecules, or water molecules by means of confinement operation. Given that the SC-XRD data of 1·3H2O·3/2CH3OH are collected in the immersed mixed solution, the Q peaks here are preferred to be assigned as methanol molecules. The relatively low heights of the Q peaks may be due to the presence of methanol molecules disrupting the hydrogen bonding network originally formed by the water molecules, resulting in a weakening of the Q peak heights.

Figure S1. The asymmetric unit of 1·3H2O·3/2CH3OH.

Figure S2. The asymmetric unit of the stable state in air (1·9/2H2O, left) and the guest-saturated state (1·3H2O·3/2CH3OH, right) at 150 K. The Q peaks in the pore of the framework remain unassigned, except for a notable Q peak associated with O1, which has been identified as H2O. The other Q peaks have not been assigned.

Figure S3. Building units of the title 2D coordination polymer.

Figure S4. Pore structure and supramolecular packing of 1·3H2O·3/2CH3OH.

Figure S5. Distribution of H2O and CH3OH in 1·3H2O·3/2CH3OH at 85, 120, 130, 150, 190, and 293 K.

Figure S6. The hypothesized distribution of guest-saturated samples following exchange with CH3OH, H2O, and D2O, and the inferred instability of the framework in pure CH3OH.

Figure S7. The full PXRD patterns of the guest-saturated samples during the guest-exchange process.

Figure S8. Temperature-dependent χMT values of the guest-saturated samples with various H2O-CH3OH ratios.

Figure S9. Temperature-dependent χMT values of the guest-saturated samples with 5:5 H2O-CH3OH ratio at 1 K min-1 (2 K to 250 K).

Figure S10 Temperature-dependent χMT values of the guest-saturated samples with 10:0 H2O-CH3OH ratio at 1 K min-1 (2 K to 250 K).

Figure S11. The enlarged view of the χMT of the guest-saturated samples with various H2O-CH3OH ratios product in the interval of 60−120 K.

Figure S12. Temperature-dependent unit-cell volume of 1·9/2H2O and 1·3H2O·3/2CH3OH.

Figure S13. a, Temperature-dependent χMT values of the guest-saturated samples with 10:0 D2O-CH3OH ratio at 1 and 0.5 K min-1. b, The enlarged view of the χMT product in the interval of 50−110 K.

Figure S14. a, Temperature-dependent χMT values of the guest-saturated samples with 5:5 H2O-D2O ratio at 1 and 0.5 K min-1. b, The enlarged view of the χMT product in the interval of 50−110 K.

Figure S15. a, Temperature-dependent χMT values of the guest-saturated samples with pure D2O, pure H2O and 5:5 H2O-D2O ratio at 1 K min-1. b, Temperature-dependent χMT values of the guest-saturated samples with 8:2 H2O-CH3OH and D2O-CH3OH ratios at 1 K min-1.

Figure S16. a, Temperature-dependent χMT values of the guest-saturated samples with 8:2 D2O-CH3OH ratio at 1 and 0.5 K min-1. b, The enlarged view of the χMT product in the interval of 50−110 K.

Figure S17. Plot of the guest dependence of the HS FeII molar fraction (γHS). The Solv-1/Solv-2 values on the x-axis represent the proportion of the mixed solvents described in the Figures S8-11 and S13-S16.

Figure S18. Temperature-dependent χMT values of the guest-saturated samples with 8:2 H2O-CH3OH ratio at an ambient temperature of 250 K.

Figure S19. The enlarged view of the χMT of the guest-saturated sample with maintaining 8:2 H2O-CH3OH ratio product in the interval of 140−220 (a) and 60−115 K (b).

Figure S20. Temperature-dependent χMT values of the guest-saturated sample with 8:2 H2O-CH3OH ratio after in-situ heating at 300 K for 10 min.

Figure S21. The enlarged view of the χMT of the guest-saturated sample with partial guest losing 8:2 H2O-CH3OH ratio product in the interval of 140−220 (a) and 60−115 K (b).

Figure S22. Temperature-dependent χMT values of the guest-saturated sample with 10:0 H2O-CH3OH ratio at an ambient temperature of 250 K.

Figure S23. The enlarged view of the χMT of the guest-saturated sample with maintaining 10:0 H2O-CH3OH ratio product in the interval of 140−220 (a) and 60−115 K (b).

Figure S24. Temperature-dependent χMT values of the guest-saturated sample with 10:0 H2O-CH3OH ratio after in-situ heating at 300 K for 10 min.

Figure S25. The enlarged view of the χMT of the guest-saturated sample with partial guest losing 10:0 H2O-CH3OH ratio product in the interval of 140−220 (a) and 60−115 K (b).

Figure S26. Temperature-dependent χMT values of the guest-saturated samples with 2:8 H2O-CH3OH ratio. The fresh sample was measured at an ambient temperature of 250 K to start the cooling-warming cycles (1, 2, 5 K min-1, a). Then the sample was warmed up to 300 K and held for 10 min, followed by cooling down to 250 K to measure in the cooling-warming cycles (0.25, 0.5, 1, 2, 4 K min-1, b). c, The temperature-sweep rate vs HS FeII molar fraction (γHS) for the sample with 2:8 H2O-CH3OH ratio starting different ambiences.

Figure S27. Temperature-dependent χMT and γHS values of the guest-saturated samples with the 2:8 H2O-CH3OH ratio under in situ heating at 395 K for 1 hour (the fourth cooling-warming cycle).

Figure S28. Temperature-dependent χMT values of rehydrated sample after heating at 395 K under various scan rates.

Figure S29. The temperature-sweep rate vs HS FeII molar fraction (γHS) for rehydrated sample after heating at 395 K starting at an ambient temperature of 250 K.

Table S1. Crystal data and structural refinements for 1·3H2O·3/2CH3OH.

| 1·3H2O·3/2CH3OH |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Temperature/K | 293 | 190 | 150 | 130 | 120 | 85 |
| Formula | C27.5 H30.5 Fe N12 O4.5 Pd |  |  |  |  |  |
| Mr/g mol-1 | 763.39 |  |  |  |  |  |
| Crystal size/mm | 0.05×0.08×0.03 |  |  |  |  |  |
| Wavelength/Å | 0.77484 |  |  |  |  |  |
| Space group | P1 | P1 | P1 | P1 | P1 | P1 |
| Crystal color | yellow | red | red | red | red | red |
| Crystal system | triclinic | triclinic | triclinic | triclinic | triclinic | triclinic |
| a/Å | 7.4570(15) | 7.2880(15) | 7.2770(15) | 7.2810(15) | 7.2780(15) | 7.2600(15) |
| b/Å | 14.711(3) | 14.504(3) | 14.509(3) | 14.499(3) | 14.500(3) | 14.476(3) |
| c/Å | 15.442(3) | 15.422(3) | 15.381(3) | 15.355(3) | 15.347(3) | 15.344(3) |
| α/ | 104.19(3) | 104.70(3) | 104.67(3) | 104.60(3) | 104.59(3) | 104.57(3) |
| β/ | 99.92(3) | 100.07(3) | 99.99(3) | 99.89(3) | 99.88(3) | 99.87(3) |
| γ/ | 90.28(3) | 90.33(3) | 90.32(3) | 90.32(3) | 90.32(3) | 90.32(3) |
| Volume/Å3 | 1613.5(6) | 1550.4(6) | 1545.1(6) | 1543.3(6) | 1542.0(6) | 1535.6(6) |
| Z | 2 | 2 | 2 | 2 | 2 | 2 |
| Dc / g cm–3 | 1.571 | 1.635 | 1.641 | 1.643 | 1.644 | 1.651 |
| μ / mm–1 | 1.062 | 1.105 | 1.109 | 1.110 | 1.111 | 1.116 |
| F(000) | 775.0 | 775.0 | 775.0 | 775.0 | 775.0 | 775.0 |
| range/° | 2.864 to 50.052 | 2.776 to 50.054 | 2.782 to 50.044 | 2.906 to 50.044 | 2.906 to 50.054 | 2.91 to 50.054 |
| Data/restraints/parameters | 5202/422/424 | 5053/721/424 | 4992/25/424 | 4930/403/424 | 4910/25/424 | 3590/375/400 |
| Goodness-of-fit on F2 | 1.070 | 1.034 | 1.038 | 1.029 | 1.033 | 1.370 |
| Reflections collected | 10053 | 9820 | 9540 | 9249 | 9169 | 5359 |
| R1 [I ≥ 2σ(I)] | 0.0675 | 0.0692 | 0.0699 | 0.0745 | 0.0761 | 0.1307 |
| wR2 [all data] | 0.1997 | 0.1962 | 0.2012 | 0.2148 | 0.2183 | 0.3547 |
| Largest diff. peak and hole/e.Å-3 | 1.89/-1.41 | 1.99/-1.71 | 1.96/-1.66 | 2.34/-2.05 | 2.20/-1.98 | 4.47/-1.92 |

Table S2. Selected bond lengths and angles for 1·3H2O·3/2CH3OH at different temperatures.

|  | 293 K | 190 K | 150 K | 130 K | 120 K | 85 K |
| --- | --- | --- | --- | --- | --- | --- |
| Fe1−N4 | 2.161(6) | 1.981(5) | 1.967(5) | 1.965(6) | 1.972(6) | 1.986(12) |
| Fe1−N5 | 2.156(5) | 1.947(5) | 1.952(6) | 1.946(6) | 1.946(6) | 1.966(14) |
| Fe1−N6 | 2.152(5) | 1.950(5) | 1.950(5) | 1.942(6) | 1.949(6) | 1.943(14) |
| Fe2−N7 | 2.148(5) | 2.146(5) | 2.149(6) | 2.151(6) | 2.152(6) | 2.130(14) |
| Fe2−N8 | 2.177(5) | 2.161(5) | 2.159(6) | 2.157(6) | 2.168(6) | 2.121(14) |
| Fe2−N12 | 2.187(5) | 2.179(5) | 2.175(5) | 2.177(5) | 2.178(6) | 2.164(12) |
| N51−Fe1−N41 | 90.4(2) | 90.3(2) | 89.9(2) | 90.2(2) | 90.2(2) | 91.4(5) |
| N51−Fe1−N4 | 89.6(2) | 89.7(2) | 90.1(2) | 89.8(2) | 89.8(2) | 88.6(5) |
| N5−Fe1−N41 | 89.6(2) | 89.7(2) | 90.1(2) | 89.8(2) | 89.8(2) | 88.6(5) |
| N5−Fe1−N4 | 90.4(2) | 90.3(2) | 89.9(2) | 90.2(2) | 90.2(2) | 91.4(5) |
| N62−Fe1−N4 | 88.0(2) | 91.2(2) | 88.9(2) | 91.3(2) | 88.9(2) | 91.4(5) |
| N63−Fe1−N4 | 92.0(2) | 88.8(2) | 91.1(2) | 88.7(2) | 91.1(2) | 88.6(5) |
| N62−Fe1−N41 | 92.0(2) | 88.8(2) | 91.1(2) | 88.7(2) | 91.1(2) | 88.6(5) |
| N63−Fe1−N41 | 88.0(2) | 91.2(2) | 88.9(2) | 91.3(2) | 88.9(2) | 91.4(5) |
| N62−Fe1−N5 | 89.6(2) | 89.8(2) | 89.9(2) | 90.1(2) | 90.0(2) | 89.7(5) |
| N63−Fe1−N5 | 90.4(2) | 90.2(2) | 90.1(2) | 89.9(2) | 90.0(2) | 90.3(5) |
| N63−Fe1−N51 | 89.6(2) | 89.8(2) | 89.9(2) | 90.1(2) | 90.0(2) | 89.7(5) |
| N62−Fe1−N51 | 90.4(2) | 90.2(2) | 90.1(2) | 89.9(2) | 90.0(2) | 90.3(5) |

Symmetry codes: 1 – x, 1 – y, – z; 2 –1 + x, + y, + z; 3 1 – x, 1 – y, – z.

Table S3. Selected structural parameters for 1·3H2O·3/2CH3OH at different temperatures.

| Compound | 1·3H2O·3/2CH3OH |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Parameter | 293 K | 190 K | 150 K | 130 K | 120 K | 85 K |
| <Fe1−N>[a]/Å | 2.156(5) | 1.959(5) | 1.956(5) | 1.951(6) | 1.956(6) | 1.965(13) |
| <Fe2−N>[a]/Å | 2.170(5) | 2.162(5) | 2.161(5) | 2.162(6) | 2.166(6) | 2.138(13) |
| ∑Fe1[b] | 11.2(2) | 6.8(2) | 5.2(2) | 6.4(2) | 5.2(2) | 12.4(5) |
| ∑Fe2[b] | 5.6(3) | 11.72(8) | 12.0(2) | 13.6(2) | 13.2(2) | 14.4(5) |
| dN−O[c] | 2.904(4) | 2.817(3) | 2.822(3) | 2.824(4) | 2.821(3) | 2.850(3) |

[a] The average Fe–N bond lengths (Å);

[b] Octahedral distortion parameters ();

[c] The distance of hydrogen bonds between uncoordinated nitrogen atom of 1,2,4-triazole in the prentrz ligand and oxygen atom of adjacent H2O molecule.

References

- Scott, H. S., Ross, T. M., Moubaraki, B., Murray, K. S. & Neville, S. M. (2013). Spin crossover in polymeric materials using schiff base functionalized triazole ligands. Eur. J. Inorg. Chem. 803-812.

- Xue, J-P., Hu, Y., Zhao, B., Liu, Z-K., Xie, J., Yao, Z-S. & Tao J. (2022). A spin-crossover framework endowed with pore-adjustable behavior by slow structural dynamics. Nat. Commun., 13, 3510.